Status of Diamond Characterization
Maria Hempel
BRIL Meeting
11.03.2014

---
PLT Diamonds
- 19 PLT diamonds
- 2 show irradiated behavior --> sent to Rutgers
- 4(+2?) are not measured yet
- 9 are possible candidates with more or less good measurement results
  - Odp file is attached to indico
- 6 are not recommended to use
- We still need 3 more diamonds for the first 12 diamonds
- Where to get the other 12 diamonds from?

---
Other Diamonds
- 7 (batch 0390) non-metallized diamonds in my office
  - Will send them to GSI
- 6 SC0 diamonds were measured
  - For 2 of them CCE curve and optical measurement is not done yet (today or tomorrow)
  - 2-3 will be sent to GSI
- 2 (batch 0390) were metallized in GSI
  - Expecting them soon in Zeuthen
- 2 (batch 0228) were metallized in GSI
  - Expecting them soon in Zeuthen