## Slide 1: ATLAS CMOS strip sensor Test & Irradiation Programme
Craig Buttar
15th May 2014
craig.buttar@glasgow.ac.uk

## Slide 2: Charge to meeting
● Discuss the testing of incoming CMOS sensors.
● Define the testing procedures including a irradiation and testbeam programme.
● Establish email list
It should identify who will do the work and and available infrastructures and provide detailed testing milestones for the next year.
Focus on devices in hand and pixel test structures

## Slide 3: International CMOS programme: Year 1
Goals
  Signal/Noise; S/threshold, radiation hardness, uniformity within pixels, charge collection efficiency should be measured using small devices in a small number of selected vendors.
Sensor & Readout
  Relevant foundries selected
  HR and HV CMOS processes evaluated with basic devices.
  Bulk and Surface Radiation hardness evaluated
  Hit efficiency evaluated with representative devices, within a pixel
  Charge collection efficiency understood, or close to
  S/N S/T measured to be acceptable
  Boundary electronics architecture understood
  Cut lines, stitching, multi-reticule possibilities evaluated.
  Common read-out selected

## Slide 4: Devices
Now or soon
  TJ180 test structures
    Mainly electronics: transistors, capacitors, resistors
  H35 available early July
    Based on proposed test structures (see backup)
    Limited supply
Basic test structures (H35 & TJ180): available Oct/Nov
  Sensors 3x3 pixels
  Sensors 5x5 pixels with fast amplifier
  Fast amplifier
  “realistic” amplifier
  Electronics test structures
Architectural test structures: available Jan/Feb
  Parallel traces to periphery
  Total length devices
  Test structures
  Some structures in H35 wafers

## Slide 5: Timeline
TJ180 & H360 Available
  From now
Basic submission
  Pixel and readout test structures
  Submit to TJ180 & H35 July/August
  Devices read for testing: Oct/Nov
  First results presented at November ATLAS week
Architectural submission
  Architectural test structures
  Submit to TJ180 & H35
  Devices ready for testing: Jan/Feb
  First results presented at February ITK week
Final report ready May 2015
Irradiations
  CERN PS: Start Sept
  Birmingham: from ~now
  Ljubljana?
Testbeam
  CERN SPS in October
Does architectural submission require input from testing of basic test structures?

## Slide 6: Testing: Current devices: TJ180 test structures
This module contains CMOS devices with different sizes, and different gate and threshold voltage options. Other devices like resistors, FOXFETs, diodes and capacitors have been implemented. The list of devices integrated in the CMOS test structures is the following:
  1.8 V thin oxide transistors, minimum L = 0.18 µm :
  3.3 V thick oxide transistors, minimum L = 0.35 µm :
  Polysilicon resistors (p+ unsilicided) with W = 1 µm and two lengths: 10 µm and 20 µm.
  Field oxide transistors (FOXFETs) to measure radiation effects on inter-device isolation (STI).
  p+ in n-well diodes (typically used in bandgaps)
  Capacitors
  More details in backup slides

## Slide 7: Testing: Current devices: TJ180 test structures
Circuit components, no bulk test structures
Test on probe station
  Or on carrier?
Are probe cards available?
Irradiate up to 600kGy
Interested groups?
Feedback required for next submission?

## Slide 8: Testing current devices: H35
Similar to “basic test structures”

## Slide 9: Testing: basic sensors
3x3 test structures
  Diode structure?
  I-V, C-V
  signal development: evaluate pixel size/fill-factor, drift/diffusion
  Irradiation: n and p
    Upto 2x1015cm-2 neq
    Requires probe station for studies?
  How to measure drift vs diffusion?

## Slide 10: Testing: basic test structures
5x5 pixels with fast amplifiers
  Source/Laser/X-ray
  Mounted on readout board
    Apply bias voltages for pixel and amplifier
    Readout to scope and Alibava/or other readout
  Pulse shape  signal development, CCE, fill-factor
  TCT measurements
  Testbeam measurements
  Irradiation: n and p
    Upto 2x1015cm-2 neq

## Slide 11: Testing: amplifiers
Fast and realistic amplifier test structures
  Measure gain, timewalk
  Irradiate up to 600kGy (also n and p?)
  Test on probe station and/or readout board

## Slide 12: Tasks
Definition of tests and procedures
  TJ180 test structures in hand  already defined?
  H35 test structures (probably similar to other tests)
  3x3 pixels
  5x5 pixels
  Amplifiers and electronics test structures
  (Architectural structures)  Sept?
  Ensure tests can be compared across labs
Design and manufacture of readout boards
  Common for H35 and basic test structures
  Design by mid-June; boards ready mid-July for H35
Irradiation
  Coordinate irradiations: collect samples and distribute to facilities, distribute to labs after irradiation
Testbeam
  Coordinate with ITK TB coordinator to get time on telescope for characterising devices
  Develop TB module
Next 2 weeks

## Slide 13
Backup: Slides from May 6th CMOS meeting

## Slide 14: “Basic” Submission Test Devices
Proposed test circuits:
“Sensor” diodes, 3x3 pixels. Tests: signal development, depletion/capacitance, irradiation. Variation: pixel size, fill factor.
Integrated 5x5 pixels with amplifiers. Tests: depletion, CCE, irradiation. Variation: pixel size, fill factor.
Front-end amplifier without the “sensor” part, but with I/O test pads. Possibly different shaping time. Tests: gain, irradiation, timewalk (?), output matching.
Transistor test structures: gain, threshold matching. (E.g. see P. Pangaud’s GF talk.)

## Slide 15: “Architectural” Submission
Partitioning the available area (assume 5x5 mm2) into 3 sub-sections to investigate the effect of different pixel size. Initially considered 3 sizes: x1, x2, x4.
Part 1: parallel traces to the periphery. Addresses the channel density, pixel size. Can use different timewalk design for different pixels. Can implement traces near pixels to inject external signals (noise susceptibility).

## Slide 16: “Architectural” Submission (2)
Part 2: 2 complete channels with correct total length implemented in a “snaked” geometry. The idea is to test that OR’ing pixels does not cause problems.
Chip periphery should be close to final :
Timing and location information.
Tuning of shaping/thresholds, changing power.
Readout to an FPGA or equivalent.

## Slide 17: Testing Sensors: What would we like to test?
Basic submission :
  Amplifier speed and gain
  Signal quality
  Signal size (drift/diffusion fraction, depletion depth)
  Charge collection Speed (drift/diffusion fraction)
Architectural submission: pixel readout along the strip:
  Cross talk
  Signal quality
General evaluation for both:
  Noise
  Signal Speed
  Depletion Voltage
  Power consumption and its interplay with noise and signal speed
  Temperature dependence
  Radiation hardness
  Pixel size optimization
  Pixel efficiency map?

## Slide 18: What tools ?
Laser
  1064 nm ..
Sources
  55Fe
  90Sr
Test beams
  DESY/CERN/Focused X-rays at Diamond

## Slide 19: Radiation damage studies
What
  X-rays
  Neutrons
  Protons
Where
  Ljubljana, Karlsruhe, Birmingham …
Main issues
  Time for Irradiating & Re-Testing
  SHE Issues

## Slide 20: TJ180 current test structures
  1.1. Device list
This module contains CMOS devices with different sizes, and different gate and threshold voltage options. Other devices like resistors, FOXFETs, diodes and capacitors have been implemented.
The list of devices integrated in the CMOS test structures is the following:
- 1.8 V thin oxide transistors, minimum L = 0.18 µm :
  o W-array of both NMOS (SVt, HVt and Triple-Well SVt) and PMOS (SVt and LVt) of several gate width (to measure the radiation-induced narrow channel effect, and possible lateral leakage currents)
  o L-array of both NMOS (SVt, HVt and Triple-Well SVt) and PMOS (SVt and LVt) of several gate length (to measure possible radiation effect dependencies on gate length)
  o W/L-array of both NMOS (SVt) and PMOS (SVt) of several gate size with constant W/L=10
  o W/L-array of Triple-Well NMOS only of several gate size with constant W/L=600 (for noise measurement).
  o 4 edgeless NMOS with minimum size matching DRC (to measure the radiation effects on the gate oxide only).
- 3.3 V thick oxide transistors, minimum L = 0.35 µm :
  o W-array of both NMOS (SVt, MVt and Triple-Well SVt) and PMOS (SVt) of several gate width (to measure the radiation-induced narrow channel effect, and possible lateral leakage currents)
  o L-array of both NMOS (SVt, MVt and Triple-Well SVt) and PMOS (SVt) of several gate length (to measure possible radiation effect dependencies on gate length)
  o W/L-array of both standard Vt NMOS and PMOS of several gate size with constant W/L=10
  o 4 edgeless NMOS minimum size matching DRC (to measure the radiation effects on the gate oxide only).

## Slide 21: TJ180 current test structures
- Polysilicon resistors (p+ unsilicided) with W = 1 µm and two lengths: 10 µm and 20 µm.
- Field oxide transistors (FOXFETs) to measure radiation effects on inter-device isolation (STI). In particular, 2 FOXFETs with n+ diffusion source and drain and Metal1 gate, 2 FOXFETs with n-well source and drain and polysilicon gate, 2 FOXFETs with n-well source and n+ diffusion drain with Metal1 gate.
- p+ in n-well diodes (typically used in bandgaps). In particular, 2 diodes with same area and very different perimeter very large and very small), to measure the radiation effect on forward-biased diodes and the influence of the STI periphery on the radiation-induced leakage current.
- Capacitors
  o Metal Interface Metal (MIM) in single and stacked configuration. Both capacitors are made by a matrix 960 elements, each one with a size of 5 µm x 5 µm for a total area of 0.24 mm2 (28.0 pF (single), 55.1 pF (double)).
  o n-well accumulation capacitors with thin and thick oxide. Both capacitors are made by a matrix 126 elements, each one with a size of 5 µm x 5 µm for a total area of 0.35 mm2 (28.9 pF (1.8 V), 16.0 pF (3.3 V)).
A voltage overdrive protection for the MOS gate is guarantee by a double diode. The n-well diode (405 µm perimeter and 124 µm2 area) anode is connected to the substrate, the cathode is connected to the MOS gate. The p-well diode (607 µm perimeter and 186 µm2 area) anode is connected to the MOS gate, the cathode to the voltage supply.