## Slide 1
IPN Orsay
Piezo radiation resistance
N. Gandolfo
From an experiment* driven by the following team : M. Fouaidy, G. Martinet, N. Hammoudi, F. Chatelet, A. Olivier, S. Blivet, F. Galet
*M. Fouaidy, G. Martinet, N. Hammoudi, F. Chatelet, A. Olivier, et al.. Radiation hardness tests of piezoelectric actuators with fast neutrons at liquid helium temperature. 2007, pp.20.<in2p3-00148346>

## Slide 2: Piezo radiation resistance
Outline
Introduction
Experimental setup
Measurements of the neutrons fluence
Measurements of electrical parameters
Conclusion

## Slide 3: Piezo radiation resistance
Introduction
Idea : Irradiate piezos with fast neutrons and see what happens.
Tools : Neutrons irradiation facility at the CERI cyclotron (Orléans)
Deuterons beam : Energy ≤ 25 MeV, Current up to 35µA
Collision with a water cooled thick beryllium target
Production of a high neutrons flux with low γ dose (<20%)
Neutrons energy spectrum in the range of 1 to 20 MeV
The total dose of ~1015 n/cm² (10 Years LHC operation) is nearly achieved in 8 hours
Cryostat :
Main dimensions : Inner diameter: 270 mm, Height: 600 mm
Could be operated with Liquid Helium or Liquid Argon
Minimum distance between neutrons source and irradiated component : 80 mm
Piezo actuators (which are not very lucky) :
4 Noliac (from Noliac) : 36x10x10 multilayer low voltage stacks
4 PICMA (from Physik Instrument) : 36x10x10 multilayer low voltage stacks

## Slide 4: Piezo radiation resistance
Experimental setup
The experimental setup was inspired by a previous cryogenic sensors radiation resistance test for LHC*
*Junquera, T., Thermeau, J. P., Amand, J. F., & Casas-Cubillos, J. (1997). Neutron Irradiation Tests of Calibrated Cryogenic Sensors at Low Temperatures. Adv. Cryog. Eng., A, 43(LHC-Project-Report-153), 765-772.
Deutons beam
Be target (3 mm thickness)
Piezos in Al vacuum chamber
LHe Dewar
To acquisition & control system
d (20 to 25 cm)

## Slide 5: Piezo radiation resistance
Measurement of the neutron fluence
Neutron fluence value is obtained by measuring radioactivation of 16 high purity Nickel foils (O.D = 3 mm)
Radiation exposition mean values :
Noliac : 5.3 x1014 n/cm²
PICMA : 2.5 x1014 n/cm²
(Exposure time : 8 hours)
Neutron dose map [for PICMA test] (x1014 n/cm²)
Noliac piezos assembly
PICMA piezos assembly
Nickel foils
Notes: The Activity of high purity Nickel foils is determined by γ rays spectrometry gamma ray of 58Co at 810 keV
LN2 cooled ORTEC Ge-Li detector

## Slide 6: Piezo radiation resistance
Actuator nominal capacitance values from 300 K to 4 K
Noliac : 9 µF  ~1.5 µF (83% drops)
PICMA : 12.5 µF  ~2.7 µF (78% drops)
Electric parameters measurement
Resistance variation Vs Integrated dose
Losses variation Vs Integrated dose
Capacitance variation Vs Integrated dose
PICMA
Noliac
For temperature <100 K : Displacement is proportional to capacitance
Values of parameters prior to exposure to neutrons and after radiation are compared

## Slide 7: Piezo radiation resistance
Conclusion
No significant modification of electromechanical performance of piezoelectric actuators after exposure to fast neutrons fluence up to 7x1014 n/cm² at LHe temperature.
No major damage was observed but negligible performance degradation may be due to aging effect is measured
Weak linear increase of loss factor by up to 10 %
no impact on cryogenic thermal budget
PICMA &NOLIAC piezoelectric actuators suited of use in radiation environment up to fluence ~ 1014 n/cm²