## Slide 1
Session 1 – Materials and Processes
Session 2 – open discussion
Session 3 – cavity production, fabrication, and analysis activities
WG#4 Cavity Fabrication and Preparation- Summary
Conveners: UMEMORI, Kensei (KEK)
MAMMOSSER, John (ORNL)

## Slide 2: WG#4 Session 1-Materials and Processes
Summary:
Gigi Ciovati (Jlab) presented pressure test results on cavities which showed good agreement with mechanical simulation on yielding after heat treatment. Two data was shown: FG 800deg/2h and Medium-purity ingot Nb 1400deg/9h.
  No significant difference in the elastic properties between them.
  Medium-purity ingot Nb has higher yield strength.

## Slide 3
Rogerio Ribas (CBMM) gave an overview of the production process of niobium and bulk ingot materials
  R&D is ongoing ,looking at defining the melting procedures to achieve reproducible RRR ingots
  500 years of niobium available for production
Ganapati Myneni (ISOHIM) gave an overview of the history of large grain cavity fabrication
  Proposes use of reactor grade material for cavity fabrication
  Develop specs for uniform grain proposed

## Slide 4
Rong-Li Geng (Jlab) presented results of a study aimed at identifying and controlling foreign material contamination during fabrication
  Contamination from machining and cleaning process was suspected
  After control of these procedure, less contaminants found and good EB welding achieved.
Alena Prudnikava (uni Hamburg/DESY) presented results from CBP studies on remaining defects
  Scratches and features caused AL2O3 which imbeds during the process at multiple steps
  Refresh of media at last step of CBP reduced defects
  Shearing is evident and process not optimized

## Slide 5
Shigeki Kato (KEK) presented results from a study on VEP non homogenous removal and improving steps
  Top Iris removal much higher due to H2 bubble attack
  Development of Ninja cathode. High speed stirring to improve removal uniformity.
Vijay Chouhan (Marui Galvanizing Co) presented the study using the Ninga cathode to improve uniformity of removal
  Best results (uniform removal) at 50rpm
  Relatively rough equator surface might be due to bubble attack
  Must be optimized for each cavity structure

## Slide 6: WG#4 Session 3 – cavity production, fabrication, and analysis activities
Carlo Pagani (INFN) presented the results from the XFEL 3.9 GHz cavity fabrication and testing results
  Some effort to get PED certification (10 months), causing delays
  Cavity performance was excellent and will now be sent to DESY for module assembly

## Slide 7
Hiroshi Hara (MHI) presented ongoing SRF activities towards cavity mass production
  Prepare dumbbells using of spinning and deep drawing to reduce number of parts is underway
  2 Cell cavity fabricated using improved processes and results were excellent
Grigori Shirkov (JINR) presented activities on the linear collider cavity and hardware production
  Successful development of explosion bonded SS-Ti, Nb-TI-SS joints
  Cavity development work, deep drawing of half cell and EBW, is ongoing

## Slide 8
Masashi Yamanaka (KEK) gave a presentation on hydroforming cavities from seamless tube
  Single cell cavity fabricated and tested with good results 35MV/m
  Some issues still exist with thinning of material at equator to 1.5mm
Kiyohiko Nohara (Shinohara Press Service) presented studies on reducing cost of HOM components
  Press forming method produced best results
  HOM cans and Hooks successfully produced

## Slide 9
Yegor Tamashevich (uni Hamburg/DESY) presented improved methods with second sound detection
  Very successful analysis routine developed, including 3D ray trace simulation, which matched well with thermal mapping
  Success will allow use of less sensors
  Attempt to use this method on a dressed cavity will come next
Stefan Lagotzky (uni Wuppertal) presented statistical model for field emitter activation to estimate electron loading
  New model successfully developed
  Correlation with small samples underway, using measurement by DC field emission scanning microscope

## Slide 10: WG#4 Session 2 – open discussion
XFEL cavity production from industry has been a great success due to DESY’s efforts and preparation. This will be very useful for future projects and therefore some questions of interest relating to QA were presented for open discussion aimed at Lab and Vendor exchange
A big thanks to DESY staff and Ambra Gresele (E. Zanon) for a great discussion!!

## Slide 11
Open Discussion Summary
Q1 -Are the current QA specifications for elliptical cavities adequate, to detailed or just right?
After the learning curve, the detailed specifications were welcomed and very useful
Amount of details were adequate and detailed enough to reduce errors in production
Just Right!!

## Slide 12: Q1a. Where can improvements be made?
All agreed that the fine details on what defects matter are not well understood
Fabricators would benefit from a manual on defect identification for those that really matter for performance
  DESY is working on cataloging defects in connection with RF performance

## Slide 13: Q1b. Is the process of collecting and transferring data adequate, to detailed or just right?
At the beginning there was some problems but after that it worked well
Fabricators are using the data as well to improve performance
Each cavity has 400 documents that are checked at DESY, this can be a challenge to keep production moving but all is working well

## Slide 14: Q1c - Are there areas where specifications are very difficult to meet and what would be a better way?
Some adjustments were made during production to reduce discrepancy reports
Other than that all specifications were met and understood well

## Slide 15: Q2 - What would make the cavity fabrication easier for the vendors and why?
Welding of He jacket could be improved some
DESY, vendors relationship was excellent and this is the reason for the production success
Most important to maintain collaboration between vendor and labs.

## Slide 16: Q3 - From the experience of the processing and assembly, are there areas that if changes were made could reduce risk of failure and improve success?
DESY provided good training and continues to remain a good resource to answer questions and provided support
  Frequent conversations are taking place and this is seen as a good relationship between vendor and customer
  Both have a very open/ sharing relationship