## Slide 1: Design of Aperiodic Multilayers for Broadband Reflectivity Response in the Soft X-ray Regime
Jirawit Ratanapreechachai (Joe)
Under supervision of Dr. Mauro Prasciolu
Group: Multilayer X-ray Optics of Dr. Saša Bajt
Date: 10th September 2014
DESY Summer Student Program 2014

## Slide 2: Introduction: What is a multilayer?
Alternating layers of two materials: spacer and absorber
In the soft X-ray regime, most materials have refractive indices close to unity.
Reflectivity from pure materials is usually very low
Much higher reflectivity obtained by using “multilayer structures”
  Figure: TEM images showing typical periodic multilayer structures

## Slide 3: Introduction: How does a multilayer work?
Reflection from each interface interferes constructively resulting in high reflectivity
Figure: Diagram of a multilayer structure showing the reflections and transmissions at each interface

## Slide 4: Introduction: Periodic VS Aperiodic ?
For periodic multilayers, usually peak bandwidths are small
Figure: Reflectivity simulation for an ideal periodic Mo/Si multilayer (40 bilayers, period = 7.0 nm, ratio = 0.5)
Periodic
Aperiodic

## Slide 5: Introduction: Aperiodic Multilayers
Larger bandwidths are desirable in some applications such as attosecond pulses, x-rays telescopes and focusing optical components
This is achieved by aperiodic multilayers
Figure: Reflectivity simulation for an aperiodic Mo/Si multilayer (20 bilayers, 5-degree incidence angle)

## Slide 6: Methods for Calculation
Fresnel Reflection Coefficient
Recursive calculation

## Slide 7: Interface Imperfections
Interface Diffusion
  Taken into account by inserting an interfacial layer between each pair of materials
Figure: TEM image of a Mo/Si multilayer illustrating the forming of MoSi2 interfacial layers

## Slide 8: Interface Imperfections
Interface Roughness
  Taken into account by multiplying the Fresnel reflection coefficient by
Figure: TEM image of a multilayer structure showing the presence of rough interfaces

## Slide 9: Inverse Problem
Given all the layer thicknesses, calculating the reflectivity as a function of wavelength or incidence angle is easy!
The inverse problem of finding the layer thicknesses from a given reflectance response
No analytic solutions!
Numerical optimization methods
GOAL
Develop MATLAB code to solve the inverse problem.

## Slide 10: Method of Optimization
Figure of merit (FOM) is defined as
Idea is to find the multilayer structure with the smallest possible figure of merit

## Slide 11: Luus-Jaakola Optimization Method
Usually periodic

## Slide 12: Results
Consider only the two extremes
  Mo/Si where only interface diffusion is important
  Sc/Cr where only interface roughness is important
Mo/Si System
Sc/Cr System

## Slide 13: Results: Diffusion
Mo/Si multilayer
  20 bilayers, 5-degree incidence angle
  broadband response between 17-22 nm (R = 20%)
Initial: Periodic

## Slide 14: Results: Diffusion
Mo/Si multilayer
  20 bilayers, 5-degree incidence angle
  broadband response between 17-22 nm (R = 20%)
Optimized: Aperiodic

## Slide 15: Results: Roughness
Sc/Cr multilayer
  200 bilayers, 5-degree incidence angle, 0.3-nm roughness
  broadband response between 4.30-4.42 nm (R = 1.0%)
Initial: Periodic

## Slide 16: Results: Roughness
Sc/Cr multilayer
  200 bilayers, 5-degree incidence angle, 0.3-nm roughness
  broadband response between 4.30-4.42 nm (R = 1.0%)
Optimized: Aperiodic

## Slide 17: Comparison with X-ray Diffraction Measurements

## Slide 18: Thank you for your attention

## Slide 19: Figure of Merit
Mo/Si
Sc/Cr

## Slide 20: Improvements
Calculation time strongly dependent on the number of layers
  Optimized initial structure
  Other numerical optimization methods
No means to find optimized number of bilayers and peak reflectance
Take into account the case when interfaces are both rough and diffuse

## Slide 21: Interface Imperfections: Interdiffusion

## Slide 22: Luus-Jaakola Optimization Method
Start with an initial ‘parent’ design (periodic)
Generate a number of ‘child’ multilayers from random variations of the parent layer thicknesses
The design with the smallest figure of merit becomes the parent for the next iteration
Repeat the process
Reduce the size of the random variations
Obtain a ‘locally’ optimized design

## Slide 23: Interface Imperfections: Roughness
Perfect Interfaces
With Interfacial Roughness
Figure 7: Effects of roughness (Top) and representation of the two types of interface imperfections (Bottom)

## Slide 24: Method of Optimization
Figure of merit (FOM) is defined as
Idea is to find the multilayer structure with the smallest possible figure of merit
Aim to reach the global minimum or at least a sufficiently deep local minimum

## Slide 25: Increasing the peak reflectance
20%
21%
22%
24%

## Slide 26: Methods for Calculation
Fresnel Reflection Coefficient (s-polarization)
Similarly for p-polarization
Recursive calculation
Layer i
Layer i+1
Interface i