## Slide 1: Nitrogen doping of SRF Nb cavities: The diffusion profile
Mario Hilbig
Presentation of summer school project
Supervisor: Alena Prudnikava
Hamburg, 9.10.2014

## Slide 2: Content
  Introduction
  Diffusionprocesses: 1st and 2nd Fick‘s law
  Nb-N: Binary phase system
  Phase growth due to diffusion
  Diffusion profiles for a α-ε-phase system
  Summary

## Slide 3: Introduction I
Quality factor
  , for
The higher the normal conductivity the lower Q0!
Normal conductivity
(6)Padamsee, Hasan ; Knobloch, Jens ; Hays, Tomas: RF Superconductivity for Accelerators. 2. Auflage. New York: Wiley, 2008.
Energy losses

## Slide 4: Introduction II
Investigation
  Diffusion of Nitrogen into Niobium and subsequent removal of skin layer
  Direct after the nitrogen diffusion: Q0 = 1·107 (normal treatment: Q0 = 2·1010)
  After layer removal Q0 became larger (up to 3 times) than achieved with normal treatment
  (1)Nitrogen and argon doping of niobium for superconducting radio frequency cavities: a pathway to highly efficient accelerating structures; A Grassellino1, A Romanenko1, D Sergatskov1, O Melnychuk1, Y Trenikhina2, A Crawford1, A Rowe1, M Wong1, T Khabiboulline1 and F Barkov1 (1: Fermi National Accelerator Laboratory, Batavia, IL 60510, USA. 2: Illinois Institute of Technology, 3300 S Federal St, Chicago, IL 60616, USA.)

## Slide 5: Introduction III
Q depends on layer removal
Physical phenomenon unknown!
What are the phases within the skin layer?
What is the Nitrogen concentration?
  (1) Nitrogen and argon doping of niobium for superconducting radio frequency cavities: a pathway to highly efficient accelerating structures; A Grassellino1, A Romanenko1, D Sergatskov1, O Melnychuk1, Y Trenikhina2, A Crawford1, A Rowe1, M Wong1, T Khabiboulline1 and F Barkov1 (1: Fermi National Accelerator Laboratory, Batavia, IL 60510, USA. 2: Illinois Institute of Technology, 3300 S Federal St, Chicago, IL 60616, USA.)
Cavity 1
Cavity 2
Cavity 3

## Slide 6: Diffusion from N2 atmosphere into solid Nb
1st and 2nd Ficks law (one-dimensional)
Assumptions:
gas atmosphere is an infinite source
incident flux is larger than diffusion flux
solid-halfroom is large against diffusion length
Solution:
Complementary errorfunction
Parameters:
    diffusion coefficient D
    boundary concentration c0 (dependent on Nb-N phase!)
  (3) Reactions of niobium and tantalum with gases at high temperatures and low pressures; E. Fromm and H.Jehn, Max-Planck-Institut für Metallforschung , Institut für Sondermetalle, Stuttgart, West Germany

## Slide 7: Diffusion from N2 atmosphere into solid Nb
Diffusion coefficients and diffusion profiles
D3
Diffusion coefficients are different by different authors!
D1
D2

## Slide 8: Phases of the Nb-N binary system
Binary phase diagrams
α-Nb
β-Nb
γ-Nb
L
L+N2
Nb2N+N2
Nb4N3+N2
NbN+N2
α+β
β+γ
ε-Nb
δ-Nb
Atomic Percent Nitrogen
Temperature °C
Weight Percent Nitrogen
Nb
Superconductive
Not Superconductive
δ
α
β
γ
ε

## Slide 9: Growth of nitride phases due to diffusion
According to Wagner the movement of a phase boundary can be determined by
For every phase is now calculated a single error function where the boundaries in x are determined by the movement
  (2) Nitridation Kinetics of Niobium in the Temperature Range of 873 K to 1273 K; James T. Clenny and Casimir J. Rosa
γ-Nb
β-Nb
α-Nb
Homogeneity range of γ-Nb

## Slide 10: Calculated profile of ε-α-system
Cavity 1
Cavity 3
Cavity 2
T=1000°C, t=60min
T=800°C, t=10min
T=1000°C, t=10min
x [µm]
x [µm]
x [µm]
c [m-3]
c [m-3]
c [m-3]

## Slide 11: Summary
Results
  Approximate nitrogen concentration in skin layer 0,05-0,15%atomic
  α-Nb in skin layer: interstitial N cause improvent of Q0
Calculation of a diffusion profile with all phases?
  Lack of data: Diffusion coefficients for other phases are not available for temperatures of interest
  Layer removal has high uncertainty and peak of Q0 might not be observed
Experiments with real samples to investigate:
  Explore diffusion of nitrogen in niobium in the temperature range 300 - 1000°C
  Investigate formed phases
  Estimate diffusion coefficients for formed phases
  Optimize nitrogen doping treatment providing best Q0-factor

## Slide 12: References
Books and papers
  Nitrogen and argon doping of niobium for superconducting radio frequency cavities: a pathway to highly efficient accelerating structures; A Grassellino1, A Romanenko1, D Sergatskov1, O Melnychuk1, Y Trenikhina2, A Crawford1, A Rowe1, M Wong1, T Khabiboulline1 and F Barkov1 (1: Fermi National Accelerator Laboratory, Batavia, IL 60510, USA. 2: Illinois Institute of Technology, 3300 S Federal St, Chicago, IL 60616, USA.)
  Nitridation Kinetics of Niobium in the Temperature Range of 873 K to 1273 K; James T. Clenny and Casimir J. Rosa
  Reactions of niobium and tantalum with gases at high temperatures and low pressures; E. Fromm and H.Jehn, Max-Planck-Institut für Metallforschung , Institut für Sondermetalle, Stuttgart, West Germany
  Combined Refinement of Diffusion Coefficients Applied on the Nb-C and Nb-N Systems; David Rafaja, Walter Lengauer, Herbert Weisenberger and Manech Joguet
  Hoppe, Bernhard: Mikroelektronik. 2. Herstellungsprozesse für integrierte Schaltungen. Würzburg: Vogel, 1998.
  Padamsee, Hasan ; Knobloch, Jens ; Hays, Tomas: RF Superconductivity for Accelerators. 2. Auflage. New York: Wiley, 2008.

## Slide 13
Thank you for your attention!
Questions?

## Slide 14: Addition: Boundary condition of diffusion flux
Error function:
  At t=0 the slope is infinite at x=0
  Since this leads to a infinite flux
  Since the gas pressure provides only a finite flux,
  this assumption is not satisfied
At which time t is satiesfied?
  ;
  p=1.33 Pa, T=1273 K, M=0,014 kg/mol, Dα, c0ε gives t=1,5 s

## Slide 15: Addition: Quality factor
the ac electric field in the skin layer:
.
In terms of surface resistance:
,
=> The higher the purity of Nb the lower Q0!
RF surface resistance
is a const, depends on material parameters:
- penetration depth, ;
coherence length, ;
Fermi velocity, ;
the mean free path,