## Slide 1: Initial results of Proton irradiated HVStrip1 chip – MB04
B. Todd Huffman for
G.O.R.
(Glasgow, Oxford, RAL groups and also QMUL and Cambridge)

## Slide 2: Reminder of B’ham Radiation and the State of Play
Two chips irradiated.
  MB03 is no longer viable; problem when testing passive pmos structure
  MB04 working and subject of these tests
27 MeV protons
~8.0E+14 n/cm2 for MB04
Device has remained at less than -10 deg. C.
  Most of the time @ -20 deg. C.
  All bias voltages @ -60V

## Slide 3: After Radiation chip very noisy
VNFB = 5
V injected = 60mV
V injected = 150mV
Charge injection plots here 
Ivan explained that one of the set-up DAC’s should be changed. It sets a feedback level in the shaper of the amplifier. (VNBF)

## Slide 4: Also on unirradiated chip – MB01
There are several global DAC’s on HVStrip1 set-up.
Are there any others we should be playing with?
Volts
Volts

## Slide 5: Fe55 on Cold, unannealed MB04
There is clearly a signal here, but the Fe55 peak is hidden inside the noise even when VNFB is reset. Conclusion: Situation is improved, but still noise dominated.

## Slide 6: MIPS attempts
DESY testbeam time – Thanks Marcel Stanitski!!
  March 9-15; 3, 4, and 5 GeV electrons
  MB01 and MB02 placed in beam
  Self-triggered data and small amount of data triggered by the beam.
    R. Plackett, L. Vigani (Ox), J. Dopke (RAL), K. Kanisaukas (Glasgow), K. Hayrapetyan (QMUL)
Cold, 208MBq 90Sr at Cambridge – Thanks Bart Hommels!
  90Sr Source, Scint. & PMT trigger, DUT in between.
  In freezer capable of -45 deg. C. (running @ -40)
  Trigger using a LeCroy Waverunner Scope
    Only scope we found that could do a true dual channel coincidence trigger.
    J. Dopke, T. Huffman, L. Vigani, M. Arratia (Cam.), B. Hommels (Cam.)
Both cases low trigger rates.
  Desy 2-3 Hz
  Cambridge 2-3 per minute.

## Slide 7: @DESY - MB02 Full Pixel Matrix Scan
High Gain Pixel
Low Gain Pixel
Trigger on analogue output at 25mV
1000 events were acquired for each pixel (DAQ rate ≈ 1Hz)
MB02 was not calibrated beforehand, therefore, response presented in volts

## Slide 8: @DESY - Single Pixel Scan
One high gain pixel (4,0) of MB02 was selected for larger number of samples acquisition (3000 events)
Threshold was set 25mV as before
Resulted in more clearly distinguished features on histogram

## Slide 9: MB01 @ DESY & Cambridge
overflows
From fit, MP = 1672±28.0

## Slide 10: @Cambridge Triggered 90Sr Source
Irradiated chip MB04 
DESY chip MB01 unirradiated
Enough Statistics; no obvious MIP maximum visible.
Need more statistics on unirradiated devices. Left one back at Cambridge.
Overflows

## Slide 11: Some thoughts
Difficult to get MIP signals but we are having some success.
The 60V limitation on current Mother Boards is giving us less signal to MIPS than we could have.
    May get 1.4 times MIP signal @ 120V bias.
    Time to start replacing that big capacitor On Mother boards.
If changing VNFB can have such a dramatic effect, what do the other global settings do?
    Any updated documentation available?
MB04’s performance, prior to annealing, is not great.
  No 55Fe peak observed; No MIP maximum seen
    Even @ -40o C.

## Slide 12: Current short-term plans
Bart, Miguel to anneal MB04 – today!
  Collect ~24 hours data on Channels 3,0 and 17,1
Switch back to an unirradiated chip (MB06?)
  Collect high MIP statistics.

## Slide 13: Massive Thanks!
Marcel Stanitzki – DESY
Adrian Bevan, Karen Hayrapetyan – QMUL
Bart Hommels, Miguel – Cambridge
Kestutis Kanisauskas – Glasgow
Luigi Vigani, Richard Plackett – Oxford
Jens Dopke – RAL
A lot accomplished so far, more to do!

## Slide 14: Backup slides

## Slide 15: MB04 @ Cambridge

## Slide 16: DESY fitted distribution to landau

## Slide 17: Re-arrangement of the Setup
Next step was to re-arrange the setup so that DAQ would be triggered by coincidence signal of two scintillators
The objective was partially achieved after multiple alignment with the beam attempts
Trigger rate was very slow (231 events in ≈ 12h)
Scintillators
MB02
MB06
Beam Direction
HV = -60V

## Slide 18: @DESY - Triggered DAQ results
Pixel (4,0) was selected for data acquisition
Events of interest were selected within LabView VI
Threshold of 25mV was still applied for analogue output

## Slide 19: Direct comparison – MB04 (charge injection = 60mV)
Significant decrease in noise!