## Slide 1
An update on measurements
with irradiated CHESS-1 chip
I. Mandić et al.,
Jožef Stefan Institute, Ljubljana, Slovenia

## Slide 2
2e15
5e15
CC, Sr90, large passive array
Large drop of collected charge after 5e15 n/cm2
3 devices
max. neutron fluences: Device 1 - 5e15, Device 2 - 5e15, Device 3 - 1e15

## Slide 3
CC, Sr90, large passive array
Mean charge at 100 V vs fluence for 3 devices

## Slide 4
CC, Sr90, large passive array
5e15
2e15
1e15
Current vs. bias
Low current at low bias for 5e15
Large increase of current and noise above ~ 80 V
breakdown
low noise at lower bias
 what is the capacitance of the pixel array
when substrate material has high resistance?
T = -20 C

## Slide 5
Edge TCT
I-V for PPA09 (9 pixels, 45 um x 100 um) irradiated to 5e15
 no breakdown
 different than large passive array
Φ = 5e15

## Slide 6
Edge TCT
2e15
5e15
Active depth smaller at 5e15 then at 2e15
 acceptor removal finished
 Neff starts to increase with fluence
Depth
Beam direction
Charge, bias = 120 V

## Slide 7
Edge TCT
Charge collection region narrower after 5e15 than after 2e15
 difference between 2e15 and 5e15 not as dramatic as in Sr-90 measurement
Scan across the centre of the pixel

## Slide 8
Neff - effective acceptor concentration
free parameter
Edge TCT
Radiation introduced
deep acceptors:
g ~ 0.02 cm-1
acceptor removal finished at about 2e15. Neff increases at higher fluence
good agreement with E-TCT on HV2FEI4 (by G. Kramberger)
Neff from depleted depth estimated from velocity or charge profiles
 more details in:
10th Trento workshop: http://indico.cern.ch/event/351695/session/4/contribution/4/material/slides/0.pdf
presentation at AUW: https://indico.cern.ch/event/387391/contribution/7/material/slides/
Initial acceptor
removal

## Slide 9
Conclusions:
CC and E-TCT measurements with passive pixels irradiated with neutrons to 5e15
CC with Sr-90:
 large drop of collected charge in the fluence step between 2e15 and 5e15
 large increase of current and noise at high bias voltage
 but low current and low noise at low voltages
E-TCT:
 clearly see that depleted region gets smaller in the step between 2e15 and 5e15
 acceptor removal finished at ~ 2e15 for this material
 good agreement with E-TCT on HV2FEI4
 no large increase in I-V observed in PPA9 (E-TCT) pixel array
drop of CC in Sr-90 measurement is larger than expected from E-TCT
 weighting field after such high fluence (high resistance substrate)?
 some other differences in PPA09 and large passive array?