## Slide 1: Pre-Irradiation HVStripV1 Testing
R. Bates, C. Buttar, K. Kanisauskas, D. Maneuski
ATLAS Strip CMOS Regular Meeting
June 9, 2015

## Slide 2: List of tests done so far
MB06
  Fe-55 scan at -60V bias for all pixels
  Fe-55 scan for pixels (5,0) and (12,0) at bias voltages from -10V to -70V in steps of -10V
  MIP measurements for pixels (5,0) and (12,0) at bias voltages from -10V to -70V in steps of -10V
  Noise measurements for all pixels at -60V bias
MB12
  Fe-55 scan at -60V bias for all pixels
  Fe-55 scan for pixels (5,0) and (17,0) at bias voltages from -10V to -70V in steps of -10V
  MIP measurements for pixels (5,0) and (17,0) at bias voltages from -10V to -70V in steps of -10V
  Noise measurements for all pixels at -60V bias
All measurements were done in environmental chamber at +20°C

## Slide 3: Fe-55 Spectra

## Slide 4: Fe-55 Peak vs. Bias

## Slide 5: Noise Distribution

## Slide 6: Further Steps
Fe-55 measurements being done at -20°C for one high gain and one low gain pixel
Capacitors to be replaced for MB06 and MB12 which would allow to test devices at higher voltages
LabView VI to be developed to log leakage currents of both HVStripV1 chips during irradiation