## Slide 1: HV-CMOS Update
The properties device (HVStripV1) we just irradiated @ Birmingham
B. Todd Huffman
23/06/2015

## Slide 2: MB03 – Response to Fe55 g’s
Biased @ -40 volts
Biased @ -80 volts!!
Channel 2, Row 1
MB01
MB03

## Slide 3: MB03 – Response to Fe55 g’s
Biased @ -40 volts
Biased @ -80 volts!!
Channel 16, Row 0
MB03
MB01
Unfortunately; Appears MB03 is a less performant device.

## Slide 4: MB01 – Pulse Inj. (from Luigi V. earlier)
Bias-dependent gain

## Slide 5: MB03 – Pulse Inj. (Luigi V.)
Bias-dependent gain

## Slide 6: MB03 – Fe55 (Luigi V.)
Relative efficiency vs. Bias

## Slide 7: (Inj. – Fe55)/Inj.
Bias = -80 volts
Histogram of all channels
  comparing difference between gain found using Fe55 or just injecting charge into the input capacitor.
A measure of the input capacitor.

## Slide 8: Status and Plans
MB03 part of successful proton beam run last week
  27 MeV Protons at B’ham
  Currently in dry freezer (2 weeks)
Many more test chips arrive soon!
  AMS CHESS-1
    Chips in hand but small numbers, some irradiated
  TJ CHESS-1
    Two flavors; several different wafer resistivities
  Daughter boards on order – Mother board design nearly complete
Basic chips – Sensor+Amp
  Faster amp
  Several different sensor sizes
Architectural device - final design review July 1
    Full digital processing, 128 ch., 2 cm long 50 mm wide

## Slide 9: Futher quick Slides
Just More slides

## Slide 10: MB03 – Fe55 (Luigi V.)
Relative efficiency vs. Bias

## Slide 11: MB03 – Fe55 (Luigi V.)
Relative efficiency vs. Bias

## Slide 12: MB03 – Fe55 (Luigi V.)
Relative efficiency vs. Bias