## Slide 1: LCLS-II Coupler Challenges
Chris Adolphsen and Nikolay Solyak for the LCLS-II Coupler Team
TTC Meeting
Dec 2, 2015

## Slide 2: Cavity Power Coupler
Use basic DESY/XFEL TTF3 design, but
Shift Qext range higher by shortening antenna 8.5 mm
Improve cooling of warm section so can run up to 7 kW CW with full reflection
Modify waveguide assembly (use flex ring and aluminum WG box) but retain original manual knob antenna positioner
Two vendors (CPI and RI/Thales) will build full 280 coupler order, will receive 16 soon

## Slide 3: Coupler Heating
Inner conductor temperature for 15 kW TW operation for various thicknesses of the warm section inner conductor copper plating
Plating Thickness
Limit to 450 K (bake temp)

## Slide 4: Thicker Copper Plating Qualification
Increase copper plating thickness on warm section inner conductor from 30 um to 150 um
Had 5 ILC sections modified in this way – use for metrology and HTS tests
Cross section of inner conductor bellow in a test section: measure 120-180 um copper thickness variation

## Slide 5: Copper Plating Issues
After plating, the surfaces do not always look pristine as there can be loosely attached particles, blemishes and oxidation. Various methods are used to improve the surface appearance including brushing, Mo wool polishing and glass bead blasting.
The concern is that this can imbed particles in the surface that may come loose later, and that it produces trapped volumes when protrusions are folded over.
Below are SEM photos of various 150 um thick copper plated samples – our preference is not to do post processing
Bellows - Mo wool polished
Bellows - No post processing
Coupon - Bead blasted

## Slide 6: Example Plated Parts

## Slide 7: Value Engineered WG box
Original TTF3 box
designed for sheet-copper soldering
New post-less, radius’d box
designed for aluminum block machining
Pair of New Boxes being used for Coupler Tests
View into Box

## Slide 8: Coupler RF Processing
The coupler fields are generally below its multipacting threshold so it is not clear that RF processing does much other than to bake the coupler in-situ due to the RF heating.
For example, the plot below shows that the vacuum levels are unaffected by large variations in the 30 kW input power at low duty (~ 0.5%) during TW operation of a pair of couplers.
However, will have a least one coupler pair cold tested and rf processed at CW (working with labs to arrange this) before being installed in the cryomodules.

## Slide 9
Temperature Measurements and Simulations
104 K
119 K
126 K
131 K
5.4 K
6.4 K
11 K
9 K
At FNAL HTS, measure various temperatures to infer 5 and 80 K heat loads (from DT across cooling braids) versus rf input power.
Also simulate the coupler operation using the measured thermal intercept temperatures.

## Slide 10
80 K Thermal Connection
Note: In HTS CF100 flange connected to Copper can
HTTP6
XM2
HTTP7

## Slide 11
P5 – 502 Copper Thermal Straps (TAI Inc.)
Calibration at 4-150K
AL5N extension: Calibration at 5-10K (in cryostat)
Chart: Temperature, K
 | Measurements |  | 
P, W | ΔT, K | <T> | K [W/m-K]
2.44 | 9.3 | 11.9 | 4208
4.34 | 14.3 | 15.3 | 4853

## Slide 12
History of coupler test with cavity “ON” resonance regime in AES021 integrated study.
Top plot shows RF power, accelerating gradient and vacuum in warm section of FPC.
Bottom plots show temperature of sensors at 300K, 80K and 5K zones of the coupler.
Longest time constant for 80K zone
300K zone
80K zone

## Slide 13
AES021: 3.6kW; “ON-resonance”
AES027: 4kW; “ON-resonance”
Temperature Maps: Cavity ON-Resonance

## Slide 14
FNAL HTS Coupler Heat Load Results for 3 Cavities
5 K Intercept Heat Load
On Resonance 3D Simulations: tan(delta) = 3e-4, plating RRR = 50, 5.4 K, 104 K and 320 K intercepts at 3.6 kW
80 K Intercept Heat Load
On and Off Resonance
W

## Slide 15: Comparison to XFEL CM Dynamic Heat Loads
The plots below show XFEL measured 4 and 40 K CM heat loads normalized to our coupler simulation results for their couplers (5, 50 and 310 K intercepts) at their average rf power (forward + reflected), in particular, 2.6 kW at 23.6 MV/m
CM Number
CM Number
4 K Normalized Load
40 K Normalized Load

## Slide 16
  Simulated Inner Conductor Temperature
  4 kW, ON-resonance (COMSOL)
Increase Cu plating (inner conductor) 100150um: Tmax=400K; Heat flux to 80K = 28W (worst case with 10% of surface roughness).
Measurement

## Slide 17: Cornell Coupler Test
Cornell HTC tests with modified couplers showed no decrease in Qo when varying the on-resonance input power up to a level comparable to that at LCLS-II for a fixed gradient of 15 MV/m
Pf = 200W
Pf = 2kW
Cooled flanges with He gas lines

## Slide 18: Summary
Have successfully reduced the warm section inner conductor temperature using thicker copper plating.
Reexamined issues of plating surface finish, surface roughness, oxidation and rf processing. Also improved WG box design.
Measurement of the coupler heat loads in HTS is difficult as it requires detailed knowledge of the material thermal properties.
Measured loads are about twice that predicted, XFEL data in better agreement but have large errors.
The coupler dynamic loads are only ~ 20% of total loads at 4 K and 40 K, and have ~ 100% overhead with two cryoplants, so can accommodate larger loads.