## Slide 1: Introduction and Update from last Collaboration Meeting
Hasan Padamsee
Cornell

## Slide 2: Major Workshops Relevant To SRF Technology
FCC Workshops (Washington DC following first one in China)
  Future Circular Collider(s)…CePC…more later
ERL Workshop at BNL
SRF 2015 at Whistler (Sept 2015)
  Much progress on many fronts
LCWS 2015 at Whistler (Nov. 2015)
  Main topic: ILC prospects
  But also CLIC, FCC, Laser-based…
Others…?

## Slide 3: SRF 2015 Conference
SRF enters a Golden Era
Major Accelerators Under Construction or Completion

## Slide 4
SPIRAL-II – France (28 cavities)
  30 MeV, 5 mA protons -> Heavy Ions
HI-ISOLDE – CERN (60 cavities)
FRIB – MSU (340 cavities)
  500 kW, heavy ion beams for nuclear astrophysics
RISP
    400 kW, heavy ion beams for nuclear astrophysics (350 cavities)
Low Beta
ESS – Sweden (150 cavities)
  1 – 2 GeV, 5 MW Neutron Source ESS - pulsed
PIP-II – Fermilab – 800 MV (115 cavities)
  High Intensity Proton Linac for Neutrino Beams
ADS (200 cavities)
  China, India
High Intensity Protons
CEBAF Upgrade - JLAB (80 cavities)
  Upgrade 6.5 GeV => 12 GeV electrons
XFEL – Hamburg (840 cavities)
  18 GeV electrons – for Xray Free Electron Laser – Pulsed)
LCLS-II – SLAC (300 cavities)
  4 GeV electrons –CW XFEL (Xray Free Electron Laser)
Installed Voltage will rise from 7 GeV => 25 GeV
Total ≈ 2500 Nb Cavities,
High Beta

## Slide 5: Basic SRF R&D Progress
Major Advances on the Q-Frontier
Progress in New Materials
  Nb3Sn, gradients increase
Hints of Progress for Nb/on/Cu
  Q-slope coming down

## Slide 6: Advances on the Q-Frontier
Standard Treatment

## Slide 8: Q > 3x1010 at 16 MV/m and 2 K

## Slide 9: Active Nb3Sn Vapor Diffusion Programs
Fermilab
Jefferson Lab
Cornell

## Slide 10: Nb3Sn Recent Results: Cornell Q > 2 x1010 at 2 K and 19 MV/m
Still work to be done for high field applications

## Slide 11: Hints for improvement in Nb/Cu High Power Impulse Magnetron Sputtering (HiPIMS)
Target material is partly ionized
Nb ions reach substrate with a higher energy than magnetron sputtering
Produce high-quality homogeneous films.

## Slide 12: Basic SRF R&D Advances: Funding Limited
Projects
Basic R&D

## Slide 13: Goals for this TTC Workshop
Large number of new projects based on SRF
Exchange information on production of cavities, cryomodules, couplers and tuners to benefit new projects
  Esp LCLS-II, our hosts
Share knowledge and advance understanding of High Q frontier

## Slide 14: How we can help our hosts? With LCLS-II at SLAC

## Slide 15: LCLS-II Challenges
4 GeV, over 550 meters of SC Linac
35 Cryomodules at 1.3 GHz..like XFEL (ILC)
2 Cryomodules at 3.9 GHz
280 Cavities – 16 MV/m (max 18 MV/m)
CW Operation
Aiming for high Q at 2 K (> 2.7 x1010)
Qext is also high 4x107
  need for good microphonics and resonance control
High Power CW coupler
  7 kW full reflection, CW

## Slide 16: Overlapping Benefits to Other Accelerators
Unfortunately we are missing many interested colleagues from the other big US project
  MSU/FRIB low-beta community
  A review is going on at MSU
Other low-beta participants are here
  HI-ISOLDE, CADS, PIP-II…
  RISP project from Korea is another a big low-beta challenge
We hope that those present from low-beta community can fill the gap

## Slide 17: Some Goals for 5 Working Groups
1. High Q
  Better Understanding of why N-doping gives increasing Q vs E
  Better Understanding of magnetic flux expulsion mechanism and optimization
2. Cavities
  Lessons learned from on-going/finished cavity production from XFEL and JLAB => for near-future projects like LCLS-II &…
3. Cryomodules
    Lessons learned from on-going/finished CM productions
4 &5. Input Coupler/Tuner

## Slide 18: Presenters Tasks: Lessons Learned
What did we do well?
What could we improve?
Mistakes to avoid
Problems we could have avoided

## Slide 19: Challenge for Co-Chairs Work Around Human Limitations
Try to penetrate through the fog

## Slide 20: Each Presenter Tends to Give Limited Views of “Reality”
<= I see blanket
<= I see a snake
I see a rope =>

## Slide 21: Co-Chairs Job! Try to find the “true picture” through the fog

## Slide 22: So Hopefully On-Going Projects Can Minimize Natural Tendency to…