## Slide 1: Flux expulsion efficiency for different cavity materials and treatments
Sam Posen
TTC Meeting, SLAC
2 December 2015

## Slide 2: Maintaining High Q0 in Presence of External B Fields
High Q0 can reduce cryogenic costs in high duty factor SRF linacs by tens of millions of dollars
High Q0 in vertical test must be preserved to cryomodule
Significant source of Q0 degradation: flux losses
Bext
  Use of non-magnetic components
  Magnetic shielding/active compensation
Btrap
  Cool through transition with dT/dy (bulk Nb)
  Minimize pinning centers
Rs
  Optimize mean free path
Notes: Even a few mG can have a dramatic effect

## Slide 3: Maintaining High Q0 in Presence of External B Fields
High Q0 can reduce cryogenic costs in high duty factor SRF linacs by tens of millions of dollars
High Q0 in vertical test must be preserved to cryomodule
Significant source of Q0 degradation: flux losses
Bext
  Use of non-magnetic components
  Magnetic shielding/active compensation
Btrap
  Cool through transition with dT/dy (bulk Nb)
  Minimize pinning centers
Rs
  Optimize mean free path

## Slide 4: Minimize Trapping 1: Cool through Tc with dT/dy (bulk Nb)
A. Romanenko et al., Appl. Phys. Lett. 105, 234103 (2014).

## Slide 5: Minimize Trapping 1: Cool through Tc with dT/dy (bulk Nb)
A. Romanenko et al., Appl. Phys. Lett. 105, 234103 (2014).
Clear trend – ΔT necessary for expulsion

## Slide 6: Minimize Trapping 2: Minimize Pinning in SRF-Treated Nb
Surface features:
  Oxides
  Nitrides
  N- or O-rich niobium
  Mechanical damage
  Contamination
Bulk features:
  Grain boundaries
  Dislocations
  Impurities
How important are these to pinning?
Inner surface
Outer surface
Bulk
Notes: Another important question is what qualities are important to pinning? For example, in N-doped niobium, we have surface features like nitrides and N-rich material—how does the pinning strength of these features compare to that of bgrain boundaries and dislocations?

## Slide 7: Previous Studies
Previous studies, e.g.
  Aull, Kugeler and Knobloch, PRSTAB 15, 062001 (2012)
  A. Dhavale et al, Supercond. Sci. Tech., 25, 065014 (2012)
  G. Ciovati, and A. Gurevich, Proc. SRF 2007, TUP13 (2007)
Qualitative trends, but no measurement as a function of thermal gradient, which is crucial
Notes: Before N-doping, so limited understanding of dependence on state of surface
Before understanding that thermal gradient plays an important role in expulsion
Difficult to extract quantitative understanding

## Slide 8: Experimental Considerations
Goal: measure flux trapping as a function of thermal gradient and material treatment
Connection to Rres – Performing study on cavities directly determines required conditions to avoid severely degraded RF performance
Notes: In the last year or two we’ve recognized that cooling through transition with a spatial thermal gradient strongly affects the amount of flux that is trapped

## Slide 9: Measuring Flux Expulsion During Transition
An axial magnetic field on the order of 10 mG is applied during cooldown. Fluxgate magnetometers at the equator measured the magnetic field before BNC and after BSC superconducting transition.
Fluxgate magnetometers
Temperature sensors
Complete trapping: BSC/BNC = 1
Complete expulsion: BSC/BNC ~ 1.8
External field coils
Measurement technique from A. Romanenko et al., Appl. Phys. Lett. 105, 234103 (2014).

## Slide 10: Measuring Flux Expulsion During Transition
Poor expulsion: BSC/BNC ~ 1.1
Good expulsion: BSC/BNC ~ 1.6

## Slide 11: Example of Cavity that Expels Flux Well
Complete Expulsion
Complete Trapping

## Slide 12: Example of Cavity that Expels Flux Poorly (Large Trapping)
Complete Expulsion
Complete Trapping

## Slide 13: Large Survey
Measured many single cell 1.3 GHz cavities
Thermal cycles – start from 15-100 K, cool down to 7 K, warm up
Parasitic measurements on other experiments
22 datasets measured (i.e. treatment then into dewar)

## Slide 14: Quickly Apparent Trend With Batches of AES Cavities
AES Single Cells Batch 1
AES Single Cells Batch 2
Notes: 7:30

## Slide 15: Quickly Apparent Trend With Batch of AES Cavities
AES Single Cells Batch 1
AES Single Cells Batch 2
Notes: Another thing that quickly became apparent is that the first batch tends to grow very large grains after a few cycles of 800 C. Expulsion from large grain material would be similar to what was seen in the sample studies, but the trend with deltaT gives us a much clearer picture of the range of expulsion that is possible for a given cavity depending on cooldown.

## Slide 16: Quickly Apparent Trend With Batch of AES Cavities
AES Single Cells Batch 1
AES Single Cells Batch 2
Large grains?
Dislocations?
Notes: Another thing that quickly became apparent is that the first batch tends to grow very large grains after a few cycles of 800 C. Expulsion from large grain material would be similar to what was seen in the sample studies, but the trend with deltaT gives us a much clearer picture of the range of expulsion that is possible for a given cavity depending on cooldown.

## Slide 17: Previous Studies
Previous sample studies, e.g.
  Aull, Kugeler and Knobloch, PRSTAB 15, 062001 (2012)
  A. Dhavale et al, Supercond. Sci. Tech., 25, 065014 (2012)
No measurement as a function of thermal gradient, but qualitative trend: larger grain material seems to expel better
Notes: Before N-doping, so limited understanding of dependence on state of surface
Before understanding that thermal gradient plays an important role in expulsion
Difficult to extract quantitative understanding

## Slide 18: Other Fine Grain Cavities – Poor Expulsion
Complete Expulsion
Complete Trapping
Poor expulsion observed for other fine grain cavities

## Slide 19: Large Grain Cavity – Strong Expulsion
Complete Expulsion
Complete Trapping
Strong expulsion observed for LG cavity

## Slide 20: Conversion to From Poor to Strong Expulsion
Complete Expulsion
Complete Trapping
1000 C 4 h vastly improves expulsion

## Slide 21: Long Treatment at 800 C
Complete Expulsion
Complete Trapping
After 5 days at 800 C, good expulsion observed in cavity from “Batch 2”

## Slide 22: Long Treatment at 800 C
Complete Expulsion
Complete Trapping
Continued studies needed to optimize furnace treatment using standard 800 C

## Slide 23: Surface Alteration With No Significant Effect on Expulsion
EP vs BCP
Heavy doping
90 C bake
Add’l EP
Outside BCP
120 C bake
N-dope 2/6
Different surface conditions in cavities with similar bulk history: similar expulsion

## Slide 24: Effect on Q vs E
1000 C Bake
Poor expulsion: BSC/BNC ~ 1.1
Good expulsion: BSC/BNC ~ 1.6
AES017 cooled in 10 mG

## Slide 25: Summary
Treating for strong expulsion can reduce requirements for:
  Shielding/active compensation of external fields – Bext
  Sensitivity to trapped flux – Rs(Btrap)
  Cryogenic plant size and power consumption
Experiment: Measure trapped flux as a function of treatment and spatial temperature gradient
  Thermal gradient at transition critical for all preparations
Modification of bulk structure through furnace treatment shows trend of improved flux expulsion
Modification of surface structure shows minimal influence on flux expulsion
Additional studies are required to determine reproducible conditions for strong expulsion of flux (try at 800 C)

## Slide 26: Implications for Achieving High Q0 in Cryomodules
If reduced grain boundary density improves expulsion, path to optimize preparation – furnace treatment, larger ASTM spec for half-cell sheets, ingot LG Nb for sheets
Consistent with high Q0 in LG studies, e.g. W. Singer et al., Phys. Rev. ST-AB, 16, 012003 (2013)
N-doping discovery made on cavity with strong expulsion

## Slide 27: Outlook
Cavity studies – Progressive measurements with 6 hr 800 C furnace treatments
Sample studies – with progressive steps of 6 hr at 800 C, measure:
  Grain size and dislocation content (SEM-EBSD)
  Mechanical properties (tensile test)
  Flux expulsion (small dewar)