## Slide 1: WG1: High Q - Introduction
Alexander Romanenko
TTC Meeting, SLAC
1 Dec 2015

## Slide 2: High Q working group – focus this time
Two recent discoveries enabling high Q motivated a very active effort to reveal the science behind
  Nitrogen doping – DAY1 (Monday)
  Magnetic flux management – DAY 2 (Tuesday)
Focus on underlying science
Presentations fall into two categories:
  Experimental findings
  Theoretical models currently at the table to explain the experiments

## Slide 3: Nitrogen doping: a breakthrough in Q
Standard state-of-the art preparation
This was the highest Q possible up to 2012
Record after nitrogen doping – up to 4 times higher Q!
A. Grassellino et al, 2013 Supercond. Sci. Technol. 26 102001 (Rapid Communication) – highlights of 2013
1.3 GHz
Since the discovery -> developed to production-ready for LCLS-II within the context of high Q collaboration (FNAL/Cornell/Jlab)

## Slide 4: N Doping – small deviation from standard ILC treatment
Example from FNAL 2/6 doping process:
Bulk EP
800 C anneal for 2 hours in vacuum
2 minutes @ 800C nitrogen diffusion
800 C for 6 minutes in vacuum
Vacuum cooling
5 microns EP
Cavity after Equator Welding
EP 140 um
Ethanol Rinse
External 20 um BCP
Short HPR
800C HT Bake
RF Tuning
EP 40 um
Ethanol Rinse
Long HPR
Final Assembly
Long HPR
Helium Tank Welding Procedure
VT Assembly
HPR
HOM Tuning
Ship to DESY
Leak Check
120C bake
XFEL
X
A. Grassellino et al, 2013 Supercond. Sci. Technol. 26 102001 (Rapid Communication)

## Slide 5: “Production” recipe for LCLS-II – 9-cells for prototype cryomodule(s)
Work in collaboration with Jlab and Cornell to demonstrate transfer and validation of best recipe

## Slide 6: Statistics for two doping recipes on 1.3 GHz 9-cells
Data from Cornell/Jlab/FNAL
16 MV/m
2.7e10
Recipe 2/6
Recipe 20/30
<Q>=3.24e10
<Emax>=16.3 MV/m
Emaxmedian=16.5MV/m
Data from FNAL/JLab
<Q>=3.6e10
<Emax>=22.2 MV/m
Emaxmedian=22.8MV/m

## Slide 7: “Reversed” field dependence of RBCS
Rs(T) = RBCS(T)+Rres
A. Grassellino et al, 2013 Supercond. Sci. Technol. 26 102001 (Rapid Communication)
Origin of the anti-Q-slope

## Slide 8: WG1 – High Q – N doping - contributions
We know from the outset that RBCS decreasing with rf field amplitude is underlying the drastic improvement in Q
  what is the physics behind?
Experimental clues: What can we learn from Rres/Rbcs decomposition and fitting? Can we isolate some superconducting parameters which drive the effect?
    A. Palczewski (Jlab)
    D. Gonnella (Cornell)
    M. Checchin (FNAL)
Theoretical models challenged with the particular charge of “what is different about N doping”?
    B. Xiao (BNL)
    A. Gurevich (ODU)
Example of unoptimal doping:
    K. Umemori (KEK)

## Slide 9: Day 2: Magnetic flux management
Flux expelled efficiently
Flux mostly trapped
Same cavity, just cooled differently through 9.2K
2K, 1.3 GHz
A. Romanenko, A. Grassellino, O. Melnychuk, D. A. Sergatskov, J. Appl. Phys. 115, 184903 (2014)

## Slide 10: Magnetic probes reveal the new physics
Full expulsion of the magnetic field should give ~2x higher field at the equator in superconducting state
Fluxgate
magnetometers
Efficient flux expulsion
Poor flux expulsion
H
It turns out the expulsion efficiency can be controlled by the cooldown procedure (fast/slow, uniform or not)
A. Romanenko, A. Grassellino, O. Melnychuk, D. A. Sergatskov, J. Appl. Phys. 115, 184903 (2014)

## Slide 11: Thermal gradient at NC/SC interface is key parameter for flux expulsion
A. Romanenko, A. Grassellino, A. C. Crawford, D. A. Sergatskov, and O. Melnychuk, Appl. Phys. Lett. 105, 234103 (2014)

## Slide 12: WG1 – High Q – Magnetic flux management - contributions
What are the realistic magnetic environments we have to deal with?
  S. Chandrasekharan (FNAL)
We now understand that temperature gradient at the phase front is the main parameter for expulsion, why is it so?
  T. Kubo (KEK)
How does the material itself (bulk and surface) affect the flux expulsion?
  S. Posen (FNAL)
If the flux is trapped, how does its dissipation depend on the material properties (bulk and surface)?
  M. Martinello (FNAL)
What is the possible theoretical description of the observed trapped flux dissipation?
  A. Gurevich (ODU)
  M. Martinello/M. Checchin (FNAL)