## Slide 1: Microwave suppression of nonlinear surface resistance and extended Q(H) rise in alloyed Nb cavities
Alex Gurevich
Old Dominion University,
Department of Physics and Center for Accelerator Science,
Norfolk, VA 23529, USA
TESLA Meeting, SLAC, Dec. 1, 2015
Supported by DOE under grant No. DE-SC0010081

## Slide 2: Outline
What is behind the extended Q(H) rise in Ti or N -doped Nb cavities and what makes
them special: exotic defects, special processing, new SRF physics or else?
Counterintuitive suppression of surface resistance by the rf field extending to
100-120 mT – half of the superheating field of Nb!
Effect comes from the tell-known broadening of gap peaks in the density of states by
strong dc or rf currents in the BCS theory.
Quick fixes of the low-field Mattis-Bardeen theory are inadequate. Recently Rs(H)
has been derived from the dynamic nonequilibrium BCS theory which describes
well the experimental data on Ti and N-doped cavities. A.Gurevich, PRL 113, 087001 (2014).
Materials conditions: sharp peaks in the density of states and fewer subgap states:
apparently N or Ti-allowing does the job.
How far can it be extended and can negative Q-slopes be fully reversed without reducing
the breakdown field? If so can it be extended beyond the superheating field of Nb?
S-I optimal Nb dirty layer may extend the Q-rise above the superheating field of Nb
A.Gurevich, AIP Advances, 5, 087001 (2015).

## Slide 3: Extended microwave enhancement of Q(H)
Ti-alloying, JLab
N and Ar alloying, FNAL
A. Grasselino et al, SUST 26, 102001 (2013)
P. Dhakal et al, Phys Rev. ST-AB 16, 042001 (2013)
Dirty layer due to diffusion of N or Ti into a few μm thick layer ( >> λ = 40 nm)
at the surface
Decrease of Rs(B) up to B ≈ 0.5Bc: microwave suppression of surface resistance

## Slide 4: Microwave suppression of Rs is not unique to Nb cavities
350 nm thick YBa2Cu3O7 or Nb
striplines on MgO substrates:
minimum in Rs at 10 kV/m
but no minimum on sapphire
or LaAlO3 …? Surface states or
nonlinear dielectric losses in MgO?
M. Hein et al, APL 80, 107 (2002)
Recent observations on 60 nm
Al striplines @ 5.5 GHz and 0.2 K
P.J. deVisser et al, PRL 112, 047004 (2014)
Earlier observations on Pb and other LTS
A.B. Pippard, Proc. Roy. Soc. 203, 210 (1950)
M. Spiewak, Phys. Rev. 113, 1479 (1959)
Yu.V. Sharvin and V.F. Gantmakher, JETP 12, 866 (1961)
R.L. Richards, Phys. Rev. 126, 912 (1962)
R.T. Lewis, Phys. Rev. 134, A1 (1964)
J.F. Koch and C.C. Kuo, Phys. Rev. 164, 618 (1967)
S. Sridhar and J.E. Mercerau, PRB 43, 203 (1996)
Suppression of Rs(H) by dc or rf field can be:
1. significant but also very sample dependent
2. masked by high radiation and vortex losses
3. Affected by substrates

## Slide 5: What could make Rs(H) to decrease with field?
Mattis-Bardeen formula for the surface resistance in the dirty limit:
In BCS the product λ3Δ is inversely proportional to the superfluid density , Δ2 so:
Here Δ decreases with H because currents break Cooper pairs. Thus, according
to the conventional wisdom, Rs(H) should increases with H proportionally to the
density of thermally-dissociated electrons
Can the microwave suppression of Rs(H) come from the log. (often hidden in the A factor)
in Rs = (Aω2/T)exp(-Δ/kT) ?

## Slide 6: Mattis-Bardeen theory in the dirty limit
In the dirty limit of l < ξ, the relation between the current density J(r) and the electric
field E(r) becomes local:
The reactive conductivity σ2 = 1/ωμ0λ2 accounts for the Meissner effect, and the small
dissipative conductivity σ1 results from thermally-dissociated quasiparticles at hω << kT
At hω  0, the integral diverges. At finite hω, the
divergence is cut off giving the logarithmic factor

## Slide 7: Broadening of gap peaks in N(ε) reduces Rs
Idealized
BCS model
At 1-2 GHz and 2K, we have hf/kT ≈ 10-2, so Rs simplifies to:
Broadened gap
peak and subgap
states in the
Dynes model
Density of states with broadened peaks:
The log. term in Rs results from the singularity
in the BCS density of states (γ = 0) at ε = Δ
No singularity in N(ε) extracted from tunneling exps.
which reveal finite N(ε) at ε < Δ (subgap states)
T. Proslier et al, APL 92, 212505 (2008)
Small broadening of gap peaks
in N(ε) can reduce Rs by 4-5 times

## Slide 8: Current-induced broadening of N(ε) in clean limit
Rocking “tilted” electron spectrum in the
current-carrying rf state, J(t) = J0cost
Superfluid velocity vs(t) = J/nse
J. Bardeen, Rev. Mod. Phys. 34, 667 (1962)
Reduction of the energy gap εg =  - pF|vs|
increases the density of thermally-dissociated
normal electrons, which supposedly increases
Critical pairbreaking velocity vc = Δ/pF
At J > 0, the energy gap εg is no longer equal to Δ
2 - 2vpF
2 + 2vpF
Current-induced broadening of N(ε)
??

## Slide 9: Current-induced broadening in dirty limit
Tunnelinng measurements by Anthore,
Pothier, and Esteve, on a 40 nm Al wire, PRL 90, 127001 (2003)
Broadening of the gap peaks in N(ε) by current was calculated some 50 years ago:
K. Maki, Prog. Theor. Phys. 29, 10; 333 (1963);
in Superconductivity, part 2, ed. R.D. Parks, 1967;
P. Fulde, Phys Rev. 137, A783 (1965)
BCS
at J=0
current
Dynes natural
broadening
at J = 0
N(ε) oscillates between black (H=0) and red (H=Ha) curves
If H > Hc(γ/Δ)3/4 the current-induced broadening takes over:
A poor man prediction of logarithmic decrease of Rs(H)

## Slide 10: Sanity check from experiment
Arrhenius fit of the Ti-doped Jlab data using
the generic formula:
where A(H), U(H) and Ri(H) were measured at
different fields
Take into account rf heating to provide
stable fit in a wide temperature range
Both U and Ri depend weakly on H, but A exhibits a logarithmic decrease, consistent
with the above qualitative consideration

## Slide 11: Can Mattis-Bardeen help us obtain Rs(H) at high fields?
Linear response nonlocal relation for the current density J induced by a weak
magnetic vector potential A
Rs is defined by the exponentially small, out-of-phase dissipative component of J which
must be calculated with big care.
I(ω,R,T) is given by a complicated MB integral which is entirely determined by the
density of states and coherence factors of a clean superconductor.
The effect of impurities is accounted by the factor exp(-R/l)
What if we substitute current-broadened N(ε,J) and the coherence factors into the M-B
I(ω,R,T) to calculate Rs(H) at high fields? B.P. Xiao, C.E. Reece, M.J. Kelly, Physica C490, 26 (2013)
M-B theory cannot be used to calculate the nonlinear response by
inserting field-dependent parameters in the linear conductivity σ1

## Slide 12: Why a quick fix of M-B does not work?
The M-B factorization I(ω,R,T)×exp(-R/l)
only works at very weak fields below few mT:
At high fields current pairbreaking becomes
intertwined with impurity scattering which
affect both N(ε) and the coherent factors
N(ε) in the clean limit is
very different from N(ε) in
the dirty limit
dirty
clean
Problems of calculation of Rs(H)
Go back to BCS and rederive Rs(H) at high fields
Solve nonlinear dynamic BCS equations with
strongly oscillating N(ε) and other parameters
To account nonlinear current pairbreaking and kinetics
of nonequilibrium quasiparticles at strong rf fields
Much more complicated problem than the
low-field M-B linear response

## Slide 13: Nonequilibrium theory in the dirty limit
A(r,t) is the magnetic vector potential,
A.I. Larkin and Yu.N. Ovchinnikov, In Nonequilibrium
Superconductivity, (North Holland, 1986),
W. Belzig, et al Superlatt. & Microstruct. 25, 1251 (1999).
N.B. Kopnin, Theory of Nonequilibrium Superconductivity (2001).
D(t,t’) explicitly depends on both A(r,t) and the impurity mean free path
time-dependent Usadel equation for 4x4 matrix Green’s functions
nonlinear electromagnetic response for slow variations of A(r,t) at low frequencies hν << kT

## Slide 14: Results
Nonlinear conductivity as a function of rf amplitude:
Temporal oscillations of spectral function M(t):
rf driving parameter:
Quasiparticle gap
reduced by current
Δ0 is the SC gap at H =0
Slow temporal and spatial variations of J(x,t):
λ >> ξ and hω << kT.
A.Gurevich, Phys. Rev. Lett 113, 087001 (2014).

## Slide 15: Nonequilibrium superconductivity
BCS
at J=0
current
Dynes natural
broadening
at J = 0
Oscillating rf field causes strongly oscillating density of states N(ε,t) which drives quasi-particles out of equilibrium
Non Fermi-Dirac
distribution function
Temporal oscillations of the quasiparticle
density under strong rf fields
phonon
Cooper pair
dissociated
quasiparticles
at hν << Δ the number of quasiparticles
can only change due to dissociation
and recombination of Cooper pairs
caused by electron-phonon collisions
Do quasiparticles have enough time during
the rf period (1 ns) to absorb a phonon
and recombine at low T?
Oscillating or frozen density of quasiparticles?

## Slide 16: RF power transfer mechanisms
phonon
Cooper pair
dissociated
quasiparticles
phonon-assisted dissociation
and recombination of Cooper pairs
inelastic scattering of quasiparticles
on thermal phonons
Kaplan, Chi, Langenberg, Chang, Jafarey, Scalapino PRB 14, 4854 (1976)
For Nb @ 2K, τr ≅ 400 ns
For Nb @ 2K, τs ≅ 17 ns
changes the number of quasiparticles
does not change the number
of quasiparticles
phonon
e
e
Both processes transfer the absorbed rf power from quasiparticles to the lattice, but
because (τr, τs) >> ν-1 = 0.5 ns (2GHz), electrons cannot effectively transfer power
during the rf period: quasiparticles are overheated with respect to the lattice:
Temperature of electrons T(H) is higher than temperature of the lattice
frozen density of quasiparticles does not change during the rf period

## Slide 17: Field-dependent surface resistance
Integration of the total rf power over the region of the rf
field penetration yields the surface resistance:
Rs depends on the electron temperature T(H) which is determined self-consistently
by the global power balance:
α is determined by multiple mechanisms of the rf power transfer
electron
overheating
diffusion
of heat
Kapitza
which of the three is a
bottleneck?

## Slide 18: Good agreement with experiment
α = 0.91
different values of α
Fast Matlab code to calculate Rs(H)
3-4 fold microwave reduction of σ1(H)
for weak overheating, α < 0.1
Of α = 0.91 used to fit the data indicates
significant electron overheating as only 9%
comes from the phonon heat transfer.
For α = 0.91, the maximum overheating
remains weak even at the breakdown field
where ΔT ≈ 0.17 K
Microwave suppression of Rs (H) is not a
“new BCS”: it can be derived from the
dynamic BCS at low temperatures and
frequencies hf << kT in the dirty limit
1400 C data from P. Dhakal et al,
Phys Rev. ST-AB 16, 042001 (2013)

## Slide 19: Are nonequilibrium effects important in Nb cavities?
Theory with equilibrium
distribution function and
no electron overheating is
not sufficient to explain the
observed microwave
suppression of Rs(H) on
1400 C Ti-alloyed cavities
A lot of poorly understood
physics of nonequilibrium
energy relaxation is hidden
in the parameter α
most likely reduced Hc1 in the dirty limit

## Slide 20: What makes it so dependent on the cavity treatment?
BCS
at J=0
current
Natural
broadening
at J = 0
model
Current-induced broadening of
N(ε) should be stronger than
the “natural” broadening
effect of different treatments
on the subgap states
tunneling measurements
tunneling spectroscopy from P. Dhakal et al, Phys Rev. ST-AB 16, 042001 (2013)
Ti-alloyed high-T heat-treated Nb cavities with
extended Q(H) rise do exhibit much sharper gap
peaks in N(ε) and much less subgap states

## Slide 21: Tuning Rs for weak rf field with parallel dc field
Superimposed parallel strong dc and weak rf fields probe the rf suppression of Rs(H) under equilibrium conditions
H0
Ha
Calculated for different ratios of hν/Δ
Rs(f,H0) tuned
by dc field
AG, PRL 113, 087001 (2014).
Similar to old
calculations of
Rs(H) for the
clean limit
M.P. Garfunkel, Phys. Rev.
173, 516 (1968)

## Slide 22: Can the extended Q(H) rise in N-doped Nb cavities be extended above the superheating field of Nb?
A. Grasselino et al, SUST 26, 102001 (2013)
Hs, Hc1?
Alloyed Nb
film of optimum
thickness
Cavity grade
bulk Nb
A few nm thick
Al2O3 spacer
To combine the extended Q(B) rise and
to reverse the reduction of Hc1 and Hs
Use an optimized Nb bilayer to push
the breakdown field above both
superheating fields up to 250-300 mT
A few μm thick dirty layer at the surface
Increases the GL parameter κ = λ/ξ, and
decreases both Hs and Hc1:
before
after
A. Gurevich, AIP Advances, 5, 017112 (2015)
Possible cure by optimized dirty layer?

## Slide 23: Conclusions
Extended Q(H) rise occurs as N or Ti doping results in a dirty layer with non-suppressed
Tc and Δ at the cavity surface. Penalty of reduced Hc1 and Hs
The microwave suppression of Rs(H) is not unique to Nb cavities: it has been observed
on many other materials.
The effect results from the well-know current-induced broadening of the gap peaks
in the density of states in the BCS theory at hν << kT.
A theory of Rs(H) was proposed based on the solution of time-dependent Usadel
equations of nonequilibrium BCS superconductivity in the dirty limit. Dependence of
Rs(H) on the mean free path at high fields can be different from Rs at low fields
Good agreement with experiments on Ti and N-alloyed Nb cavities
Extended Q(H) rise is facilitated by sharper peaks in the density of states N(ε)
and fewer subgap states. Apparently it is what Ti or N-doping does.
Possibility to extend the extended Q(H) rise beyond the superheating field of Nb
by depositing optimized N-doped Nb multilayers