## Slide 1: Trapped flux dissipation in SRF cavities: experimental results and model
Martina Martinello
TTC Meeting, SLAC
2 December 2015

## Slide 2: Outline
Introduction
Experimental procedure
Trapped flux sensitivity
Consistency of the calculation
Mean free path calculation
Sensitivity vs Mean free path
Trapped flux theoretical model
Conclusions

## Slide 3: Introduction on Sensitivity
Accelerators in CW need very low surface resistance to decrease cryogenic costs
To maintain the ultra-high Q-factors of N-doped cavities it is necessary to reduce the trapped field losses
This losses can be reduced by:
  Minimizing environmental field Bext
  Minimizing trapped field with fast cooldown and bulk material optimization
  Minimizing trapped flux sensitivity

## Slide 4: Previous Results
Slide from D. Gonnella SRF 2015

## Slide 5: Outline
Introduction
Experimental procedure
Trapped flux sensitivity
Consistency of the calculation
Mean free path calculation
Sensitivity vs Mean free path
Trapped flux theoretical model
Conclusions

## Slide 6: Flux Trapping during Cooldown
2
1.5
1
0.5
0
The amount of trapped flux depends on:
external magnetic field ()
flux expulsion ()
No trapped flux when:
      mG
      or
      @ the equator
@ equator:
Simulation with perfect diamagnetic () walls:
Magnetic flux fully expelled
Magnetic flux fully trapped

## Slide 7: Trapped Flux Surface Resistance
At low T (1.5K):
The trapped flux surface resistance can be defined as:
The surface resistance is defined as:
“Intrinsic” residual resistance
Trapped flux surface resistance

## Slide 8: Experimental procedure
In order to estimate
Cavity cooled with of external field
Slow cool-down (
In order to estimate
Cavity cooled in less than (using compensation coils)
OR
Fast cooldown with full expulsion ( if )

## Slide 9: Cavity instrumentation
Helmholtz Coil
3 fluxgates at the equator
3 thermometers:
  Bottom iris
  Equator
  Upper iris

## Slide 10: Outline
Introduction
Experimental procedure
Trapped flux sensitivity
Consistency of the calculation
Mean free path calculation
Sensitivity vs Mean free path
Trapped flux theoretical model
Conclusions

## Slide 11: Trapped Flux Sensitivity
  Trapped flux sensitivity defined how much the cavity dissipate per unit of trapped magnetic field :
  Cavities subject to different surface treatment show different trapped flux sensitivity
N doped
“Air doped”
EP
120C baked

## Slide 12: Sensitivity vs Surface Treatments
Cavity Name | Surface Treatment | m.f.p. (nm) | Rfl/Btr (nW/mG)
AES011 | 2/6 min N2 + EP | 143 | 1.45
AES017 | 2/6 min N2 + EP | 180 | 0.98
AES018 | EP + 30 min He | 400* | 0.71
AES019 | 10 min N2 + EP | 168 | 1.24
ACC002 | 20 min N2 + EP | 50 | 1.96
AES014 | 120C bake | 2* | 0.52
AES009 | 2/6 min N2 + EP @Jlab | 57 | 1.49
AES0017_2 | Additional 2/6 min N2 + EP | 138.6 | 1.39
AES021 | Air 30 min + EP | 19.9 | 0.56
Cavity Name | Surface Treatment | m.f.p. (nm) | Rfl/Btr (nW/mG)
AES011 |  | 143 | 1.45
AES017 |  | 180 | 0.98
AES018 | EP + 30 min He | 400* | 0.71
AES019 |  | 168 | 1.24
ACC002 |  | 50 | 1.96
AES014 | 120C bake | 2* | 0.52
AES009 |  | 57 | 1.49
AES0017_2 |  | 138.6 | 1.39
AES021 |  | 19.9 | 0.56
*m-SR measurement

## Slide 13: Trapped Flux Sensitivity Field Dependence
Sensitivity does have a field dependence
Lightly doped cavities have a smaller field dependence than EP
At high field the sensitivity of N doped might be comparable with EP
M. Martinello, M. Checchin, A. Grassellino, A. Romanenko et Al. in Proceeding of SRF 2015

## Slide 14: Impact of different sensitivity
N-doped
120C baked
1.5K

## Slide 15: Impact of different sensitivity
Btrap=10.8 mG
N-doped
120C baked
120C baked Btrap=10.7mG
1.5K
Sensitivity=0.5 nW/mG

## Slide 16: Impact of different sensitivity
Btrap=10.7 mG
Btrap=10.8 mG
Sensitivity=1.5 nW/mG
N-doped
N-doped Btrap=10.8 mG
120C baked
120C baked Btrap=10.7 mG
1.5K
Sensitivity=0.5 nW/mG

## Slide 17: Outline
Introduction
Experimental procedure
Trapped flux sensitivity
Consistency of the calculation
Mean free path calculation
Sensitivity vs Mean free path
Trapped flux theoretical model
Conclusions

## Slide 18: Consistency of Ro calculation
1.5 K
Cavity cooled in less than (using compensation coils)
OR
Fast cooldown with full expulsion ( if )
In order to estimate
Same results within the measurement uncertainty

## Slide 19: Consistency of the sensitivity calculation
AES009 10mG

## Slide 20: Consistency of the sensitivity calculation
AES009 10mG
AES009 23mG

## Slide 21: Consistency of the sensitivity calculation
AES009 10mG
AES009 23mG
AES017 10mG

## Slide 22: Consistency of the sensitivity calculation
AES009 10mG
AES009 23mG
AES017 10mG
AES017 20mG

## Slide 23: Consistency of the sensitivity calculation
AES009 10mG
AES009 23mG
AES017 10mG
AES017 20mG
AES019 10mG
AES009 10mG
AES009 23mG
AES017 10mG
AES017 20mG
AES019 10mG

## Slide 24: Consistency of the sensitivity calculation
AES009 10mG
AES009 23mG
AES017 10mG
AES017 20mG
AES019 10mG
AES019 20mG

## Slide 25: Outline
Introduction
Experimental procedure
Trapped flux sensitivity
Consistency of the calculation
Mean free path calculation
Sensitivity vs Mean free path
Trapped flux theoretical model
Conclusions

## Slide 26: Mean Free Path Calculation using SRIMP
From frequency vs T (close to Tc) data:
From Q vs T (at low T) data:
The code used for these interpolation find the values of mean free path and energy gap which minimize the errors in both these interpolation.
Matlab SRIMP program used to calculate mean free path:
J. Halbritter, KFK-Extern, 3/70-6 (1970)
N. Valles. Ph. D. Cornell University (2013)
S. Meyers, Proceeding of LINAC 14 (2014) TUPP018

## Slide 27: Outline
Introduction
Experimental procedure
Trapped flux sensitivity
Consistency of the calculation
Mean free path calculation
Sensitivity vs Mean free path
Trapped flux theoretical model
Conclusions

## Slide 28: Sensitivity vs Mean Free Path
The sensitivity of the trapped flux as a function of mean free path has a maximum around
M. Martinello, M. Checchin, A. Grassellino, A. Romanenko et Al. in Proceeding of SRF 2015
Over-doped
Light-doped
EP/BCP
Air-doped
120 C bake

## Slide 29: Sensitivity vs Mean Free Path
The sensitivity of the trapped flux as a function of mean free path has a maximum around
M. Martinello, M. Checchin, A. Grassellino, A. Romanenko et Al. in Proceeding of SRF 2015

## Slide 30: Sensitivity vs Mean Free Path
The sensitivity of the trapped flux as a function of mean free path has a maximum around
M. Martinello, M. Checchin, A. Grassellino, A. Romanenko et Al. in Proceeding of SRF 2015

## Slide 31: Experimental results summary
The sensitivity of the trapped flux as a function of mean free path has a maximum around (“bell-shaped” curve)
Over-doped cavities have higher sensitivity because their mfp fall near the maximum
120C bake and EP cavities have low sensitivity because their mfp is far from the maximum
Most of the cavity losses might be due to static vortex dissipation
Because of the sensitivity field dependence light doped cavities might have same sensitivity as EP cavity at high field

## Slide 32: Outline
Introduction
Experimental procedure
Trapped flux sensitivity
Consistency of the calculation
Mean free path calculation
Sensitivity vs Mean free path
Trapped flux theoretical model
Conclusions

## Slide 33: Model Assumptions
Local vortex description
Non-interacting vortexes
Single flux quantum per vortex
T<<Tc (no T dependent)
Two contributions:
  Static (NC Core)
  Dynamic (Lorentz force)
    Parabolic pinning potential
    Single pinning point per vortex
Magnetic field 100% trapped
M. Checchin, M. Martinello, A. Grassellino, A. Romanenko in Proceeding of SRF 2015

## Slide 34: Local vortex description
z
BRF
RF
λ
2a
J. Bardeen, M.J. Stephen, Phys. Rev. 140, A1197 (1965)
Normal-conducting core of radius
Clean limit:
Dirty limit:
Static dissipation (NC core)
Dynamic dissipation (flux oscillation)
Normal skin effect:
Anomalous skin effect:

## Slide 35: Dynamic Resistance: Vortex Dissipation
During the SC transition the field H is applied to the superconductor of area A. The magnetic field will be 100% trapped creating N vortexes with a single flux quantum φ0 each, and area πa2:
Final formula with static and dynamic contributions:
May be approximated as (pure static contribution):

## Slide 36: Sensitivity vs Mean Free Path Explanation
The smaller the mean free path the smaller the NC core diameter
The NC core diameter does not depend anymore from mfp. The larger the mean free the lower the resistivity
The losses seems governed by the static dissipation of the vortexes which appears to be different in clean and dirty limits
CLEAN LIMIT
DIRTY LIMIT
2a

## Slide 37: Outline
Introduction
Experimental procedure
Trapped flux sensitivity
Consistency of the calculation
Mean free path calculation
Sensitivity vs Mean free path
Trapped flux theoretical model
Conclusions

## Slide 38: Conclusions
The sensitivity as a function of mean free path follow a “bell-shaped” trend with a maximum around
This trend is consistent with both experimental data and model simulation
The dissipations seems governed by the static dissipation: in dirty limit the NC core dimension decreases with mfp while in clean limit the NC core dimension is constant and the resistivity decreases with the mfp
The sensitivity does have a field dependence found experimentally
Lightly N doped cavities might have same sensitivity as EP at high field

## Slide 39: Thank you for your attention

## Slide 40: Back up Slides

## Slide 41: Mean Free Path Calculation
Measurements of frequency vs T close to Tc
Measurements of Q vs T at T<<Tc
The interpolation is done using Halbritter SRIMP code (matlab coversion by Cornell). The parameters of the interpolation are:
                London penetration depth: → fixed
                Critical temperature: → fixed
                Intrinsic coherent length: → fixed
                Mean free path (m.f.p.):
                Energy gap:
                Penetration depth at f0 :
                Residual resistance:
Matlab SRIMP program used to calculate mean free path:
J. Halbritter, KFK-Extern, 3/70-6 (1970)
N. Valles. Ph. D. Cornell University (2013)
S. Meyers, Proceeding of LINAC 14 (2014)