## Slide 1: Development of a quarter-wave coaxial coupler unit for 1.3 GHz TESLA-type SRF cavities
Yi Xie
Fermilab
TESLA Technology Collaboration Meeting 2015
Dec. 2nd 2015

## Slide 2: Outline
Motivation;
  What and why coaxial coupling;
  Previous work;
Our work on coaxial coupling scheme;
  Design and fabrication;
  Superconducting joints;
  Cavity processing and testing results;
Discussions and future work.

## Slide 3: Coaxial coupling scheme
Fields asymmetries and kicks from all couplers

## Slide 4: Different coaxial coupling scheme
To preserve axial symmetry of RF structure in the acceleration channel.
Waveguide-coaxial (Cornell)
Coaxial coupler (FNAL)
Nb-Pb SRF gun (DESY/Jlab)

## Slide 5: Advantages of coaxial coupling
  Preserve field symmetries, no coupler kicks;
  Distance between can be shorter, for ILC cavity, difference is 9 cm, higher real estate gradient;
  Cavity body stay cylindrically symmetric, easy fabrication;
  Better cleaned separately if using flange connections (superconducting joints);

## Slide 6: Jlab-DESY effeorts
Assembly drawing
Parts before assembly
Test results
See P. Kneisel & J. Sekutowicz
PRST-AB 13, 022001 (2010)

## Slide 7: Euclid-Fermilab methods
For Eacc ~ 35 MV/m,
the Hsurf is < 0.15 mT,
Lower enough permitting
Superconducting joints
Quarter-wave

## Slide 8: Flange choice
Test welding with Nb1Zr
  There are two ways to attach coaxial coupler: welded on or detachable using SC joints.
  We choose detachable CF flanges with Nb1Zr material, and RRR300 Nb gaskets.
Temperature rise at the knife edge of Nb1Zr CF

## Slide 9: Qext measurments
  Simulations and room temperature RF measurements
  make sure the coupler provides enough coupling.
Measured and simulated Qext of the quarter-wave coaxial coupler

## Slide 10: HOM damping
  Simulations (HFSS) show coaxial coupler provides required Qext for HOMs .
S21 from FPC to HOM coaxial couplers
A very detailed band calculations (Qext, R/Q) shows that the proposed quarter-wave coupler unit supplied with standard HOM dampers meets the ILC requirements for HOM damping.

## Slide 11: Coupler fabrication
  AES fabricated the coupler unit along with a single-cell PAVAC cavity provided by Fermilab.

## Slide 12: Superconducting joints
When we tighten the bolts,
this gap get down to very thin-one A4 paper thickness probably,
We could face off NbZr Flanges a little bit so we can tighten the bolts more.
First try with Copper seal, then Nb seal.
Not great Nb1Zr knife edge.

## Slide 13: Cavity-coupler unit processing
1. Vacuum Leak Check (with copper);
2. Optical inspection of the cavity and the coupler unit;
3. Thickness measurements;
4. BCP/HPR validation (due to exotic geometry);
5. 120 um BCP ;
6. Pre-bake cleaning/HPR;
7. 600C bake 3 hour;
8. Light BCP (20 um);
9. Installation with niobium seal (SC joint);

## Slide 14: First vertical rf test results
Strong X-ray
1.7K
No quench
Power limit

## Slide 15: Previous baseline Parvac cavity results
Q0
Eacc(MV/m)
2K

## Slide 16: Before and after adding coupler unit

## Slide 17: Conclusions
Achievements;
  Working coaxial coupling unit until 26 MV/m;
  First working SC joints inside a 26 MV/m cavity;
Discussions;
  120 C bake to eliminate multipacting (no working);
  More tests to identify Q loss:multipacting or joint loss;
  Add coupler unit to a 9cell;
Suggestions?

## Slide 18: Acknowledgement
As a SBIR project, we thank the entire Fermilab SRFD department for collaborations.

## Slide 19: Multipacting events