## Slide 1: Performance of LG and FG dressed cavities in XFEL cryomodules
J. Sekutowicz
TTC15 Meeting/SLAC
December 2nd, 2015

## Slide 2
Outline
Introduction
  European XFEL and FLASH
  Cooling procedures
LG prototype cryomodule (XM-3)
    Vertical test at 2K and 1.8K and sp test
    Qo at 2K and 1.8K after the FCD and SCD
FG production cryomodule (XM4)
    Vertical test at 2K and sp test
    Qo at 2K, 1.8K and 1.56K after the FCD and SCD
    Mechanical vibrations and VS stability
Upgrade scenario
    FLASH
Final Remarks

## Slide 3
Layout of the XFEL sc linac
101 cryomodules in total: 17 in the injector section and 84 in the main linac
Each cryomodule houses eight 1.3 GHz 9-cell sc TESLA cavities.
Injector linac 4 cryomodules
3rd harmonic RF section
Booster Linac 12 cryomodules
Undulators
BC2
E=2 GeV
e- gun
E=5MeV
BC1
  Introduction a. European XFEL and FLASH

## Slide 4
Layout of the FLASH facility
7 “old fashion” TESLA-type cryomodules, 56 cavities with old end-groups.
There is space for 8 CMs or even more if we make tunnel longer and re-locate the injector (funding is not clear for this option).
  Introduction a. European XFEL and FLASH

## Slide 5
E-XFEL and FLASH originate from the TESLA collider and therefore they nominally operate (FLASH) and will operate (E-XFEL) in so called short pulse (sp) mode
RF-pulses |  | Max RF DF [%]
Max RF pulse length incl. rise time [µs] | Rep. Rate [Hz] | 
1400 | 10 | 1.40
Both accelerators are based on the SRF technology and thus have potential for much larger DF, up to 100% (cw).
Having additional cw and long pulse modes will allow for more flexibility in the time structure of the photon beams and will make both facilities even more attractive to the users.
  Introduction a. European XFEL and FLASH

## Slide 6
  Introduction b. Cooling procedures
-0.07 K/min
-3 K/min
T
[K]
300
0
Fast cool-down (FCD), which is applied always at CMTB as the first cool-down procedure.

## Slide 7
  Introduction b. Cooling procedures
Slow cool-down (SCD), which up to now was applied at CMTB twice (XM-3 and XM4) to study its impact on Qo.
T
[K]
16
2
13 h at ca. 14K
-0.016 (-0.03) K/min
Diagram shows T measured on LHe vessels vs. time

## Slide 8
  2. LG prototype cryomodule (XM-3) a. Vertical test at 2K and 1.8K and sp test
XM-3 cavities:
7 cavities have cells (not end-groups) made of LG Nb, 1 of FG Nb
All cavities had new HOM feedthroughs.
Chart: XM-3 Cavities, Vertical test at 2K
| 1190000 | 659000 | 365000 | 1190000 | 1930000 | 3170000 | 4690000 | 4600000 | 6130000 | 8380000 | 11900000 | 14400000 | 17600000 | 21600000 | 26200000 | 28200000 | 28900000 | 29400000 | 29900000 | 30400000 | 30700000 | 31100000 | 31400000
AC114 | 22300000000 | 21100000000 | 20100000000 | 22500000000 | 23100000000 | 23900000000 | 23800000000 | 20400000000 | 20400000000 | 21000000000 | 22800000000 | 22800000000 | 23500000000 | 22900000000 | 20900000000 | 18800000000 | 16100000000 | 14000000000 | 11600000000 | 9390000000 | 7760000000 | 6600000000 | 5670000000
AC156 | 23800000000 | 25000000000 | 25100000000 | 24500000000 | 23100000000 | 22000000000 | 20800000000 | 20000000000 | 19400000000 | 19200000000 | 19100000000 | 19000000000 | 18900000000 | 18900000000 | 18600000000 | 18600000000 | 18500000000 | 18100000000 | 17800000000 | 17400000000 | 17300000000
AC146 | 22500000000 | 23700000000 | 24500000000 | 24500000000 | 23200000000 | 21100000000 | 18600000000 | 16900000000 | 16800000000 | 16400000000 | 15800000000 | 15200000000 | 14300000000 | 13700000000 | 13300000000 | 12500000000 | 12200000000 | 11500000000 | 11000000000 | 10800000000
AC154 | 37100000000 | 36700000000 | 33900000000 | 30600000000 | 25700000000 | 23800000000 | 23200000000 | 23400000000 | 23300000000 | 22800000000 | 21500000000 | 20200000000 | 19400000000
AC157 | 20400000000 | 19700000000 | 18900000000 | 18900000000 | 19500000000 | 19500000000 | 19500000000 | 19700000000 | 20200000000 | 20900000000 | 21000000000 | 20200000000 | 17900000000 | 15000000000 | 12900000000 | 11200000000 | 8990000000 | 7500000000 | 5470000000 | 4210000000
AC158 | 29400000000 | 30500000000 | 28700000000 | 25300000000 | 22600000000 | 21200000000 | 20100000000 | 20300000000 | 20700000000 | 20600000000 | 20400000000 | 20300000000 | 19900000000 | 19500000000 | 18800000000 | 18300000000 | 17500000000 | 16500000000
AC151 | 30600000000 | 31300000000 | 31800000000 | 31200000000 | 30600000000 | 28900000000 | 27300000000 | 26300000000 | 25600000000 | 24000000000 | 22100000000 | 19100000000 | 15400000000 | 12000000000 | 9520000000 | 8730000000
AC152 | 26800000000 | 26500000000 | 22400000000 | 20400000000 | 19400000000 | 18700000000 | 17700000000 | 16400000000 | 15500000000 | 14400000000 | 13300000000 | 12300000000 | 11400000000 | 10500000000 | 10200000000 | 10100000000 | 9860000000

## Slide 9
Chart: VT of 4 LG cavities at 1.8K, (XM-3 Cavities)
| 1100000 | 1590000 | 2270000 | 2890000 | 3690000 | 4730000 | 6020000 | 7840000 | 10100000 | 11600000 | 13300000 | 15400000 | 17900000 | 19600000 | 21500000 | 23400000 | 25500000 | 28400000 | 30800000 | 33200000 | 35300000 | 37400000
AC154 | 54900000000 | 58600000000 | 60900000000 | 62000000000 | 63700000000 | 64700000000 | 63500000000 | 62800000000 | 57200000000 | 54700000000 | 51800000000 | 48800000000 | 46300000000 | 45700000000 | 45300000000 | 44200000000 | 42000000000 | 39500000000 | 37400000000 | 32300000000 | 28800000000 | 27000000000
AC155 | 27200000000 | 30500000000 | 34400000000 | 38500000000 | 41100000000 | 43500000000 | 45000000000 | 45000000000 | 43300000000 | 39200000000 | 36600000000 | 34600000000 | 32700000000 | 31200000000 | 29100000000 | 27100000000 | 25300000000 | 23700000000 | 22200000000 | 21300000000 | 19200000000 | 17400000000 | 15700000000 | 13900000000 | 14400000000
AC153 | 28700000000 | 32600000000 | 37300000000 | 42000000000 | 45800000000 | 49100000000 | 51300000000 | 52000000000 | 50500000000 | 46500000000 | 43300000000 | 40600000000 | 38500000000 | 37500000000 | 36200000000 | 34800000000 | 33200000000 | 31400000000 | 30200000000 | 28100000000 | 26100000000 | 24500000000 | 24900000000
AC158 | 36700000000 | 38800000000 | 40300000000 | 42500000000 | 44400000000 | 45400000000 | 42900000000 | 40500000000 | 38400000000 | 35500000000 | 34900000000 | 34900000000 | 34400000000 | 33100000000 | 29200000000 | 27100000000 | 24700000000
  2. LG prototype cryomodule (XM-3) a. Vertical test at 2K and 1.8K and sp test

## Slide 10
XM-3 cavities, sp-test (FCD):
Cavity | Max Eacc [MV/m] | Max oper. Eacc [MV/m] | Operation Limit
C1_114 | 26.1 | 23.2 | X-ray > 10-2 mGy/min
C2_156 | 31.6 | 31.1 | Quench
C3_146 | 40.8 | 40.3 | Quench
C4_154 | 38.5 | 38.0 | Quench
C5_157 | 31.5 | 31.0 | Quench
C6_158 | 38.1 | 37.6 | Quench
C7_151 | 28.1 | 22.7 | X-ray > 10-2 mGy/min
C8_152 | 33.0 | 32.5 | PWR
Gradients
Eacc [MV/m] | 14.1 | 20.0 | 23.5
Pdiss [W] | 0.62(?) | 1.63(?) | 2.77
<Qo> [1010] | 3.45 (?) | 2.7(?) | 2.04
Qo (2K)
  2. LG prototype cryomodule (XM-3) a. Vertical test at 2K and 1.8K and sp test

## Slide 11
  2. LG prototype cryomodule (XM-3) b. Qo at 2K and 1.8K after FCD and SCD
<Qo> summary for XM-3:
Eacc | Mode | <Qo> at 2K FCD | <Qo> at 2K SCD | <Qo> at 1.8K FCD | <Qo> at 1.8K SCD
[MV/m] | - | [1010] | [1010] | [1010] | [1010]
~7.0 | cw | 3.1 | 2.5 (-25%) | 4.7 | 3.3 (-42%)
9.5 | cw | - | - | 4.7 | -
10.1 | lp | 2.6 | - | 4.7 | -
12.0 | lp | 2.4 | - | - | -
13.6 | lp | - | - | 4.4 | -
14.7 | lp | - | - | 4.1 | -
Mode | sp | lp | cw
Max <Eacc> [MV/m] | 33.5 | 14.7 | 9.5
<Eacc> summary for XM-3

## Slide 12
  3. FG production cryomodule (XM4)
XM4- technical remarks
XM4 houses 8 TESLA/XFEL cavities made of polycrystalline Nb.
All HOM couplers are equipped with high conduction feedthroughs.
During tests at AMTF in 2014, four FPCs (Cav# 1, 2, 3, 4) were heavily overheated and burned. This happened due to improper assembly of inner conductors of warm parts . All 4 warm parts have been exchanged.
Two HOM couplers have detuned filters:
Cav#1 HOM2 Qext = 6.9E10
Cav#2 HOM1 Qext = 1.4E10 !!

## Slide 13
  3. XM4 a. Vertical test at 2K and sp test
Chart: VT at 2K
| 2.2400000000000002 | 3.99 | 7.1 | 9.7899999999999991 | 12.2 | 15.1 | 18 | 21 | 23.8 | 26.3 | 28.1 | 29.1 | 30 | 30.8 | 31.4 | 31.6 | 31.7
C1_626 | 19200000000 | 19800000000 | 19400000000 | 18000000000 | 16800000000 | 15600000000 | 14600000000 | 13800000000 | 13100000000 | 12200000000 | 11400000000 | 10600000000 | 9930000000 | 9150000000 | 8450000000 | 8110000000 | 7910000000
C2_607 | 21100000000 | 22800000000 | 22700000000 | 21800000000 | 20500000000 | 18900000000 | 17600000000 | 16500000000 | 15700000000 | 15000000000 | 14300000000 | 13500000000 | 12400000000 | 11300000000 | 10000000000 | 8870000000 | 7590000000 | 6570000000 | 5560000000
C3_556 | 25800000000 | 26000000000 | 23900000000 | 21500000000 | 19600000000 | 18000000000 | 17000000000 | 16000000000 | 15100000000 | 14100000000 | 13000000000 | 12300000000 | 11200000000 | 10300000000 | 9200000000 | 8260000000 | 7420000000 | 6720000000 | 6230000000
C4_597 | 27100000000 | 27800000000 | 24100000000 | 22700000000 | 22200000000 | 19700000000 | 19500000000 | 17200000000 | 15700000000 | 15000000000 | 13300000000 | 11400000000 | 9870000000 | 14300000000 | 13600000000 | 12800000000 | 12900000000
C5_606 | 21600000000 | 23500000000 | 23800000000 | 23300000000 | 22200000000 | 20400000000 | 18900000000 | 17600000000 | 16800000000 | 16000000000 | 15400000000 | 14700000000 | 13700000000 | 12700000000 | 11500000000 | 10200000000 | 8850000000 | 7160000000 | 5790000000
C6_621 | 21300000000 | 20300000000 | 22100000000 | 21600000000 | 20000000000 | 18500000000 | 17000000000 | 15800000000 | 15100000000 | 14200000000 | 13200000000 | 12100000000 | 10700000000 | 9120000000 | 7620000000 | 6410000000 | 5510000000
C7_592 | 22400000000 | 24600000000 | 24900000000 | 24100000000 | 22700000000 | 20900000000 | 19500000000 | 18000000000 | 17100000000 | 16300000000 | 15500000000 | 14800000000 | 13800000000 | 12800000000 | 11600000000 | 10500000000 | 9230000000 | 8140000000 | 7390000000 | 6140000000
C8_594 | 20800000000 | 22500000000 | 22400000000 | 21700000000 | 20500000000 | 19000000000 | 17900000000 | 16900000000 | 16200000000 | 15600000000 | 15000000000 | 14100000000 | 13000000000 | 12000000000 | 10800000000 | 9510000000 | 8250000000 | 6650000000
XM4 cavities:

## Slide 14
  3. XM4 a. Vertical test at 2K and sp test
XM4 cavities: sp test at CMTB (Denis Kostin)
Cavity | Max Eacc [MV/m] | Max oper. Eacc [MV/m] | Operation Limit
C1_0626 | 33.5 | 31.0 | PWR
C2_0607 | 34.8 | 31.0 | PWR
C3_0556 | 31.1 | 30.6 | Quench
C4_0597 | 34.5 | 29.9 | X-ray > 10-2 mGy/min
C5_0606 | 39.0 | 31.0 | PWR
C6_0621 | 24.4 | 23.9 | Quench
C7_0592 | 22.0 | 21.5 | Quench
C8_0594 | 35.1 | 31.0 | PWR
Eacc [MV/m] | 15 | 20.5
<Qo> [1010] | 2.4 | 2.3 (?)
Gradients
Qo(2K)

## Slide 15
Chart: Eacc [MV/m]
| 10.536666666666667 | 3.68 | 5.57 | 7.8 | 12.08 | 13.6 | 15.25 | 14.86
VT <Qo> | 20800000000 | 23600000000 | 23600000000 | 22800000000 | 19600000001 | 19000000002 | 17900000003 | 18100000004
18.06.15, 3M | 27652946859.9034
11-13.06.15, 3M | 35757575756.0076 | 31769230771.0299 | 30452777776.4653 | 29103529411.7843
22.06.15, 11:00, 3M | 26548888889.3421
22.06.15, 15:00, Pickups | 24192654377.1203
24.06.15, 3M | 23735197744.1062
26.06.15, 3M | 28610281926.2797
17-18.10.2015, 3M | 22667090277.1389 | 23834559899.4246 | 26897913720.8611 | 29945269350.577
21.10.2015, 3M | 22558234345.2264
10-21.11.2015, 3M, SCD | 28227522210.7721 | 22084705562.0071
09.11.2015, 3M, SCD | 28801096255.5083
SP mode at CMTB | 24000000000 | 23000000000
cw tests at 2K, FCD & SCD
In most of runs 3 methods (3M) were used to determine Eacc (to minimize an error): Read out of pickups (calibrated the sp mode), {Pin , Qload } for each cavity, and IOT (PIOT*0.95/8).
sp Qo value is too high
cw and sp Qo values agree
No Qo difference for FCD and SCD
21% difference in Qo for FCD and SCD
  3. XM4 b. Qo at 2K, 1.8K and 1.56K after FCD and SCD

## Slide 16
cw tests at 1.8K (FCD & SCD) and 1.56K (SCD). 2K (SCD) for comparison
There is no difference between in Qo for the FCD and SCD at 1.8K.
  3. XM4 b. Qo at 2K, 1.8K and 1.56K after FCD and SCD
Chart: Eacc [MV/m]
| 13.808571428571428 | 8.0887499999999992
23.06.15 , FCD, 1.8K | 37636527515.3225 | 39822152405.8053
24.06.15, FCD, 1.8K | 35049481788.7632
10-21.11.2015, 3M, SCD, 1.8K | 44201982252.1923 | 40699808491.0742
26-27.11.2015, 3M, SCD, 1.56K | 69761307045.5567 | 60461669007.6244 | 58904939533.051
26-27.11.2015, 3M, SCD, 2K | 25788483500.5553 | 28373312389.5955

## Slide 17
Surface resistance vs. T for SCD
  3. XM4 b. Qo at 2K, 1.8K and 1.56K after FCD and SCD
Chart: T [K]
| 1.56 | 1.8 | 2
Rs(at ~7.5 MV/m) | 4.0258e-09 | 6.3575e-09 | 9.9645e-09
Rs(at ~10.5MV/m) | 4.7708e-09 | 6.9042e-09 | 1.0891e-08

## Slide 18
  3. XM4 b. Qo at 2K, 1.8K and 1.56K after FCD and SCD
Eacc | Mode | 2K FCD | 2K SCD | 1.8K FCD | 1.8K SCD | 1.56K SCD
[MV/m] | - | [1010] | [1010] | [1010] | [1010] | [1010]
7-8 | cw | 3 | 2.9 | 4.0 | 4.3 | 6.9
~10 | cw | 2.8 | 2.2 (-21%) | - | 4.1 | 5.9
11-12 | cw | 2.5 | - | - | - | 
13.5 | cw | 2.3 | - | 3.76 | - | 
15 | cw | 2.3 | - | 3.5 | - | 
19 | lp(DF=0.18) | 2.0 | - | - | - | 
<Qo> summary for XM4
Mode | sp | lp | cw
Max <Eacc> [MV/m] | 31.8 | 19 | 15
<Eacc> summary for XM4
?

## Slide 19
  3. XM4 c. Mechanical vibrations and VS stability
2 dominating mechanical vibrations
30Hz and 49Hz
Typical microphonics spectrum observed at CMTB for TESLA/XFEL structures assembled in a XFEL cryomodule.

## Slide 20
Piezo tuner: An Active Noise Cancellation (ANC) with Integral Feedback Controller for slow drifts and RF-feedback were applied for the vector sum stabilization :
Piezo fast tuner with ANC and integral feedback controller
  3. XM4 c. Mechanical vibrations and VS stability
Courtesy R. Rybaniec

## Slide 21
VS amplitude SD= 1E-4
XFEL spec
Phase SD= 0.02°
spec missed by factor of 2
  3. XM4 c. Mechanical vibrations and VS stability
Chart: Eacc [MV/m]
| 5.1100000000000003 | 6.85 | 8.86 | 10.31 | 13.46 | 15.33
 | 0.00025702 | 0.00019706 | 0.00013549 | 0.00013051 | 0.00010721 | 9.5868e-05
sp E-XFEL spec
Example: cw mode, operation at 15MV/m, Qload =1.5E7 for all FPCs, C#2 detuned.

## Slide 22
Summary of LG and FG cavities tests in all 3 operation modes
  4. Upgrade scenario
 | Mode | sp | lp | cw
XM-3 / LG | Max <Eacc> [MV/m] | 33.5 | 14.7* | 9.5*
XM4 / FG | Max <Eacc> [MV/m] | 31.8 | 19 | 15
Demonstrated Gradients
*limit was set at that time for DHL to 16W.
Mode | lp | cw
XM-3 / LG | 4.1E10 @14.7MV/m | 4.7E10 @9.5MV/m
XM4 / FG | 2.0E10 @19MV/m | 2.3E10 / 3.5E10 @15MV/m
Demonstrated Qo in lp/cw operation at 2K and 1.8K

## Slide 23
Summary, cont.:
  4. Upgrade scenario
No quench was observed for cw/lp modes in all conducted tests.
Only one of 32 HOM couplers, which had detuned filter (HOM1, C#2), was causing heating of its end group in cw mode when out-coupled power was >8W. All other 31 operated very stable.
Maximum demonstrated DHL was 71 W in cw mode at ~15 MV/m. Operation was very stable. This proves that the E-XFEL cryomodule helium supply and return system can handle at least 77W dissipation.

## Slide 24
  Three remarks
  We are at the very beginning of the discussion to determine the best upgrade of the FLASH accelerator. Nothing has been decided yet! Funding is unclear.
  It seems, that FLASH can be upgraded both to the higher beam energy and higher duty factors.
  The FLASH upgrade could be seen as a pilot project for the duty factor upgrade of E-XFEL, but it does not mean that the whole concept will be the same for both. The main difference results from the cry-losses budget /CM.
  4. Upgrade scenario a. FLASH

## Slide 25
  One of the possible options:
  All cavities of 7 present CMs will be replaced with new XFEL FG or LG cavities
  One XFEL-like CM will be added
  Present FPCs will be replaced with new XFEL-like FPCs which warm parts will have thicker Cu-coating (LCLS II like) and which Qext will be adjustable in the range from 3E6-3E7.
  New cw-operating RF-sources will be added to the klystrons and new cw-operating electron injector will be implemented.
  4. Upgrade scenario a. FLASH

## Slide 26
  4. Upgrade scenario a. FLASH
Mode Parameter | sp | lp | cw
Max Eacc [MV/m] | 30 |  | 15
DF [%] | 1.4 |  | 100
Beam Energy [GeV] | 1.9 |  | 1
FG: 2K Cryo-losses/CM [W] | 15 (Qo=1E10) |  | 90 (Qo=2.3E10)
LG: 1.8K Cryo-losses/CM [W] | 9.5 (Qo=2E10) |  | 52 (Qo=4.1E10)
Proposed key parameters, based on demonstrated gradients.

## Slide 27
  5. Final remarks
cw and lp tests of the E-XFEL production cryomodule (XM4) prove feasibility of the FLASH upgrade both to higher energy and higher DF.
Demonstrated XM4 gradients, up to 15MV/m in cw mode, make feasible an inexpensive (not necessary an optimal) option of the E-XFEL cw upgrade.
Both LG and FG XFEL cavities demonstrate very high gradients, not only in VTs but also in cryomodules, up to 40MV/m, which are crucial for high beam energies in the nominal sp mode.
Very high Qo, up to 4.7E10@15MV/m@1.8K of the LG cavities demonstrated both in VTs and in cryomodule and their very high maximum gradients, make them very attractive for the FLASH and XFEL upgrades.

## Slide 28
Acknowledgements
I want to express my gratitude to all Colleagues contributing to and supporting the experiments and R&D programs towards cw/lp operation modes:
DESY: V. Ayvazyan, J. Branlard, M. Ebert, J. Eschke, T. Feldmann, A. Gössel, D. Kostin, F. Mittag, W. Merz, W.-D. Möller, C. Müller, R. Onken, D. Reschke, , R. Rybaniec, I. Sandvoss, H. Schlarb, A. Sulimov……
and R. Brinkmann and H. Weise
TUL: W. Cichalewski, A. Piotrowski, K. Przygoda
Thank you for your attention

## Slide 29
Backup

## Slide 30
Time structure of the XFEL nominal electron beam (sp, short pulse operation)
Beam pulse length | ms | 0.65
Repetition rate | Hz | 10
Max. # of bunches per pulse |  | 2700
Min. bunch spacing | ns | 240
Bunch charge | nC | ≤ 1
Beam current | mA | 4.2
Nominal beam DF | % | 0.65
650 µs
100 ms
240 ns
~100 fs
  Backup sp mode

## Slide 31
Backup sp mode
Additional operation modes;
Continuous wave (cw) operation for Eacc ≤ 7 MV/m
Long pulse (lp) operation at Eacc > 7 MV/m with DF ≤ (7/Eacc)2 to keep HL constant
Example of lp operation at Eacc = 14 MV/m with DF up to 25%
≥ 750 ms
frep = 1Hz
~100 fs
1s
≤ 250 ms
10 µs, up to 0.1nc