## Slide 1: Fabrication and evaluation of low RRR large grain single cell cavity
Mechanical Engineering Center, KEK
Masashi YAMANAKA
2015.12.2 TTC Meeting @SLAC

## Slide 2: Objectives and result
H | C | O | N | Fe | Si | Ta | RRR
< 10 | < 30 | < 30 | 10 | 3 | 20 | 1034 | 100
Chemical compositions (unit: ppm) and RRR
Motivation
Reduce the niobium material cost
Approach
Use low RRR cheap niobium
Use sliced ingot sheet
Objectives
Manufacture a single cell cavity
Evaluate the performance
50 mm
Sliced ingot niobium（φ260）
Boundary was traced by felt pen
Material was manufactured by CBMM
1.3 GHz single cell cavity manufacture by CFF at KEK
Cell shape: TESLA-like (end cell)
31
Result of vertical test

## Slide 3: Slicing of niobium ingot
After sawing
After mechanical polishing
After chemical polishing
Mechanical polish*
Multi-wire saw*
(Max. 450 mm available)
I want to omit this process
Saw marks are observed
HF
HNO3
H3PO4
（1：1：2）
* These processes were held at Japanese company outside KEK

## Slide 4: Fabrication
Press forming for cells（Same way to ordinary process）
Crack occurred
Just at surface, no leak
EB welding for equator part
EBW test (plate)
Welding bead across the boundary is smooth (not affected)
Deformation is not uniform due to anisotropy
It is difficult to keep circularity at edge (equator)
Leak check was achieved before trimming edge

## Slide 5: 1-cell cavity made by CBMM niobium
LG takes time to fabricate a cavity comparing with FG
Crack
Sputter
Bead is not uniform

## Slide 6: Vertical test
5 mm
Welding
bead
5 mm
Polishing
inside
1st VT：28 MV/m
2nd VT：23 MV/m
The max. gradient was not improved.
Does the quench occur at another point?
We decided to try one more time.
Inner view at the equator after 1st VT
There are ripple and crater cause quench
Inner view (same position to left) after polishing. Well removed.

## Slide 7: Vertical test2
Finish by hand polishing
We could not detect the quench or heat sources by inspection
5 mm
5 mm
2nd VT：23 MV/m
3rd VT：31 MV/m
To polish widely around heated point
Example of polishing (before)
(position: between iris and equator)
Boundary is observed (it is not a defect)
After polishing (same position to left)
It became smooth as we cannot observe
the boundary clearly
The max. gradient was improved.
We needed 3 times VT
including EP, inspection, repairing ….
It means high cost

## Slide 8: Comparison with high RRR niobium
Fine grain (TD)
Large grain (TD)
42
36
31
 | H | C | O | N | Fe | Si | Ta | RRR
LG (TD) | < 5 | < 10 | < 10 | < 10 | < 10 | < 10 | 80 | 390*
FG (TD) | < 10 | 40 | 100 | 40 | 20 | 20 | 700 | 258**
LG (CBMM) | < 10 | < 30 | < 30 | 10 | 3 | 20 | 1034 | 100*
Measurement RRR: * by KEK, ** by TD
The effect of low RRR and high Ta is not separated here.

## Slide 9: Summary and acknowledgement
A single cell cavity using low RRR large grain niobium was fabricated and evaluated. The gradient attained to 31 MV/m.
3 times VT and repairing inside with inspection were required to get high gradient. It becomes the reason of high cost.
LG takes time to fabricate a cavity comparing with FG.
The effect of Low RRR and high Ta is not separated here.
φ260×500 niobium ingot was provided by CBMM
Ta
RRR