## Slide 1
ULVAC Inc.
Tomohiro Nagata, Hiroaki Masui, Noriyuki Abe,
Seiichi Shinozawa, Hirohiko Murakami
KEK
Masashi Yamanaka, Hitoshi Inoue, Eiji Kako
Production of High Purity
Niobium for SRF Accelerators

## Slide 2: About ULVAC
Vacuum Equipments
Vacuum Pump
Materials
Vacuum Technology

## Slide 3: Products for SRF accelerators
600kW EB melting furnace
Nb ingot
Nb sheets:
Nb tubes:
RRR > 300
For welding-type cavities
For seamless cavites
For beam tubes
ULVAC can produce
high-purity Nb ingots

## Slide 4: Manufacturing scheme
RRR
Mechanical
Chemical
Deforming
Machining
Annealing
Forging
Evaluation
Refining
Recycle
Consistently integrated production
We can supply various shape and size
as you like.
Comparable with
KEK measurements

## Slide 5: Collaborative cavity development
Nb Ingot
RRR>300
Vertical Test
Large tube
Small tube
Disk
Parts supply
Forming
Seamless cavity
Beam tube
Half cell
Welding
Polish
Rinse
Assembly

## Slide 6: Welding type 1-cell cavity
Nb Ingot
RRR>300
Vertical Test
Large tube
Small tube
Disk
Seamless cavity
Beam tube
Half cell
Welding
Polish
Rinse
Assembly
Forming
Parts supply
Can be used our Nb materials for SRF accelerators?

## Slide 7: Welding type 1-cell cavity
 | H | O | N | C | Zr | Fe
ASTM Type5 | 5 | 40 | 30 | 30 | 100 | 50
ULVAC | 1 | <10 | <10 | 10 | <10 | <10
 | Si | W | Ni | Ti | Al | Ta
ASTM Type5 | 50 | 70 | 30 | 50 | 50 | 1000
ULVAC | <10 | 10 | <10 | <5 | <10 | 140
Chemical components (for Ingot)
Property confirmation
 | Ultimate Tensile Strength (MPa) | Yield Strength (MPa) | Elongation (%)
ASTM Type5 | >95 | >50 | >30
ULVAC | 149 | 61 | 38
Mechanical properties (for Disk)
 | Top | Bottom
Ingot | 324 | 338
Disk | 325 | 
RRR (for Ingot and Disk)
(ppm)
Nb disk satisfies the ASTM Type 5 (RRR Grade) specification
No degradation in process to disk

## Slide 8: Welding type 1-cell cavity
Eacc max. = 41 MV/m @2K
Yes !
Vertical test @ KEK
Can be used our Nb materials for SRF accelerators?

## Slide 9: Seamless type 1-cell cavity
Nb Ingot
RRR>300
Vertical Test
Large tube
Small tube
Disk
Seamless cavity
Beam tube
Half cell
Welding
Polish
Rinse
Assembly
Forming
Parts supply
Investigation for low-cost manufacturing

## Slide 10: Seamless type 1-cell cavity
OD 130mm x ID 123mm (t = 3.5mm)
Length : 400mm
After process is performed at KEK
Mold
Oil injection
Roller
< Necking >
< Hydroforming >
Succeed in forming

## Slide 11: Seamless type 1-cell cavity
Eacc max. = 37 MV/m @2K
Eacc max exceeds ILC specification (> 35 MV/m)
Eacc max and Q0 value are slightly lower than welding-type cavity
< Polish >
< Welding beam tube >
< Rinse>
Vertical test @ KEK

## Slide 12: Seamless type 1-cell cavity
After polish
Inside view
Outside view
Dent
Why accelerating performance is lower than that of welding type cavity?
Micro size dent inside cavity
Non-uniform crystalline grain size
We could not remove deep rough point
Or, material starts to thinner locally
Origin of performance degradation?

## Slide 13: Crystalline uniformity confirmation
RD
TD
ND
1㎜
1㎜
1㎜
1㎜
1㎜
Weak process power
Strong process power
We should apply more strong process for seamless tube

## Slide 14: Summary
ULVAC can supply high purity Nb products satisfy ASTM 5 and ILC spec.
In welding type 1-cell cavity, good accelerating performance was obtained.
(Eacc max = 41 MV/m, Q0 =1.0 x 1010 @32MV/m (@2K))
We succeed in forming of seamless 1-cell cavity.
In seamless type 1-cell cavity, Eacc max = 37 MV/m @2K.
However, accelerating performance should be improved.
Future plan
φ138 x φ131 x 830mm
<Scale up study>
Trial manufacturing of seamless tube for 3-cell
was already finished.
Necking and Hydoroforming process will be performed near future.
<Improvement of accelerating performance for seamless cavity>
We will optimize forging, deforming and annealing condition,
so as to be uniform grain size.
seamless tube for 3-cell

## Slide 15
Thank you for your attention !