## Slide 1: CHESS2 architecture

## Slide 2: From CHESS1
Leakage current and detector capacitance has been measured [UCSC] using probe stations.
Isolated amplifiers have been measured [UCSC] using a DIY board.

## Slide 3: From CHESS1
Charge collection efficiency has been measured under irradiation [Igor Mandić Ljubljana]
Sr-90 electrons, mean charge, 25 ns shaping

## Slide 4: Objective of CHESS2
Demonstrate HVCMOS as a viable solution for ATLAS strip detector.
  Record hits on full reticle sensor
  Amplify and discriminate signal
  Encode hit position in sensor and send to external readout electronics
Further investigate performances of HVCMOS MAPS sensors
  Evaluate sensors performances with different substrate resistivity 20, 100, 1000 Ohms.
  Verify radiation hardness using test structures.
  Characterize the detector with edge-TCT structure and passive pixels arrays.

## Slide 5: HV-CMOS Monolithic Active Sensors
Deep nwell
depletion
-HV
Full depletion
-HV
-
+
+
+
+
+
-
-
-
-
-
+
Drift
-
+
+
+
+
+
-
-
-
-
-
+
Drift
External amplifier
In strip amplifier
STRIP Baseline
STRIP HVCMOS

## Slide 6: Strip sensor dimensions
800µm
40µm
32 pixels in a strip
128
strip

## Slide 7: Specifications
Substrate resistivity | 20Ohms to 1000Ohms
Substrate high voltage bias | 120V
Pixel size | 40µm x ~800µm
Number of pixel per strip | 32
Number of strips | 128
Timing resolution | 25ns
Maximum number of hits per strip | 1 + flag
Maximum number of hits per 128 strips | 8
Readout speed | 320MHz
Additional contraint | Radhard design

## Slide 8: CHESS2 architecture
128 x 32
pixels
Column Decoder (5 bits Input– 1 Hot Output)
Column Decoder (5 bits Input– 1 Hot Output)
Half Comparator,
Latch & Hit encoding
Strip Encoder
Row Decoder (7 bits Input– 1 Hot Output)
colReg
5bits
6b
Trim DAC (4b) + Calibration (1b) + Masking (1b)
rowSel
clk
SACI
Control Logic
rowReg
7bits
PADS
PADS
LVDS
LVDS
Global DACs
Doesn’t reflect actual size or placement
…

## Slide 9: List of programmable possibilities
In pixel:
  Configure a single pixel – configure all pixel in a row – configure all pixel in a column
  Configure signal injection for each pixel [RAM]
  Adjust threshold for each pixel [RAM]
Periphery
  Mask the comparator output for each pixel [RAM]
  External Reset signal to all comparators
SACI global control
  Adjust the amplifier bias
  Adjust the comparator bias
  Adjust the threshold level
  Adjust the LVDS power consumption
  Adjust the LVDS levels and common mode
  Adjust parameters in the encoding and readout blocks.