## Slide 1: CHESS1 testing

## Slide 2: CHESS1 NMOS - unirradiated
Current
to cont.
Smaller gain

## Slide 3: CHESS1 NMOS – higher current

## Slide 4: PMOS CHESS1 - unirradiated

## Slide 5: CHESS1 bonded for testing
Looks nice no? Thanks Jaya John and Forest!
Measured:
3Mrad irradiated

## Slide 6: CHESS2 amplifier
IFB
3.3
3.3
InSF
In
Casc
Load
Out

## Slide 7: Setup
Pulser
CHESS1
Buffer
Scope
9ns falltime

## Slide 8: Configuration used
Bias | Description | Config1 (V) | Config5 (V)
VNBias | Bias for the NWELL | 0.340 | 0.340
Casc | Cascode voltage | 2.6 | 2.6
VPLoad | Pmos Load voltage | 2.1 | 2.1
iN | Amplifier bias current | 1.0 | 1.0
iNSF | Source Follower Bias | 0.57 | 0.57
iFB | Feedback current | 2.664 | 2.53

## Slide 9: Gain – config1
Gain seems to be quite reproducible.

## Slide 10: Rise time config1
Rise time difference:
- State of the circuit:
  Perfect circuit in simulation
  3MRad irradiated sample in reality
- Output capacitance:
  6p used in simulation
  ?? In reality

## Slide 11: FWHM config1
FWHM difference:
- State of the circuit:
  Perfect circuit in simulation
  3mRad irradiated sample in reality
- Output capacitance:
  6p in simulation
  ?? In reality

## Slide 12: Noise config1
Noise difference:
Unexplained increase of the noise with larger input signals
  Slow decaying high Z node??
  …
More measurement to be done, in particular with no signal.
Unexplained region

## Slide 13: Config1 to Config5
Config5 higher reset current:
  Lower noise
  Faster reset
  Smaller gain
  Faster pulse
  Let’s verify that: …
Bias | Description | Config1 (V) | Config5 (V)
VNBias | Bias for the NWELL | 0.340 | 0.340
Casc | Cascode voltage | 2.6 | 2.6
VPLoad | Pmos Load voltage | 2.1 | 2.1
iN | Amplifier bias current | 1.0 | 1.0
iNSF | Source Follower Bias | 0.57 | 0.57
iFB | Feedback current | 2.664 | 2.53

## Slide 14: Gain config1 – config5
Gain decreases from config1 to config5 as expected.
Config5 [3MRad] seems to have much higher gain than anticipated.
  To be understood.
  Measurement of un-irradiated sample needed.

## Slide 15: FWHM config1 – config5
  FWHM decreasing from config1 to config5 as expected.
Simulation done here with a load = 1pF
  FHWM increases with the input capacitance in simulation
  Load used probably too low. 6pF maybe more realistic.
  Estimation of the load capacitance needed.
  Measurement of un-irradiated sample needed.

## Slide 16: Rise time config1 – config5
Rise time decreases from config1 to config5 as expected.
Big discrepancies in rise time measured vs simulated.
  In part due to bad model of load capacitance.
  Again estimation of the load capacitance needed.
  To be done with un-irradiated samples.

## Slide 17: Noise config1 – config5
Noise decreases from config1 to config5 as expected.
Seems to be a problem of coupling between signal and noise
  To be investigated
  To be done with un-irradiated samples.

## Slide 18: SNR config1 – config5
SNR increases from config1 to config5 as expected.
Expect better SNR once noise is understood.
To be measured on un-irradiated samples.

## Slide 19: TCT laser system

## Slide 20: Laser scan on a 45µm x 800µm pixel.
Non-optimized laser spot size. We have no good idea of what the spot size is here.
10MIP of laser signal
0V HV bias
We see a roughly 800µm long structure.
Active arrays are alive. More precise measurements to come.

## Slide 21: Summary
Schedule for NMOS and PMOS irradiation being decided - end of September at CERN if possible [after ITk would be great].
Isolated amplifier measured in depth for 1MRad and 3MRad CHESS1. Agreement between measurement and simulation is not great but not completely crazy either. Need to be done with un-irradiated CHESS1 to be in controlled situation. Does anyone have any left?
Noise of CHESS1 need to be understood better.
Active arrays in CHESS1 are alive. Adjustment of the TCT laser in progress and more results to come.