## Slide 1
Julius Kühn
High Brightness Electron Beams (HBEB) Institute for Accelerator Physics
PCHB Meeting
Helmholtz-Zentrum Dresden-Rossendorf
4.12.2015
On the way to operate CsK2Sb photocathodes in Gun 1.0

## Slide 2
Outline
Status of the photocathode lab
Preparation of the first photocathodes
Time schedule (Summary and Outlook)
Status of the transfer systems and vacuum suitcase
PLUG Design
Photocathode roughness
Photocathode preparation and characterization at EMIL

## Slide 3
Photocathode Lab in operation

## Slide 4
Our goals
High QE CsK2Sb photocathodes
Allow high bunch charge and current 100 mA means 25 W laser power at 1% QE
Reproducible growth procedure & robust lifetime
Necessary for operation
Smooth substrates and films
Low emittance, low field emission

## Slide 5
Status of the photocathode lab
We have prepared a number of photocathodes with varying results
Preparation chamber
effusion cell for Sb, SAES Dispenser for K and Cs
sequential growth and co-deposition of K and Cs
spectral response measurement from 250 – 600 nm
  (H. Kirschner, Master Thesis, ready in MAR 16)
Surface Analysis chamber
XPS and LEIS (Specs),
Momentatron for emittance measurement (M. Schmeißer, Master Thesis, 2014)
Photocathode Preparation and Analysis System (PAS)
setup and commissioning after the return from
Transfer system #1
transfer system #1 is complete, all parts were cleaned in the clean room
DEZ 15: setup of clean room tent in the photocathode lab
JAN 16: setup and commissioning of transfer system
Vacuum suitcase
Setup and commissioning is finished
disassembly and cleaning is done
reassembling and vacuum commissioning is on-going
Poster
M. Schmeißer

## Slide 6
Substrate characterization
For cathode research:
polished Mo samples, 10x10 mm
roughness : ~10 nm rms, can be 1-3 nm rms
AFM; Rq = 10,66 nm rms White Light Interferometer 20x; Rq = 8,30 nm
Sample 1; Pos 2
work done by Grzegorz Gwalt, Frank Siewert
On-going: change in surface roughness due to heat treatment, sputter cleaning

## Slide 7
Substrate Characterization by XPS
For cathode research:
polished Mo samples, 10x10 mm
roughness : ~10 nm rms, can be 1-3 nm rms
Cleaning: heat to 450°C for 30 min, Ar+ sputter cleaning for 30 min
Or heat to 600°C for 60 min
Results in very low surface contamination, confirmed by XPS
Mo 3d

## Slide 8
Results P004:
Polished Mo substrate
10 nm Sb film evaporated at 100°C
Surface composition KSb after K deposition
zero QE for green light, small QE for daylight
Surface composition Cs2KSb after Cs deposition
QE ≈ 5%
3.8% and 3.6% QE after 1 and 2 days
Results P005 :
< 10nm Sb film evaporated at 100°C
K2.4Sb surface composition after K deposition, strong oxygen impurities
K rich composition after Cs deposition, strong oxygen impurities
0.175% QE
Cs-K-Sb PHOTOCATHODES

## Slide 9
Cs-K-Sb PHOTOCATHODES: difference between good (P004) & bad (P005)
Same substrate, same cleaning, low contaminations confirmed by XPS
Same growth procedure, same type of sources
P005 Sb layer not as thick
Water and Oxygen partial pressure worse by 102
Strong degasing of K source due to first use!
need to degas at higher temperatures
Control over vacuum conditions is essential. Mass spectrometer allows to ensure low residual gas pressures.
Sb 3d / O 1s

## Slide 10
Cs-K-Sb PHOTOCATHODES
Results P006:
10 nm Sb film evaporated at 100°C
K1.7Sb surface composition after K deposition
not all Sb reacted, some still in metallic state
0.05% QE for green light
Cs2.7K1.7Sb composition after Cs deposition
All Sb reacted, Alkali rich surface
5.2% QE
QE decays from 5 to 3%
in about 4 days
Combined exposure of H2O and O2 in 3*10-10 mbar vacuum

## Slide 11
Photocathode roughness
H. J. Qian et al. PRSTAB, 15, 040102, (2012).
λ=50nm
We need to be better than 10 nm!
Roughness introduces an increase in emittance:
XRR yields roughness and thickness of the deposited layer
XRD allows to quantify crystallization processes
and correlate QE with certain phases
M. Gaowei et al.
XRR results for sputtered layers on Si
Layer | Roughness (nm) | Thickness (nm)
3rd layer | 0.69 | 51.2
2nd layer | 0.62 | 22.6
1st layer | 0.60 | 17.8
Substrate | 0.24 | 

## Slide 12
Photocathode preparation and Characterization at
Energy Materials In-situ Laboratory

## Slide 13
PLUG Design – Copper vs. molybdenum
For gun operation, consider:
Cooling of the thermal load from RF and drive laser:
Cu has low surface resisitivity and good thermal conductivity and contact
Properties as a cathode substrate:
Mo is favorable for cathode QE
Cu migrates into Antimony layer, results in 50% lower QE
Thermocontact experiments:
cathode cooling with LN2 but GUN 1.0 80 K He – on going!
PLUG - Options :
Mo-Plug: sputter cleaned and heat treatment (Mo)
Mo-plug: sputter-cleaned only at the center where the cathode will be deposited  lower field emission from rim (MoOx)
Cu-plug with Mo film deposited as a diffusion layer at the plug center  Mo layer deposited by e-beam evaporation
Scenario Gun 1:
6 W RF losses
1.2 W laser power
Aperture and anode
for the PAS:
Scenario Gun 2:
24 W laser power
Omicron sample
holder with PLUG:
PLUG-Holder w/ PLUG in GUN 1.0

## Slide 14
Transfer systems and vacuum suitcase
14
Cathodes must be stored and handled in < 10-10 mbar UHV
Vacuum suitcase is available. Vacuum ~ 1*10-11 mbar
Stability with NEG + getter pump is good for >3 months
Cleaning and assembly in ISO 5 clean room conditions done!
DEZ 15: Setup & commissioning of transfer system 1 @ PAS
Engineering: Petr Murcek (HZDR), Kerstin Martin, Andre Frahm
Transfer system #2 ordering process started!
Transfer System #1
Transfer System #2
Vacuum Suitcase
PAS
Gun Module

## Slide 15
Transfer systems and vacuum suitcase
15
Cathodes must be stored and handled in < 10-10 mbar UHV
Vacuum suitcase is available. Vacuum ~ 1*10-11 mbar
Stability with NEG + getter pump is good for >3 months
Cleaning and assembly in ISO 5 clean room conditions done!
DEZ 15: Setup & commissioning of transfer system 1 @ PAS
Engineering: Petr Murcek (HZDR), Kerstin Martin, Andre Frahm
Transfer system #2 ordering process started!
Transfer System #1
Transfer System #2
Vacuum Suitcase
PAS
Gun Module

## Slide 16
Time schedule
setup and commissioning of transfer system #1 under clean room tent
NOV15
spectral response measurements on CsK2Sb photocathodes
photocathode life time studies: Simulation of transfer to Gun 1.0
Characterization of Cu photocathode for Gun 1.0
Characterization of sequential growth process of CsK2Sb photocathodes
Setup and commissioning of transfer system #2 in the clean room
Design finished & start of ordering process of transfer system #2
DEZ15
JAN 15
MAR 16
JUN 16
JUL 16
Operation of Gun 1.0

## Slide 17
Acknowledgements
Mario Schenk, Alexander Büchel, Jörg Borninkhoff Daniel Böhlick, Kerstin Martin, André Frahm
Grzegorz Gwalt, Frank Siewert
Susanne Schubert, Jared Wang, Howard Padmore
Arthur Woll
Zihao Ding, Mengjia Gaowei,
John Sinsheimer, John Smedley
Martin Schmeißer, Zihao Ding, Hans Kirschner, Thorsten Kamps, Andreas Jankowiak
Petr Murcek
Regan Wilks, Marcus Bär, Gerd Reichert, Simone Raoux

## Slide 18
Thank you for your attention!