## Slide 1
Outline:
Motivation/CBM-ToF requirements
What is an Multigap Resistive Plate Chamber (MRPC)?
Cosmic test results with float glass MRPC prototype
Low resistive glass as resistive electrodes for MRPCs
Beam test results with low resistive glass MRPC prototype
Module design
ToF – project timeline
Summary / Next steps
Ingo Deppner for the CBM-TOF Group
9th Terascale Detector Workshop 2016
(M)RPCs for CBM

## Slide 2
Motivation
Open questions in nuclear physics:
Is there a 1st order phase transition at high ρB?
Is there a QCD critical endpoint?
What is the equation-of-state at high ρB?
What is the property of hadrons in dense medium?
Phase diagram of strongly interacting matter

## Slide 3
Motivation
Central Au+Au/Pb+Pb collisions, 4p yields
?
Maximal interaction rate in CBM for heavy systems is 5 - 10 MHz

## Slide 4
Requirements
80 W
1 ns
Compressed Baryonic Matter Experiment at FAIR facility @ GSI
CBM-ToF Requirements
full system time resolution sT ~ 80 ps
Efficiency > 95 %
Rate capability  25 kHz/cm2
Free streaming DAQ
Ocupancy < 5%
Low power electronics
(~120.000 channels)
TRD
TOF
ECAL
RICH
Dipole magnet
PSD
MVD & STS
MUCH

## Slide 5
Incident particle flux
Area with < 1 kHz/cm2
URQMD simulated charged particle flux for Au + Au (central) events at 10 AGeV assuming an interaction rate of 10 MHz
kHz/cm2
Flux ranging from 0.1 to 100 kHz/cm2
At different regions MRPC counters with different rate capabilities are needed

## Slide 6
Working principle of an RPC
E0 = 120 kV/cm
Shockley-Ramo theorem
Theoretical time resolution
Number of e- per avalanche
Induced signal current (mirror charge)
Typical drift velocity in RPCs
 230 m/ns
D
Weighting field:
Effective Townsend coefficient:
 150 mm-1
Gas gap
Resistive plate
Resistive plate
Variance of a Landau distribution
 40 ps

## Slide 7
What is an (M)RPC?
80 W
1 ns
First RPC developed 1981 by
R. Santonico and R. Cardarelli, Nuclear Instruments and Methods 187 (1981) 377 - 380
Bakelite vol.res. r  1010 Wcm E  50 kV/cm t  1 ns C2F4H2/i-C4H10/SF6 (96,7/3/0.3)
Example: Atlas with 7300 m2 and 355000 readout channels
Experiments using trigger RPCs: ATLAS, CMS, Alice, PHENIX, BaBar, ARGO-YPJ, OPERA

## Slide 8
What is an (M)RPC
gas gap 0.3 mm
glass vol.res. r  1012 Wcm
E  100 kV/cm
t  100 ps
C2F4H2/i-C4H10/SF6 (85/5/10)
Al
glass
First Multi-gap RPC (MRPC) introduced 1996 by
E. Cerron Zeballos, I. Crotty, D. Hatzifotiadou, J. Lamas Valverde, S. Neupane, M.C.S. Williams, A. Zichichi Nuclear Instruments and Methods in Physics Research A374 (1996) 132-136
First timing MRPC built in 2000 by
P. Fonte, A. Smirnitski, M.C.S. Williams,
Nuclear Instruments and Methods in Physics Research A 443 (2000) 201 - 204
Design used still now by HADES
Experiments using timing MRPCs: FOPI , ALICE, STAR, HARP, LEPS2
Example: ALICE with 160 m2 and 160000 readout channels

## Slide 9
Structure of Multi-gap RPCs
e.g. FOPI
e.g. CBM
Single ended with double stack configuration
Differential with single stack configuration

## Slide 10
MRPC-P3 prototype
80 W
1 ns
Full size demonstrator with float glass for the low rate region (< 1kHz/cm2) MRPC-P3 (HD)
MRPC differential active area 52 x 53 cm2
strips 56
strip / gap 7.6 / 1.8 mm
glass type float glass
glass thickness 0.5 mm
number of gaps 8
gap width 220 mm
Impedance matched to 100 

## Slide 11
Cosmic ray stand in HD
Setup in our lab. 2014
System Time resolution
MRPC time resolution is about 40 ps including electronics resolution
PMTs
MRPC
Cluster distribution

## Slide 12
Rate capability of MRPCs
Lowering the resistivity of the electrode material - different materials 1) float glass:  = 3x1012 cm 2) low resistive glass:   1010 cm 3) ceramics:   109 cm - warming the electrodes
Decreasing the electrode thickness
Time resolution:
Efficiency:
: incident ch. particle flux : electrode bulk resistivity d: electrode thickness
How to increase the rate capability?

## Slide 13
Low resistive glass
Low resistive glass for high-rate MRPCs is developed in Beijing, China (Yi Wang)
Aging tests

## Slide 14
MRPC-P2 prototype
Full size demonstrator for high rates (1 - 10kHz/cm2)
Low resistive glass
Spacers (fishing line)
HV electrode (Licron)
Pickup electrode
27 x 32 cm2

## Slide 15
Full size demonstrator and reference MRPC developed in HD and Beijing MRPC-P2 (HD) THU-strip (Beijing) MRPC-P5 (HD) MRPC differential differential differential glass stack single double single active area 32 x 27 cm2 24 x 27 cm2 15 x 4 cm2
strips 32 24 16
strip / gap 7/ 3 7/ 3 7.6 / 1.8 mm
glass type low resistive glass low resistive glass low resistive glass
glass thickness 0.7 mm 0.7 mm 1.0 mm
number of gaps 8 2 x 4 6
gap width 220 mm 250 mm 220 mm
MRPC prototypes
MRPC-P2 THU-strip MRPC-P5

## Slide 16
2 MRPC concepts
Differential singel stack MRPC with 8 gaps
Differential double stack MRPC with 2 x 4 gaps
Advantages - lower High Voltage (< 6 kV) - smaller cluster size
Disadvantages - more complex construction - more glass plates (#10) - impedance matching hardly possible (100)
Advantages - simpler construction - symmetric signal path - fewer glass plates (#9) - lower weight - impedance matching easy possible (100)
Disadvantages - higher High Voltage (> 10 kV) - bigger cluster size
vs.

## Slide 17
Test beam time @ GSI
Test beam time in October 2014 at GSI (Hades cave)
Sm beam with 1.2A GeV kin. energy
5 mm thick lead target
„Uniform“ illumination of the counter surface
Flux on the lower part of the setup was about few hundred Hz/cm2
Delivered flux does not meet the CBM requirements
THU-Strip
Setup

## Slide 18
Beam-time @ GSI

## Slide 19
Results
Efficiency > 98 %
Resolution  62 ps
Efficiency > 96 %
Resolution  65 ps
Differential singel stack MRPC with 8 gaps
Differential double stack MRPC with 2 x 4 gaps
vs.
Data points at 11 kV in the left plot can be compared with 5.5 kV in the right plot.
Single stack MRPC shows slightly better efficiency and time resolution.
Single counter resolution is in the order of 45 ps including all electronic components.

## Slide 20
Beam-time @ SPS
About 1100 channels
20 MRPC
“STAR” module
Beam-time @ SPS North Area in Nov. 2015
Beam: Lead @ 30A GeV Target: Lead 1 mm
Intensity: 107 / spill
Spill length: 8 s
Rates: few kHz/cm2
Energy close to SIS300 conditions
Upper setup
Lower setup

## Slide 21
Beam-time @ SPS
21
Upper setup
)
Lower setup
1 2 3 4 5 6 7 8
Heidelberg-P5
USTC-SSS (W-) ( )
USTC-SSU (X0) ( )
USTC-DSU (L) ( )
Tsinghua-SU (K+)
Tsinghua-DS (K0)
Tsinghua-DU (p+)
Heidelberg-P2
9 10 11 12 13 14
Tsinghua-PAD (3 counter)
Bucharest2015-SS (j)
Bucharest2015-DS (K0*)
Bucharest2012 (4 counter) ( )
Bucharest-Reference
CRPC (2 counter)
Beam
Impedance matching

## Slide 22
Beam-time @ SPS
1 Track (blue) with hit multiplicity 8
2 Tracks (green) with hit multiplicity 7
1 Track (light blue) hit with multiplicity 6
1 Track (pink) with hit multiplicity 5
Event display after position calibration
RPC Hits
RPC layers
Tracks
The opportunity to construct tracks offers new possibilities to analyze and study the counters in much greater detail

## Slide 23
Beam-time @ SPS
2 new types of counters designed a. Single stack with pitch of 10.1 mm
b. Double stack with pitch of 7.2 mm
Time over Threschold distribution
Cluster matching
System time resolution
RMS = 92 ps s = 84 ps
Preliminary
a.
b.

## Slide 24
Modules
a: MRPC, b: Preamplifier (PADI), c: feed-through PCB, d: connectors, e: crate, f: TDC and read out
Preamplifier PADI
TDC GET4
 106368 read-out channels
Aproved

## Slide 25
Time line
Full-size demonstrator end 2012
TDR approved mid. 2015
Full-size modules mid. 2015
Full-size modules with ‘final’ electronics mid. 2016
Construction of the modules 2016- 2020
Integration in STAR@RHIC@BNL 2017- 2018
eTOF ready for beam 01.01.2019
Integration in CBM@SIS100@FAIR 2019- 2021
ToF ready for beam 01.06.2021
RPC type | res. material | efficiency | time resolution | rate capability
Ceramic MRPC | Ceramic |  90 % |  90 ps |  500 kHz/cm2
Pad MRPC | sem. glass |  95 % |  50 ps | > 30 kHz/cm2
Strip | sem. glass | > 95 % |  50 ps | > 30 kHz/cm2
Strip | float glass | > 95 % | 60 ps – 70 ps |  1.5 kHz/cm2
The CBM requirements are fulfilled.
ToF – Project Timeline

## Slide 26
CBM-ToF @ STAR
CBM “STAR” module
STAR eTOF
3 layers 12 sectors 36 modules 6912 channels
one sector
Particle flux < 45 Hz/cm2, Multi-hit probability < 7.4%
collider
Fix target

## Slide 27
Summary / Next steps
Summary
The high rates in CBM require a special materials for MRPC electrodes  Ceramics and Low resistive glass from Beijing, China
MRPC solutions for all rate conditions available.
The design of the MRPC are driven by the free-streaming readout  impedance matching is realized.
The single stack MRPC shows slightly better efficiency and time resolution in comparison to a double stack MRPC.
Single counter resolutions are in the order of 50 ps to 70 ps including all electronic contributions.
All types of MRPC detectors fulfill the CBM ToF requirements.
Results of the last CERN beam time are still preliminary and analysis is ongoing.
A participation in BES II of STAR @ BNL with about 10% of the full CBM Tof wall is being planned.
Next steps
Selection of the final layout and counter configurations this year based on the last SPS beam time results.
Integration of the final electronics and readout until summer this year.
Load test for all available full size prototypes in Nov. 2016 with final electronics with heavy ions at SPS CERN.
Integration and beam time test of one module at BNL in Feb. 2017

## Slide 28
Thank you for your attention
Contributing institutions:
Tsinghua Beijing,
NIPNE Bucharest,
GSI Darmstadt,
IRI Frankfurt
USTC Hefei,
PI Heidelberg,
ITEP Moscow,
HZDR Rossendorf,
CCNU Wuhan,
Special thanks go to:
Norbert Herrmann

## Slide 29
Backup
80 W
1 ns
Backup Slides

## Slide 30
Backup Slides
CBM Physics topics
Deconfinement / phase transition at high ρB
QCD critical endpoint
The equation-of-state at high ρB
chiral symmetry restoration at high ρB
Observables
excitation function and flow of strangeness and charm
collective flow of hadrons
particle production at threshold energies
excitation function of event-by-event fluctuations
excitation function of low-mass lepton pairs
in-medium modifications of hadrons (ρ,ω,φ → e+e-(µ+µ-), D)
non twisted part
connector
p
p
K
D. Kresan Au + Au @ 25GeV
Kaon acceptance depends critically on TOF resolution

## Slide 31
Backup
80 W
1 ns

## Slide 32
Particle identification with Time-of-Flight
80 W
1 ns
Time-of-Flight (ToF) methode:
stop-detector (MRPCs)
start-detector (plastic, diamond)
target
tst
tsp
L
tToF = tsp – tst - offset
PID with ToF:

## Slide 33
Separation power
80 W
1 ns
A larger distance helps, howewer the efficiency of weakly decaying particles (Kaons) drops

## Slide 34
80 W
1 ns
FOPI L=1m
CBM L=6m
measured
simulated
System time resolution 88 ps
System time resolution 80 ps
Particle identification with Time-of-Flight
K+ ID up to 1.3 GeV/c
K+ ID up to 3 GeV/c

## Slide 35
Start – T0 determination
80 W
1 ns
Diamond start counter - use available solutions - limited to reaction rates of about 100 kHz/cm2
Software solution - available for all systems - needs fast particles from reaction - demonstrated to work for central and semi- central heavy system
Beam Fragmentation Counter - peripheral HI – reaction have fast particles from projectile fragmentation - equip inner most region of the ToF wall with timing counters (ceramic MRPCs)
Reaction Counter - needed for high rate pA - reactions - reaction counters at polar angles 35  <  < 60

## Slide 36
Reflectometer measurement on the MRPC – P2
Rise time measurement on the MRPC – P2
Impedance = 93 
Detector signal properties

## Slide 37
Experiments at FAIR
FLAIR
80 W
1 ns
PANDA
APPA
S-FRS
CBM
NuSTAR