## Slide 1: AMS-Chess1 Characterization
K. Kanisauskas, T. Binnie, C. Buttar, J. Dopke, T. Huffman, J. John, D. Maneuski, R. Plackett, L. Vigani, Q. Xiu
ATLAS Strip CMOS Regular Meeting
March 29, 2016

## Slide 2: AMS-Chess1
Edge-TCT measurements performed for irradiated and non-irradiated samples
Laser scans done at different bias voltages
APA8 structure investigated
45×800μm2 size pixels
Same DAC settings used for both samples:
VPLoad: 2100
Casc: 2600
iNSF: 570
iN: 1000
iNBias: 340
iPFB: 2475

## Slide 3: Laser Setup
1060nm laser was used
Test chip is cooled down using peltier
Temperature monitored close to AMS-Chess1 chip during measurements
Measurements for non-irradiated and irradiated samples done at the same temperature (≈ -8℃)
Constant dry air supply available (dew point ≈ -11℃)

## Slide 4: Edge-TCT (1)
Data was taken for CH38 and CH41 (correspond to APA8 pixels) between -45 and 0 bias voltages
In this case positive signal observed from pixels
For irradiated device the signal completely disappears below -50V bias
Rise-times of the signal were dismissed due to jitter
Output Signal Maps
Non-Irradiated
Irradiated
Surface

## Slide 5: Edge-TCT (2)
Non-Irradiated
Irradiated
Surface
Different X-axis range

## Slide 6: Edge-TCT (3)
Signal cut was done for CH38 at the center of the pixel
Plots produced of relative signal vs x-coordinate
Depletion regions compared between irradiated and non-irradiated samples at different bias voltages

## Slide 7: Edge-TCT (4)

## Slide 8: Summary
Increase in depletion region observed for irradiated device
Different behavior of amplitude vs bias voltage seen between non-irradiated and irradiated samples
Unknown reason for signal disappearance below -50V