## Slide 1
Tutorial I: Insertion Devices – Undulators
Johannes Bahrdt
4th ARD ST3 Workshop: ps-fs Electron and Photon Beams, July 13th - 15th, 2016

## Slide 2: History of Insertion Devices
1947 first discussion of undulator radiation by Ginzburg
1951 / 1953 first production of undulator light in
the mm and visible regime by Motz et al.
1976 FEL radiation from a superconducting (SC) helical undulator at Stanford: Madey et al.
1979 / 1980 first operation of permanent magnet undulators in storage rings
(SSRL, LURE, VEPP3)
1980... SC-wavelength shifters in storage rings (VEPP3, SRS, VEPP2M)
1992… In-vacuum undulators
2008… cryogenic permanent magnet undulators (CPMUs)
(ESRF, PSI, SPRING-8, SOLEIL, DIAMOND…)
2009 First FEL lasing & saturation of 1.5A SASE-FEL in Stanford
today about 20 third-generation synchrotron radiation light sources
SASE-FELs from the infrared to the X-ray regime
(Angstrom-FELs: LCLS, USA, SACLA, Japan, XFEL, Germany)

## Slide 3: Increasing the Photon Flux vs. SRing Dipole Wiggler: A Sequence of Alternating Dipoles
brilliance scales linearly with number of poles
incoherent overlap of light from individual poles
spectrum = n times dipole spectrum
SSRL 1978
Electromagnetic 7 poles wiggler
LBL / SSRL 1985
54 poles hybrid wiggler

## Slide 4
Spectral properties of IDs

## Slide 5: Starting from Lienard-Wiechert Potential
The Lienard-Wiechert potentials are the solution
of the inhomogenious Maxwell equations
The brackets are evaluated at
the retarded time:
The acceleration and velocity fields are derived from these potentials:
A. Liènard, L’Eclaire Electrique 16(5) (1898)
E. Wiechert, Archives Neerlandaises, 1900, p. 546

## Slide 6: Radiation Emitted by Accelerated Charged Particles
In the far field we approximate:
The emitted power
is given by the
poynting vector
The spectrum is evaluated via a Fourier
transformation of the time dependent fields

## Slide 7: Radiatin from Bending Magnets, WLS, Wigglers
The critical energy divides the
power spectrum into equal parts.
on axis flux density (ph / s / mrad**2 / 0.1%BW)
vertically integrated flux (ph / s / mrad / 0.1%BW)
critical
energy
The critical energy scales
With the second power
of the electron energy
ρ=bending
radius

## Slide 8: Line Spectrum of Undulators
resonance condition
figure 8 motion in moving frame
produces higher harmonics
on axis: only odd harmonics
off axis: also even harmonics
electric field at observer
spectrum

## Slide 9
Wigglers & Undulators
Undulator Wiggler
photon phase space
undulator parameter K
undulator:
wiggler:
wiggler
undulator

## Slide 10
10
Undulator Spectrum I
amplitude term
interference term
off-axis brightness
exact
dipole series appr.

## Slide 11
Fine structure @ harmonic
Fine structure off-axis
Undulator Spectrum II
Interference term reflects the beam coherence:
Enhancement by orders of magnitude at the harmonics
Intensity suppression between the harmonics

## Slide 12: Useful Equations in Practical Units
On-axis flux density of the nth harmonic (ph / s / mrad**2/ 0.1%BW)
flux inside the central cone (ph / s / mrad**2/ 0.1%BW)
1
9
1
9

## Slide 13: Sources of Brightness Degradation
Undulator errors
Beam parameters
Phase error U41:
(rms) = 2.6°
reduction of on axis
flux density (Walker):
beam emittance: 6 x 10-9 m rad
= 0.94 m
= 2.1 m
energy spread: 8 x 10-4
black: without emittance, energy spread
red: emittance included
blue: energy spread included
magenta: emittance and energy spread incl.
Brightness gain with DLSR
phase error from
measured fields:

## Slide 14
Undulators with Reduced on-Axis Power Density
helical undulator
figure-8 undulator
Planar Undulator: Maximum power density on-axis
Reduced on-axis power density
leaf undulator
knot undulator

## Slide 15
ESRF / ELETTRA design
spectra derived
from measured
magn. fields
generate 1D-quasiperiodic lattice
original design
BESSY II design
Undulators with Reduced Higher Harmonic Content
Quasiperiodic Undulator
S. Sasaki, Conceptual design of new type quasi-periodic undulator. Sincr. Trieste, ST/M-TN-98/24 (1998)
S. Sasaki, New scheme of quasi-periodic undulators, in Proc. of the IPAC, Kyoto (2010), pp. 3141–3143

## Slide 16: Principle of APPLE II Undulator
The APPLE II design provides the highest fields among all planar VPUs
relative phase of By, Bz
defines ellipticity
ratio By / Bz
defines inclination
effective field
- 90o
90o
0o
0o
0,1
10
Bmax
Bmin
Bmin
J. Bahrdt et al., Proc. EPAC 2008, Genua, Italy; J. Bahrdt et al., SRI 2009, Melbourne Australia
J. Bahrdt et al., IPAC 2010 Kyoto, Jap; J. Bahrdt et al., IPAC 2011 San Sebastian, Spain

## Slide 17: Polarization Characterization
The BESSY II Soft X-ray polarimeter
We observe good agreement
between simulations and measurement
0 undulator phase π
elliptical
mode
inclined
mode

## Slide 18: Universal Mode of APPLE Undulator
Modification of undulator radiation polarization by beamline components
J. Bahrdt et al, SRI 2009,
Melbourne, Australia
Müller-Matrix describes beamline effects
Parameters of beamline Müller matrix
and of analyzer vs. photon energy.
Gap and shift settings for normalized
Stokes parameters at the sample.
transmissions of field amplitudes
phase difference of electric field components

## Slide 19
Photons with Orbital Angular Momentum I

## Slide 20
Photons with Orbital Angular Momentum II
J. Bahrdt, K. Holldack, P. Kuske, R. Mü ller, M. Scheer, P. Schmid, Phys. Rev. Lett. 111, 034801

## Slide 21
Beam Dynamics -Non-Linear Effects

## Slide 22: Dynamic Field Integrals of Planar Undulators / Wigglers I
second order kicks (Elleaume, EPAC 1992):
Halbach ansatz for planar undulators / wigglers
from Maxwell equations
non linear kicks of planar undukator / wiggler:
2nd order kicks do not fullfill 2D-Maxwell equations &
cannot be perfectly shimmed by principle
Quadratic scaling:
period length
field
inverse of e-energy
Notes: Alignment: Hinweis auf Hein-Dieter Nuhn

## Slide 23: Dynamic Field Integrals of Planar Undulators / Wigglers II
Non-linear kicks in terms of Fourier coefficients of transverse field distribution
These expressions can be used in a thin lens approximation (kick map)
which assumes a localized kick of the strength of the integrated quantity
Only once, the transverse vertical field distribution in the midplane
at one z-position has to be evaluated (more position for longitudinal FCs)

## Slide 24: Dynamic Field Integrals of APPLE Undulators I
elliptical mode
generic representation of 2nd order kicks for elliptical and inclined mode
inclined mode
Modes of
APPLE
operation
universal mode
f0
fπ
fπ/2
3 generic
functions
inclined mode

## Slide 25: Analytic Representation of Field (Integral) Examples: APPLE II Field & Shim Field Integral
Scalar potential of main Field
Scalar Potential of shim field integral
analytic field description
symplectic particle tracker (generating functions)
very fast (several periods in one step)
Description is based on Fourier decomposition in 3 dimensions

## Slide 26: Accuracy of Field (Integral) Description Based on Fourier Decomposition
Field integrals of L-Shim
analytic representation (black)
simulation with RADIA (red)
Main fields of APPLE II
analytic representation (black)
simulation with RADIA (red)
Parametrization of magnet field properties with high accuracy
Notes: Damit habe wir die Tools zusammen und können anfangen mit dem tracken

## Slide 27: Dynamic Kicks of APPLE II Undulators II
Elliptical mode (φ2=0)
analytic functions of
(parallel motion of diag. rows)
include gap dependence
Inclined mode (φ1=0):
analytic functions of
(antiparallel motion)
J. Bahrdt, G. Wüstefeld,
Phys. Rev. Special Topics, AB 14, 040703 (2011)

## Slide 28
Shimming Techniques

## Slide 29: Field Optimization
Strategy for APPLE undulator field optimization
single block characterization
initial sorting, assembly, in-situ sorting
trajectory and phase shimming via virtual shimiming
shimming of phase dependent field integrals with Fe-sheets
shimming of phase independent field integrals
with magic fingers at undulator ends
compensation of dynamic multipoles
dynamic field integrals cannot be described by 2D-multipoles
dynamic field integrals cannot be compensated
completely with 2D-shims
Notes: Measurements and sorting well elaborated
Next step: transfer the knowledge to industry

## Slide 30
Accuracy of field integral description
via multipole expansion around origin(y=z=0)
Wire positions z0=0,, 10, 20, 30mm and y0=10mm
thick lines: exact fields integrals,
thin lines: approximation with expansion order m=20.
y
z
y0
z0
Position of shim
multipole expansions is not applicable
outside radius of convergence
(defined by closest magnet field source position)
Limits of 2D-Multipole Expansion
Radius of Convergence
Notes: Alignment: Hinweis auf Hein-Dieter Nuhn

## Slide 31: A) Magnet Block Characterization
characterization of dipole errors
(important for larger gaps)
reproducibility:
characterization of inhomogeneities
(important for small gaps)
reproducibility:
A-magnets: 2.0 x 10-4 Tmm
3.0 x 10-4 rel.
B-magnets: 1.5 x 10-3 Tmm
2.1 x 10-4 rel.
Stretched wire system
Automated Helmholtz coil system
Notes: Alte Reproduzierbarkeiten: A 4e-4Tmm, B-magnets 2e-3Tmm, durch Temperatur dominiert?

## Slide 32: B) Magnet Sorting
excellent agreement between predicted and measured fields integrals
for BESSY undulators UE52, UE49, UE112…
efficient sorting procedure
blue: prediction
from single block measurements
red: hall probe measurements
field integrals
longitudinal distribution transverse distribution
UE52
Notes: Measurements and sorting well elaborated
Next step: transfer the knowledge to industry

## Slide 33
trajectory straightening and phase shimming
method: virtual shimming (VS): horizontal and vertical block movement
VS introduces additional phase dependent field integrals
C) Virtual Shimming
field integrals as produced by virtual shimming
Unintended side effect:
phase dependent field integrals
as produced by virtual shimming
vertical movement (dy) horizontal movement (dz)

## Slide 34
shim response of Fe-shims
on APPLE undulator magnets
D) Application of Fe-Shims
shimming of phase dependent field integrals
method: Fe-shims with phase dependent response
field integrals before (top)
and after (bottom) shimming
J. Bahrdt et al, Nucl. Instr. and Meth,
in Phys. Res. A 516 (2004) 575-585
phases,
dashed:
±λ/4
solid:
±λ/2

## Slide 35
EMIL UE48 APPLE II
Phase Dependent Field Integrals After Shimming
Small phase dependent field integral changes
plotted are the differences
with respect to zero phase
phase dependent terms
originate from non-unity
of permeanbility

## Slide 36
Downstream endpole unshimmed
E) Shimming With Magic Fingers
Downstream endpole shimmed
36
Red: difference of data
after and before shimming
Black: predict of shim magnet
array effect
vertical field integrals
horizontal field integrals
vertical field HP-scans
horizontal field HP-scans
Magic finger
EMIL UE48 APPLE II

## Slide 37
EMIL UE48 Static Field Integrals After Shimming
Small field integrals over a wide region
Red:
vertical field integhrals
Regular multipoles
Blue:
Horizontal field integrals
Skew multipoles
Gap 15mm
Gap 20mm

## Slide 38: F) Active Shimming of UE112 with Flat Wires
Current settings for gaps of 20mm
24mm, 30mm and 40mm
2 x 14 wires, 14 power supplies
maximum currents: 16A
wire diameter: 3 x 0.3mm**2
wire separation: 4mm

## Slide 39: UE112: Recovery of Injection Efficciency
Active shimming of the UE112 is essential for a top-up mode.
inclined mode: no alternative to active compensation
elliptical mode: improvement of passive shimming results
Wires compensate dynamic field integrals in plane
(enhancing their efefcts off-plane)
Notes: Alignment: Hinweis auf Hein-Dieter Nuhn

## Slide 40
Local Lattice Modifications

## Slide 41
Short Period Small Gap Devices @ Storage Rings
Mini-beta section at NSLS: short period mini gap devices
Modification of storage ring optics for small gap devices
SPEAR3
DIAMOND
SOLEIL
BESSY II
Sophisticated arrangements of double undulators in one straight
independent users @ ESRF, DIAMOND, BESSY II
Femto Slicing @ BESSY II, SOLEIL, SLS / PSI, ALS
polarization switchng @ BESSY II, SLS / PSI

## Slide 42
Local Lattice Modification for EMIL @ HZB
CPMU17 requires a physical aperture of 5mm
Lattice modification verified in April 2016
Asymmetric betatron-function as
fitted with LOCO
Data correspond to simulations
http://accelconf.web.cern.ch/AccelConf/IPAC2012/
papers/tuppp007.pdf
Vertical aperture of 4.54mm
as measured with 4 scrapers
in replacement chamber.
CPMU17 can be operated
at smallest gap of 5.5mm
with safety margin
IPAC2016: http://www.ipac16.org/proceedings/papers/thpow039.pdf

## Slide 43
Undulator Technologies

## Slide 44
Room Temperature Electromagnetic Undulators
Scaling of 2D-Electromagnetic Undulators
is different:
Similar - scaling as of PMUs
requires
Technically limited by cooling
max.: 5A/mm**2 with direct water cooling
Scaling of Permanent Magnet Undulators
2D periodic structures, e.g. planar PMUs
with linear superposition (Halbach I)
with crosstalk between girders (Halbach II)
Peculiarity of PMUs: surface currents
typically 12kA/cm
independent upon scaling
Below at 15mm gap
K-parameter of ELMU drops below 2.5
reduced tuning capabilties

## Slide 45
Comparison of Planar CPMUs and SCUs
CPMUs gain at short period lengths as expected
Black bullets: optimized magnet design of CPMU poles
J. Bahrdt, Y. Yvanyushenkov, Short period undulators for storage rings
and free electron lasers. J. Phys. Conf. Ser. 425, 032001-1-6 (2013). SRI, Lyon

## Slide 46
PM-Material

## Slide 47: Magnet Material
Vacuumschmelze, Data leaflet
DM - VACODYM/VACOMAX , 2007
High remanence
Nd2Fe17B
Br=1.47 T (typical)
Hcj=11 kOe (minimum)
TK (Br) =-0,115
TK (Hcj)=-0,77
Sintered or melt spun NdFeB magnets

## Slide 48
Fabrication of Sintered Permanent Magnets I
Courtesy of Vacuumschmelze
Production process as developed by SUMITOMO

## Slide 49
Fabrication of Sintered Permanent Magnets II
Courtesy of Vacuumschmelze

## Slide 50
Pressing Technologies
Isostatically pressed magnets
Cold isostatic pressing CIP
Rubber isostatic pressing RIP (M. Sagawa)
H
H
H
H
H
Die pressed magnets
transverse pressing axial pressing
H
H
Properties:
Remanence:
isostatic > transverse > axial
2% 4%
Dipole errors:
isostatic > transverse, axial
Higher order multipoles:
transverse, axial > isostatic
near net-shape
production is
cost effective

## Slide 51: Magnet Material Development I
Current status:
ρ/ρ0 > 0.995, is achieved with the so-called liquid phase sintering
fφ > 0.98, high alignment factor, sophisticated timing during pressing
Non-magnet particles typical < 4%
Example: energy product of Nd2Fe14B
Theory: 509 kJ/m^3 Achieved: 469 kJ/m^3
Not much space for improvement for known materials
Coercivity Hcj still one order of magnitude below theory
„Brown‘s paradoxon“
Remanence

## Slide 52: Magnet Material Development II
Grain Boundary Diffusion (GPD)
Known already for 10 years, now commercially avalilable
Coating of magnets with Dy or Tb
Heating the magnets to 800-900 degrees
Fast diffusion of Dy in liquid phase
Slow diffusion from boundary into the bulk
Establishing highly enriched Dy shells around grain bulk
Concentration
Penetration depth of Dy about d = 2.2mm
Extremely useful for
high end small period devices
H. Nakamura et al., J. Phys. D:
Appl. Phys. 44 (2011) 064004-1-5.
PrFeB samples before / after GBD
Courtesy of Vacuumschmelze

## Slide 53
Halbach Type Undulators and Wigglers
Periodic magnet structure with field B and period length λ0
Constructive interference for the wavelength given by
with M=no of magnets / period, ε=filling factor
Halbach I: pure permanent magnet
K. Halbach, Nucl. Instr. and Meth. 187 (1981) 109-117.
“One-sided fluxes -- A magnetic curiosity?” J. Mallinson, Magnetics, IEEE Transactions on Vol. 9, No. 4 (1973) pp 678 – 682.
Halbach II: permanent magnet + Fe-pole
g
Field parametrization:
P. Elleaume et al., Nucl. Instr.
and Meth. in Phys. Res. A
455 (2000) 503-523
M=4
g
x
y
ελ0/M
L

## Slide 54: Pushing the Field with Shaped Poles and Additional Side Magnets
Conventional Halbach II structure
9mm period, 20 periods, 2.5mm gap
Operation
@ MAMI
minimum dead layer (9µm)
TiN coating (3-4µm)
tight shape tolerances (<10µm)
small air gaps (10-20µm)
Notes: rechts oben width = 6mm
rechts unten width = 4mm

## Slide 55: Cryogenic Peramanent Magnet Undulators
Advantage of Cryogenic Undulators:
gain in remanence, larger tuning range for short period IDs
stability recovered at low temperatures
less sensitive to thermal variations of magnetic properties
Advantage of PrFeB Undulators:
no spin reorientaion at 135K
cooling with liquid N2, no heater
gain in stability (coercivity)
Crystal Energy of NdFeB
Heat capacity
K. Üstüner et al., 20th Conference on REPM, Crete 2008

## Slide 56
First In-Vacuum Undulators
1990, KEK, Kitamura et al.
magnets in vacuum, coating
1987, BESSY, Gudat et al.
magnets still encapsulated

## Slide 57: Cryogenic Undulator Projects at HZB
CPMU 15 built @ HZB
for University Hamburg / DESY
CPMU17 built @ HZB for EMIL BESSY II
Notes: Assembly is critical (at least in summertime)

## Slide 58: Planar Linear Superconducting (SC) Undulator APS Prototype
LHe vessel
SC magnet
He fill/vent turret
20 K radiation shield
60 K radiation shield
Beam chamber
Beam chamber
thermal link to cryocooler
LHe piping
Courtesy of Y. Ivanyushenkov, APS
Installed:
SCU1: , 72 periods, 2m cryostat
Future plans:
SCU2: ,144 periods, 3m cryostat
SCU0
21 periods

## Slide 59
Helical undulator at Novosibirsk
Elias et al., Phys. Rev. Lett., Vol 36 (1976) 717-720
Maximum Field (kG) | 4.7
Yoke | ARMCO
Number of periods | 8
Period length (cm) | 2.4
Maximum current (A) | 428
Length (cm) | 20
Aperture (cm) | 1.8
A. Anashin, G. Kezerashvily, A. Lysenko,
E. Perevedentsev, Y. Shatunov.,
BINP Preprint 84-111 (1984).
G. Kezerashvily, Nucl. Instr. and Meth.
A314 (1992) 15.
Helical Undulator for FEL at 10.6μm
λ0= 32mm, 2.4kG, total length 5m, no iron
The First Helical SCUs

## Slide 60: ILC Prototype Undulator
Courtesy J. Clarke
Undulator to be made of 4m long modules
containing 2 x 1.75m helical undulators

## Slide 61
In-Vacuum Magnetic Field Measurement Techniques

## Slide 62: In-Vacuum Hallprobe Measurement Bench
 | Feed back off | Feed back on
Yaw | 170 µrad | 14 µrad
Pitch | 42 µrad | 11 µrad

## Slide 63
Cable Qualification
Cable tray long term test:
3 cables, 26 wires each
Resistance monitoring
for damage indication
IPAC2016: http://www.ipac16.org/
proceedings/papers/thpow038.pdf
1 single wire damage
after 150.000 cycles
CuBe-sheet damage
after 200.000 cycles
Teststand

## Slide 64: In-Vacuum Moving Wire
Noise is factor of three larger than for existing HZB-system
Partly due to huge field integrals (0.8 Tmm) and
corresponding sensitivity upon wire vibrations
Vacuum chamber not installed

## Slide 65: Summary
Accurate simulation of synchrotron radiation properties
Interaction with electron beam
Field tuning for spectral performance & smooth operation
Undulator design and technology
  Short periods, IVU, SCU
  Polarization control
  On-axis power reduction
  Higher order suppression (quasi periodic)
  Field measurement & shimming