## Slide 1: Shopping list:
HVStripv1 Sr-90 Min-I signals
TJ p-on-p CHESS1 passives - VI and CV curves
CHESS1 – Connecting passive to amp

## Slide 2: HVStripV1 revisited
Chart: Pixel Signal Comparison, 60V-80V - NoShield, Iso, 1800V
HVStripV1
Sr-90 source and reading ch(13,1)
We see change with bias voltage
Running with 40 volts over-night tonight
Self-triggered
Metal layers seem to stop non-min-I electrons.

## Slide 3: TJ p-on-p CHESS1 passive devices
New probe station at Oxford
Chip floating
Use probes to measure current and apply HV to passive diodes on the chip.
  Positive HV put on the signal pad
  Guard rings floating
  Vbias held to ground
Similar procedure for CV measurements

## Slide 4
They hold positive voltage  Todd gets excited again!
Notes: Two 40x40 curves are the easy ones to see, broke down a little later than the other diodes
All other diodes are almost entirely overlaying each other
If allowed to continue, would create a smooth rise, but would be dangerous due to sudden jumps in current
Other chips gave almost exactly the same results, overlaid on top of each other

## Slide 5: CV Chip 6
Can we figure out a way to amplify a fullly depleted passive sensor??
Notes: Can see that the capacitance is higher for the larger chips
The curve is smoother at higher frequencies for testing
40x40 depleted around 25V, whereas the other two are closer to 20V
Means that operating voltage for the 40x400 and 40x200 is between 20V and 70V

## Slide 6
p. 6
TJ-CHESS-1 PonP daughterboard – bonding diagram
Each of the following pages shows a portion of the bonds needed. Please combine all bonds shown.
This diagram applies to both the v1 blue and v2 black PonP daughterboards.
Bonding Layout | X21
Version | 1
Date | 02/08/2016
Changes since previous version: v1: Very experimental | 
Pad group | Structure(s) bonded
Pad group FA | 3
Pad group FB | 0
Pad group FC | 0
Pad group CA | 0
Pad group CB | 0
Pad group CC | 0
Pad group CD | 0
Passive pixels pads | 17, 18, 19
Which structures are bonded in this layout:
This is a new layout for connecting the passive pixels to the amplifiers. It is NOT in the document “OverMOS1_PPD_testing_proposal.docx” by Fergus Wilson. See Richard or Todd for feedback/input/coffee.
TJ-CHESS-1 PonP structure numbering:

## Slide 7
TJ-CHESS-1 PonP daughterboard – bonding diagram
- introductory page
VDD3V3
1
Pad Groups
Pad Groups
FC
FB
FA
CC
CB
CA
CD
VSS (GND)
VDD1V8
Bias_GR1
Bias_GR2
vPreAmpCascN
vShaperCascN
iBias_SF
iBiasPreAmp
iBiasShaper
preRstInt_in
9
1
9
1
9
1
9
1
9
1
9
1
4
AMP_IN
Passive Pixel Pads
Chip pad - high voltage bias
Pad size: 6186.8μm x 5517.4μm
Expected diced chip size is: max 5989μm x 5217.4μm
VDD3V3
VSS (GND)
VDD1V8
Bias_GR1
Bias_GR2
vPreAmpCascN
vShaperCascN
iBias_SF
iBiasPreAmp
iBiasShaper
preRstInt_in
NOT TO SCALE
Vout
Vout
Vout
Small pads are
130μm x 300μm
with 100μm gap
Bonds anywhere along these long pads are equivalent.

## Slide 8
TJ-CHESS-1 PonP daughterboard – bonding diagram
[2/5] This page shows the outer or upper level (throw) of bond wires, for the passive pixels. Connect these second.
1
3
10
11
4
2
9
5
7
15
8
6
16
17
18
19
14
12
13
NC
Blue = inner or lower level of wire bonds
Red = outer or upper level of wire bonds
NC
NC

## Slide 9
TJ-CHESS-1 PonP daughterboard – bonding diagram
This page shows the wire bonds for the capacitors,
high voltage and passive pixel ‘jumpers’
Blue = wire bonds
If using large pads to probe passive pixels, jumper these pads.
DC blocking Capacitor
Flying lead to C1/Pad 8
C1

## Slide 10: Summary
HVStrip1 showing signs of increased signal with increased bias voltage
Passive devices on TJ CHESS1 Can hold voltage if you bias the input pad
  This will not work on active devices because of a current path to the on-sensor amplifier.
    But we CAN AC couple the passive devices to the stand-alone amplifiers on the chip! So we are going to try this.
  CV curves obtained; how do they look?
Studying (again) how to run CHESS1 motherboard.