## Slide 1
Martin Schmeißer M&T annual meeting
01.02.2017
Development of CsK2Sb Photocathodes for High-Current SRF Electron Injectors

## Slide 2
high-current Photoinjectors
Photoinjectors for new accelerators require
High brightness
High average current
Photocathode QE > 1% allows mA current
SRF technology allows high gradient and cw operation
SRF photoinjector with normal conducting cathode
Photocathode exchange system

## Slide 3
high-current Photoinjectors
Spectrometer dipole
slit scanner
Wirescanner, Screens
Faraday Cup,
Screen, BPM
beam energy | < 3.5 MeV
bunch length | < 6 ps rms
bunch charge | < 100 pC
repetition rate | < 30 kHz
TCAV
Photocathode
Transfer System
Image D. Böhlick

## Slide 4
Aim:
0.5 mm mrad emittance from gun
100mA in cw operation
2ps rms bunch length
Boundary conditions:
1% QE at 515nm req‘s 23W avg laser power on the cathode
High-QE semiconductors are highly reactive, survive only in 10-10 mbar vacuum
10ps rms Gaussian bunch with 77pC has 3A peak current
515nm available as 2. harmonic of Nd or Yb lasers
PhotoCathodes

## Slide 5
Alkali Co-Deposition Process
Momentatron
Vacuum suitcase
p < 1x10-11 mbar
p = 8x10-10 mbar
p = 6x10-11 mbar
p = 8x10-11 mbar
Spectral quantum
efficiency measurement

## Slide 6
Alkali Co-Deposition Process
Conventional process (sequential growth of Sb, K, Cs) leads to good results when K-Sb material has only partially reacted
Alkali co-deposition (K+Cs on Sb) yields good sample performance and is easier to reproduce

## Slide 7
Recent results (P013)
Photocathode P013 grown on a Mo substrate:
30nm Sb deposition at 150°C
K + Cs co-deposition at 150°C, reduce to 120° after 250min, finally let cool

## Slide 8
Recent results (P013)
No degradation of the performance was observed during cooling to -120°C.
Movement of the cold sample (exposure to p > 10-9 mbar) results in loss of QE.
 time

## Slide 9
Transfer System #1 at Prep Chamber
Transfer System #2 at Gun Module
Cathodes must be stored and handled in < 10-10 mbar UHV
Vacuum suitcase is available. Vacuum ~ 1*10-11 mbar
Suitcase and plug design are compatible to HZDR gun
Stability with NEG + getter pump is good for >3 months
All parts : cleaning and assembly in ISO 5 cleanroom conditions
Transfer system 1 is in use
Transfer system 2 ready for final testing, still in the cleanroom
Engineering Design: Petr Murcek (HZDR), Kerstin Martin, Markus Bürger, Andre Frahm
Cathode Transfer system

## Slide 10
Goals - outlook
GunLab commissioning
Installation of transfer system 2
Preparation and Characterization of Cu cathode for GunLab commissioning
  Learn about cathode transfer with a less sensitive sample
  Commissioning of beam diagnostics
  Investigate beam dynamics at low bunch charge
Operation of GunLab with CsK2Sb photocathodes
Further R&D projects
Manufacturing and photoemission experiments with single crystal metals
  Cu 100 and Mo 100
Set up of a scientific cathode preparation chamber for EMIL endstation
  Unique methods compination of hard & soft x-ray analytics

## Slide 11
Acknowledgement
Engineering:
Markus Bürger, André Frahm, Daniel Böhlick, Kerstin Martin
Susanne Schubert, Jared Wang, Howard Padmore
John Smedley, Zihao Ding, Menjia Gaowei
Hans Kirschner, Julius Kühn, Guido Klemz, Georgios Kourkafas, Jens Völker, Eva Panofski , Thorsten Kamps, Andreas Jankowiak
Rong Xiang, Petr Murcek, Jochen Teichert
GunLab and bERLinPro project teams
Sven Lederer
Thank you for your attention!

## Slide 12
cross-section of the gun module
Support posts
80 K shield
Helium gas return pipe
SC Solenoid
HOM
absorber
Cold steerer
Warm
Cold transition
2 layer magnetic
shielding
Cathode
Insert
w/ Plug
Coupler
Cathode transfer system #2
with courtesy of A. Neumann (HZB)

## Slide 13
cross-section transfer system #2
Vacuum suitcase
Gun Module
Cathode insert w/ plug
Manipulator to take the plugs off the sample holder
Plug transport
cart

## Slide 14
Cold string assembly
Valve
Cathode beam tube
Gate valve
Cathode cooler
Cavity with helium
vessel
Cold part
of TTF-III
coupler
Coupler assembly