## Slide 1: Irradiation at Birmingham
K. Kanisauskas, R. Bates, C. Buttar, T. Huffman, J.J John, D. Maneuski, R. Plackett, L. Vigani
Special thanks to L. Gonella, P.P. Allport, D.L. Briglin, P. Dervan, I. Iqbal
ATLAS Strip CMOS Regular Meeting
October 11, 2016

## Slide 2: Irradiated Devices
Two HV-CMOS test chips were chosen for the irradiation campaign
1 × AMS-Chess1 (strips) and 1 × CCPD_LF (pixels)
X-ray and MIP measurements were performed for both devices beforehand
AMS-Chess1
CCPD L-Foundry (Ver A)

## Slide 3: Irradiation Procedure (1)
The irradiation took place at MC40 cyclotron facility at the University of Birmingham (27 MeV proton beam) on 28th of September
Target fluence was set to 1 × 1015 neq/cm2

## Slide 4: Irradiation Procedure (2)
Both chips were biased to -50V, whereas LV was only supplied to AMS-Chess1
The chips were cooled down to -25℃ during the irradiation
LabView program was written to monitor temperatures and leakage currents
Unfortunately Arduino based temperature monitoring system failed during the irradiation (also preventing to further log the leakage currents)
Instead the temperature monitoring data was obtained from the facility

## Slide 5: Irradiation Procedure (3)
During the irradiation issues were encountered with translational stages which prevented to achieve the target fluence for AMS-Chess1
The devices are still being stored at the facility
Measured fluences
AMS-Chess1: 0.62 × 1015 neq/cm2
CCPD_LF: 1.2 × 1015 neq/cm2