## Slide 1
First results with passive devices on CHESS2 chip
I. Mandić, et al., JSI Ljubljana

## Slide 2
Detector
Chip from wafer 13: 200-300 Ohm-cm

## Slide 3
Chip mounted on a simple PCB:
E-TCT:
regular passive pixel array:
3x3 630 um x 40 um pixels
Sr90:
arge passive array
2x32 630 um x 40 um pixels
 bias up to 120 V, currents very low (few nA)
E-tct

## Slide 4
E-TCT
measured charge collection profile across the central pixel
Fit FWHM of the profile with:
 good fit
 extracted Neff corresponds to 200 Ohm-cm
 measured charge collection width about 70 um at 120 V  but large offset at 0 V
 depleted depth probably less than 70 µm :
 for Neff = 6.6 e13 cm-3 and Veff = 120 V:

## Slide 5
E-TCT
2d charge collection profile of the central pixel
six pixel segments can be seen
no efficiency gaps between segments
depth
surface
charge

## Slide 6
detector
ORTEC 142 charge sensitive amplifier + custom made shaper +
digital oscilloscope
HV-CMOS: small signals, large noise  S/N very bad
 must have clean sample of events
 need large detector for reasonable trigger rate
and good collimation, small scintillator
Measurement:
1) Record N waveforms
2) average over all waveforms and determine signal peak
3) sample waveforms at the peak
4) Fill spectrum
5) measure at different shaping times: 25 ns, 80 ns, 200 ns and 500 ns
Source measurements

## Slide 7
Calibration
Am241 source, 59.5 keV photon peak in 300 µm thick FZ detector
Sr90 with 300 µm thick FZ p-type silicon diode
 calibration at 25 ns shaping time : 230 electrons/mV
Averaged waveforms
Bias = 300 V
Shaping time 25 ns
Spectrum of amplitudes at sampling time
Sampling time
Bias = 300 V
Shaping 25 ns
FZ p-type silicon diode, 300 µm thick , Vfd = 70 V:

## Slide 8
Average waveform:
noise
signal
120 V
120 V
Shaping time: 25 ns
Measurement with CHESS2, W13, big array
Spectrum of values sampled at peak
Sampling point for signal
t (ns)
sampling point for noise

## Slide 9
Measurement with CHESS2, W13
depleted depth for 200 Ohm-cm at 120 V: 48 µm
 expected mean charge from depleted region: ~ 48 um x 100 el/um ~ 4800 el
 in total would expect ~ 1500 el more from diffusion?
   maybe alignment between the collimator and the structure not perfect,
  will see with more samples

## Slide 10
Summary and outlook:
First E-TCT and Sr90 measurements with CHESS2
chip from W13 200-300 Ohm-cm resistivity
measurement with passive structures
  3x3 array for E-TCT
  big array for Sr90
Bias up to 120 V, currents low (nA)
resistivity estimated from E-TCT: 200 Ohm-cm
Sr90: 4500 electrons at 120 V
continue with other resistivities
chips were irradiated with neutrons: 1e14, 3e14,5e14,1e15 and 2e15,
one chip per resistivity
  irradiated chips ready to be measured