## Slide 1: Liquid Scintillator Characterization and Development of Detector Monitoring Systems at TUM
Hans Th. J. Steiger
Technische Universität München
Lehrstuhl für experimentelle Astroteilchenphysik
DESY, Hamburg 23.03.2017

## Slide 2: PALM – Precision Attenuation Length Measurement
Sabrina Prummer, PhD Student at TUM

## Slide 3: First Test Measurements
Sabrina Prummer, PhD Student at TUM

## Slide 4: PoLiDe – Positronium Lifetime Determination

## Slide 5
PoLiDe – Positronium Lifetime Determination
H. Steiger, S. Prummer, M. Schwarz, P. Landgraf, M. Tippmann
Schematics of the Setup:
Coincidence Trigger / Tests
Coincidences in the two plastic scintillator detectors are used as trigger signals
Time difference [ns]
Counts / (0.5 ns)
Backscattering of γ‘s on one detector and redetection in the other
137Cs

## Slide 6: Monte-Carlo Simulation of the Setup
Simulation of the setup with Geant4
Investigation & optimization of:
  Geometry
  Offline event discrimination
Saint Gobain BC-400
3-inch PMT
3-inch PMT
Liquid Scintillator
22Na Source
Copper Vessel
Thin layer of highly reflecting Aluminum

## Slide 7: Monte-Carlo Simulation of the Setup
Identify “good” events with the following properties:
  Positron hits LAB and annihilates there
  Both plastic scintillators are hit by a 511 keV gamma
  No 511 keV gamma hits both plastic scintillators
  The additionally produced 1275 keV gamma (from 22Na source) does not hit any scintillator
Identify different “fake” triple events:
  Positron scintillates in LAB but leaves it before annihilation
  The 1275 keV gamma hits one or more scintillators
  One 511 keV gamma hits both plastic scintillators
  Other fake events due to the three gammas
3-inch PMT
1-inch PMT
Mario Schwarz, Master Student at TUM
Integral [V ns]
Integral [V ns]

## Slide 8: Measuring the Non-Linearity of the Liquid Scintillator
Konstantin Schweizer, Tobias Drohmann†

## Slide 9
Measuring the Non-Linearity of the Liquid Scintillator
PRELIMINARY

## Slide 10: Quenching Factor Measurements for PSD in Liquid Scintillators
Holder for calib. source
LS Cell
PMT Dark Box
The Detector Setup:
Cross-section of the LS detector

## Slide 11: Quenching Factor Measurements for PSD in Liquid Scintillators
Setup at the n-facility at the MLL-accelerator
The setup allows a variation of the initial n-energy by measuring in different off-axis positions
Energy dependence of the QF for LAB + 3g/l PPO + 20mg/l bisMSB was already measured
MLL neutron source is a unique facility for investigations with pulsed neutron beams
n-energy visible in the detector measured in different positions
Vinzenz Zimmer, PhD Thesis

## Slide 12: PSD Results from the Setup
Pulsed neutron beam at 11 MeV
LAB scintillator exhibits excellent PSD behavior
Similar results from B. von Krosigk et al., Eur.Phys.J. C73 (2013) 4, 2390
LAB + 3g/l PPO + 20mg/l bisMSB
tt = 28.5ns
Vinzenz Zimmer, PhD Thesis

## Slide 13: Detector Monitoring Systems – Filling Level Measurement System and Slow Control

## Slide 14: Level Measurement (Experiences from Double Chooz)

## Slide 15: Hydrostatic Pressure Sensors (HPSs)
Picture of a hydrostatic pressure sensor (HPS) . The housing is completely made of stainless steel and the supply cable is coated with PTFE.
HPS installed in the Gamma Catcher. The sensor is glued to the bottom center of the acrylic vessel.

## Slide 16: Critical Point Sensors (CPS)
The CPSs are composed of two optical fibers leading to an optical cone.
An amplifier sends light through one of the fibers into the optical cone, the light is totally reflected and sent back via the second fiber to the amplifier.
When the cone is submerged, the refractive index around the cone changes (from air to liquid) and the light is not totally reflected anymore.
CPS positioned between the main body and the chimney of the acrylic vessels.
Installation details and dimensions of the sensor-tip
Overview of the CPS-installation in gamma catcher and target and its connection

## Slide 17
Development of a Monitoring System for the Radon Concentration in gaseous Nitrogen
To vakuum pump
Vacuum vessel with 226Ra source
Main Valve
Counter tube
Length: 25.4 cm Diameter: 15.24 cm
Counting gas filling valve
Inhouse produced preamplifier
To ADC and HV source

## Slide 18: Thank you for your attention!

## Slide 19: Questions?