## Slide 1
Michael Steinke on behalf of LZH/AEI team
03.05.2017
Laser development for gravitational wave detectors
State of the art and the future

## Slide 2: LZH Facts
  Non-university, non-profit research
  center in Hannover
  Founded in 1986 at University
  Built in 1991,extensions in 1997/2008
  Staff of 180 people (w/o students)
  Turnover ~18M€ per year
  ~3M€ basic funds
  Total area ~ 10,000 m²
  Shop floor ~ 1,400 m²
  Clean room 300 m²
  28 Labs

## Slide 3
LZH Research focus
OPTICAL COMPONENTS AND SYSTEMS
  Optical Coating Technology
  Fiber Components
  Lasers
OPTICAL PRODUCTION TECHNOLOGIES
From nano to macro:
  Precise Surface Processing
  Generative Processes
  Joining and Cutting of Metals
  Processing of Non-Metals
BIOMEDICAL PHOTONICS
  Biomedical Engineering
  Laser Medicine
  Biophotonics

## Slide 4: How to measure Gravitational Waves?
Beamsplitter
Mirror
Interference
Photodetector
Interferometric gravitational wave detectors
  Michelson type
  Suspended (free falling) mirrors
  Gravitational wave causes phase shift between the interferometer arms
The mirrors do not really move locally, but the effect is the same and it is easier to imagine the physics

## Slide 5: Current Detector network

## Slide 6: Requirements on the laser sources
Fundamental mode (TEM00) operation
Linear polarization (PER >100:1)
Good frequency and amplitude stability
High output power (shot-noise scales with )
Single-frequency operation (kHz)
High reliability (24/7 operation)
Easy maintenance
Requirements very challenging and unique

## Slide 7: Non planer ring oscillator (NPRO)
Output power: 2 W
Beam quality (M2x,y): < 1.1
Line width: 1 kHz / 100ms
Output
beam
Pump
Light
3 x 8 x 12 mm
 Output power limited to 2W

## Slide 8: Solid-state laser technology
Solution: Solid-state (rare-erath doped crystals) laser technology to amplify NPRO
  Amplifier configuration
  Injection locked laser configuration
From seed
Amplified
output
Pump diodes
Pump diodes
From seed
Amplified
output

## Slide 9: GEO and VIRGO laser systems
GEO:
  NPRO seed
  35W Nd:YVO4 amplifier stage
VIRGO:
  NPRO seed
  20W Nd:YAG injection locked stage
  60W Nd:YVO4 amplifier stage (same as GEO)
GEO:
VIRGO (injection locked stage):

## Slide 10: LIGO laser systems
Nd:YVO4 amplifier stage similar to GEO system
Nd:YAG Injection locked high-power stage with four laser heads

## Slide 11: Laser head design
1. Water cooled base
2. Pump source: fiber bundle of 7 fibers
3. Pump light homogenizer
4. Pump light diagnostics: Power & Spectrum
5. Pump light imaging optics
6. 45° dichroic mirror
7. Pump light beam dump
8. Water cooled pump chamber for
Nd:YAG laser crystal
9. ASE beam dump
3
4
5
7
6
8
9
1
2

## Slide 12: Transverse mode control – laser setup
One major issue
  How to design resonator such that it is stable for pure TEM00 mode?
  Note: need to include thermal lensing in design
Setup for investigation on transverse mode behavior: 2 head system

## Slide 13: Transverse mode control – resonator design
symmetric resonator with short distances

## Slide 14: Transverse mode control – resonator design
symmetric resonator with long distances

## Slide 15: Transverse mode control – resonator design
slightly asymmetric resonator with long distances

## Slide 16: Transverse mode control – resonator design
strongly asymmetric resonator

## Slide 17: Transverse mode control

## Slide 18: Power scaling: 2 heads  4 heads
“Just” double the resonator: 2 heads  4 laser heads

## Slide 19: Transverse mode control – 4 head cavity design
Beam profile at ~165W:

## Slide 20: Beam quality
After high power oscillator
After high power mode-cleaner
> 88 % in TEM00 mode @ 220 W of output power from the oscillator
< 2 % in higher order modes
Transmitted output power after HPPMC > 165 W

## Slide 21: State of the art Ligo laser systems
Two laser systems have been installed in Livingston & Hanford
A third system is waiting for installation in LIGO India
~165W in TEM00 mode
kHz linewidth (single-frequency operation)
PER ???

## Slide 22: State of the art
Lessons learnt regarding the injection locked laser concept
  Not that easy to operate and maintain
  Shows significant pointing
  It has a working point
  …. not used during LIGO detection runs…...
LIGO and VIRGO thinking about 100W-class amplifiers
  Low single-pass gain
  Thermal lenses also part of design
  Complex & bulky
  100W seems realistic
Cryogenic detectors will require lasers with wavelength >1.4µm
Do we want to stick to solid-state technology for 3rd generation GWDs?
Isn't there a promising (better) alternative?

## Slide 23: Fiber technology
Became very promising over last two decades
Supported by commercial applications (in particular laser processing)
Still very active in terms of research
Advantages | Disadvantages
Wave-guiding High gain levels Amplifiers already promising | Long interaction lengths Non-linear effects Amplified spontaneous emission
No thermal lens | Modal instabilities
Beam quality given by design | Can’t freely chose fiber design (limited by technology and non-linear effects)

## Slide 24: Fiber technology
Tight requirements of GWDs
on reliability
Research:
  Ongoing at 1µm, 1.5µm and 2µm
  Lot of optical concepts
  Optical performance seems promising
  Which concepts to use?

## Slide 25: Fiber prototype at 1064nm
Seed source: NPRO with 2W output power
Fiber based single-mode 20W pre-amplifier
Two fiber spools for external thermal management of the active fiber
Home-built integrated 4+1x1 fiber combiner for counter pumping
Pump fibers directly fused to the active polarization maintaining fiber

## Slide 26: Fiber prototype at 1064nm
Pre-amplifier: 30W
Main amplifier: 200W
PER: 18dB
TEM00 content: >90%
Successfully long-term (600h) tested at 120W
Problems with pump combiner at higher power levels
Functional prototype
  Successful verification of (optical) concepts
  Next step → engineering prototype
NPRO
Pre-Amplifier
Main-Amplifier

## Slide 27: Fiber prototype at 1550nm
State of the art at 1550nm
  Max. 55W in TEM00 mode
  Specialty fibers (non-PM)
  Not monolithic
Our goal (together with AEI)
  100W
  Monolithic
  No specialty fibers & PM fibers
  Functional/engineering prototype
Promising result*
  200W
  Monolithic with commercial double-clad fibers (non-PM)
  „Good“ beam quality, no SBS
* Proc. SPIE 9728, Fiber Lasers XIII: Technology, Systems, and Applications, 97282L (March 11, 2016); doi:10.1117/12.2212480

## Slide 28: Fiber prototype at 1550nm
Simple (and all-fiber) architecture
Er/Yb codoped active fiber
Home-built fiber components

## Slide 29: Fiber prototype at 1550nm
Pumping scheme
  At 940nm (off-resonant)
  Supresses saturation of Yb-to-Er energy transfer
  Longer fiber required → SBS issue!?
Suppression of SBS
  Backward pumping
  Large mode area (LMA) fiber
    25µm core, 300µm cladding
    Commercially available (non-PM and PM)
    Excitation of FM via mode field adapter
    Use coiling-induced losses of HOMs

## Slide 30: Fiber prototype at 1550nm
Linear slope up to 111W
No Yb-band ASE and good suppression (~60dB) of Er-band ASE
Output power limited by pump power

## Slide 31: Fiber prototype at 1550nm
SBS-free
<1% power fluctuation on 1 hour scale
Polarization stable (~13dB) after warm-up time
  Next upgrade: Active spool temperature stabilization and PM fibers

## Slide 32: Fiber prototype at 1550nm
98.4% TEM00 content at output power of 10W
97.3% TEM00 content at output power of 55W
94.8% TEM00 content at output power of 111W
In combination with measured PER: 100W in linearly polarized TEM00 mode

## Slide 33: Fiber prototype at 1550nm
Frequency noise of amplifier determined by seed
Calculated linewidth
  20kHz (100ms/10Hz)
  1064nm NPRO: 1kHz (100ms/10Hz)
Interfaces for external stabilization
  Fast actuator: Piezo
  Slow actuator: Temperature
  (Similar to NPRO)
  External EOMs (for PDH stabilization) available at 1550nm

## Slide 34: Fiber prototype at 1550nm
Frequencies >1kHz
  Determined by seed
  Except “resonance” around 10kHz at 110W
Frequencies <1kHz
  Most probably determined by seed and pump
Stabilization via feedback to pumps feasible
  Low-pass transfer function
  Cut-off frequency given by effective lifetime → 1-10kHz

## Slide 35: Fiber prototype at 1550nm
Where we are
  100W lab/function prototype at 1550nm
Next steps (towards function/engineering prototype)
  Upgrade to PM fibers
  Design/development of pre-amplifier
  Minor upgrades of optical concepts (e.g. optimization of fiber length)
  Engineering
    Mechanical, electrical, cooling etc. concepts
    Optimization of fiber components
    Take profit of experiences at 1064nm (and aLIGO system)
  Further power scaling (200W is realistic)

## Slide 36: SBS Suppression schemes
  Side band modulation with fiber coupled EOM
  5W pre-amplifier
  Demodulation with high power EOM

## Slide 37: SBS Suppression schemes
SBS threshold increased from 60 W to 88 W  factor 1.5
Limited by SBS and pump brightness

## Slide 38: SBS Suppression schemes
SBS threshold increased from 60 W to 88 W  factor 1.5
Limited by SBS and pump brightness

## Slide 39: Coherent combination
  Use fiber coupled splitters / combiners
  Use knowledge gained from dynamics considerations  Control differential phase by tuning the pump power!
  Differential pump power control:
    Tunes phase
    Leaves combined power unchanged (in 1st order)

## Slide 40: Coherent combination
  Max CBC output power: 25 W
  CBC efficiency: > 95 %
  Stable locking for > 0.5 h
    For long term operation additional long-range actuator needed (e.g. thermal control)
  Control loop unity gain frequency: ~1 kHz
    Limited by laser diode power supply
  No power noise degradation due to locking scheme
  Beam quality determined by single-mode fiber: > 97% in TEM00

## Slide 41: THANKs FOR YOUR ATTENTION

## Slide 42: Challenges aLIGO solid state system
  Complexity
    How to simplify complexity? How to simplify alignment of laser to point of operation?
    How to simplify repair & maintenance?
  Pointing
    Where does it come from?
      Inherent feature of free-space scheme (coupling of mechanical noise)
      Coupling of thermal lensing with external perturbations
    How to suppress it? Can we counteract it (stabilization)?
    Will it be better with an amplifier (instead of injection-locked laser) configuration?
  What about solid-state technology if we aim for longer wavelengths (1550nm or 2000nm)?

## Slide 43: Challenges fiber technology
  Fiber design
    Good point: We will have a fiber draw tower in Hannover soon 
    Are non-standard (step-index) fibers an alternative for monolithic systems?
    How to push the limits of standard step-index fibers?
      Single-mode behavior
      Photo-darkening
  Fiber components
    Degradation under high-power operation
    Reliability
  What is the best (most reliable) way to suppress SBS? Where are the limitations?
  Will we ever encounter modal instabilities? How to counteract them?

## Slide 44: Limitations of fiber amplifiers - MI
Modal instabilities (MI)
  Threshold-like onset of modal instabilities in high-power fiber amplifiers
  Beating of modes  inversion grating  temperature grating  refractive index grating  stimulated/driven energy transfer between modes
  Hot topic regarding the power scaling of fiber amplifiers at 1.0µm
Eidam et al., Optics express 19 (14) 2011

## Slide 45: Further challenges
  Which seeder technology to use at longer wavelengths?
    No NPROs available
    External cavity laser diodes seem to be promising
    Fiber lasers are ok but have larger linewidths
    Whispering gallery mode lasers with very narrow linewidth (but expensive)
  No real experiences with single-frequency fiber amplifiers at around 2000nm (optical specs are fine but long-term stability etc.)
  Funding?

## Slide 46: Prospects and challenges: Power scaling @ 2.0µm
Fiber technology at ~2.0µm is evolving significantly (driven by commercial interests)
  Suitable coating materials (for high power operation)?
  What about photodarkening (modal instabilities)?
What about single-frequency seed sources at ~2.0µm?
  Fiber lasers (e.g. from NP Photonics or AdValue Photonics)
  Whispering gallery mode lasers (e.g. from OEwaves)
  What about their noise levels etc.? Are they already appropriate?
photonics-usa.com

## Slide 47: Going beyond 2µm
Holmium (Ho3+) emits efficiently around ~2.1µm
  So far, no demonstration of single-frequency fiber amplifiers
  Record CW output power: 407W* (monolithic fiber laser, cladding-pumped)
  Drawbacks**:
    Can only be pumped at
      ~1.9µm (by Thulium-doped lasers/amplifiers)
      ~1.15µm (Ytterbium-doped laser/amplifiers and/or Raman fiber lasers)
    Most high-power demonstrations relied on all-glass fibers
      High absorption of polymer coating
    Silica absorption increases significantly above ~2.1µm
    Experimental slope efficiencies are rather low
      Background infrared silica losses, absorption by OH- groups, re-absorption and non-radiative decay processes
* Hemming et al., CLEO 2013, OSA Technical Digest, paper CW1M.1
** Jin et al., Journal of Electronic Science and Technology, 13 (4) 2015