## Slide 1: The “Gen-II” LAPPDTM: Large-Area Ceramic-Body Planar MCP-based Photo-Detectors E. Angelico, A. Elagin, H. Frisch, E. Spieglan University of Chicago
20x20 cm2
~15mm
Large-Area Picosecond
Photo-Detector
Single PE time resolution <50ps
Gen-II LAPPD development is a joint program between the University of
Chicago and Incom Inc.
Gen-I LAPPDs are now commercially
available through Incom Inc.

## Slide 2: PMT-like Batch Production
Air transfer of the window
with pre-deposited Sb layer
Gen-II LAPPD tile #21
Indium seal and bake-out are done at the same time
Cs vapors are introduced from an external source
Many devices can be processed at the same time
using shared vacuum distribution system
Pulses from tile #21
MCPs work after
exposure to Cs
Arbitrary units
Arbitrary units
The goal is to develop an inexpensive process
scalable to a production rate of > 50 LAPPDs/week
A photo-sensitive material
(Cs-Sb) is formed over the
entire 20x20cm2 surface
of the window