## Slide 1: Proton irradiated passive test strucutres on CHESS 2
Bojan Hiti, Igor Mandić et al.
Jožef Stefan Institute, Experimental Particle Physics Department (F9)
Ljubljana, Slovenia
Strip CMOS regular meeting, 09.11.2017

## Slide 2: Samples
φ (1014 neq cm-2) | 20 Ω·cm (W1) | 50 Ω·cm (W7) | 200 Ω·cm (W13) | 1000 Ω·cm (W19)
4.2 | CERN PS | n.a. | CERN PS | CERN PS
7.7 | Los Alamos | Los Alamos | Los Alamos | Los Alamos
8.7 | CERN PS | n.a. | CERN PS | CERN PS
14 | n.a. | Los Alamos | Los Alamos | n.a.
36 | n.a. | Los Alamos | Los Alamos | n.a.
Irradiation hardness studies with CHESS2 carried out in Ljubljana:
  reactor neutrons (Ljubljana) – 4 resistivities, 5 fluences (1e14 – 2e15 neq/cm2)
  24 GeV protons (CERN PS) – 3 resistivities, 2 fluences
  800 MeV protons (Los Alamos) – 4 resistivities NEW
Characterization of passive structures using Edge-TCT and Sr90
Measurements before and after annealing
Table of proton irradiated samples/fluences

## Slide 3: Test structures
Test structures:
3 x 3 pixel array for Edge-TCT (pixel size 630 x 40 μm2)
Large pad for Sr90 measurements (1.2 x 1.2 mm2)
Edge-TCT
array
Sr90 pad
to external amplifiers
proton beam radius at Los Alamos
What fluence did the Edge-TCT structure receive?

## Slide 4: Edge-TCT: quick reminder
Generate charge carriers at a fixed depth in the sample using narrowly focused (10 μm) infrared laser
Measure collected charge at a given depth (pulse integration time 5 ns)
Run a scan along sample depth to determine depleted depth (y-direction)
Only signal from the central pixel is amplified
Peripheral pixels are biased, but not read out
IR laser beam incidence
HV
scope
GND
Substrate (p-type)
Pixels (n-well)
Beam direction
x
y

## Slide 5: Edge-TCT charge collection profile
surface
depth
surface
end of depletion zone
scan direction
Depleted depth is evaluated as FWHM of the charge collection profile

## Slide 6: Edge-TCT Results W1 (20 Ohm-cm)
surface
depth
neutrons

## Slide 7: Edge-TCT Results W7 (50 Ohm-cm)
surface
depth
neutrons

## Slide 8: Edge-TCT Results W13 (200 Ohm-cm)
surface
depth
neutrons

## Slide 9: Edge-TCT Results W19 (1000 Ohm-cm)
surface
depth
neutrons

## Slide 10: Neff vs. fluence
Acceptor introduction rate is lower with protons than with neutrons
Common in oxygenated material
proton Los Alamos

## Slide 11: 90Sr setup
HV-CMOS: small signals, large noise  S/N very low
  clean sample of events needed (no hits missing DUT)
  require a large detector (trigger rate), good collimation, small scintillator
Measurement:
  1) Record N ( = 2500) waveforms
  2) Average over all waveforms and determine time of the signal peak
  3) Sample waveforms at the peak and fill the spectrum
  4) Fit the spectrum with a convoluted landau+gauss function
detector
ORTEC 142 charge sensitive amplifier + custom made shaper (25 ns)
+ digital oscilloscope
ampl.
90Sr
PMT
cooling jig
DUT

## Slide 12: Typical Sr90 spectrum
noise peak
signal peak
deposited charge = shift between noise and signal

## Slide 13: Sr90 measurements
Chart: Vbias (V)
| 95 | 80 | 64 | 47 | 31 | 15 | 0
W1 7.7e14p ann | 1983.24 | 1680.245 | 1459.885 | 1184.435 | 881.44 | 661.08 | 247.905
W7 7.7e14p ann | 4186.84 | 4985.645 | 5811.995 | 6252.715 | 385.63 | 1900.605 | 3029.95
W7 1.4e15p ann | 4875.465 | 4434.745 | 3773.665 | 3167.675 | 2368.87 | 1349.705 | 275.45
W7 3.6e15p ann | 2038.33 | 1900.605 | 1680.245 | 1239.525 | 964.075 | 468.265 | 192.815
W13 7.7e14p ann | 275.45 | 1267.07 | 2148.51 | 3112.585 | 3856.3 | 4710.195
W13 1.4e15p ann | 4930.555 | 4076.66 | 3580.85 | 2947.315 | 2258.69 | 1294.615 | 247.905
W13 3.6e15p ann | 247.905 | 4682.65 | 4655.105 | 1404.795 | 2341.325 | 3250.31 | 3828.755
Collected charge vs. bias voltage for different resistivities / proton fluences

## Slide 14: Sr90 measurements
Very high amount of charge in the wafer of the highest initial resistivity
Chart: Vbias (V)
| 90 | 76 | 62 | 47 | 32 | 17 | 0
W19 7.7e14p ann | 14901.845 | 13524.595 | 12092.255 | 9861.11 | 7244.335 | 3883.845 | 385.63

## Slide 15: Sr90 Comparison for different substrates
Preliminary!
With Sr90 the charge in proton irradiated samples is much higher than in neutron irr.
dashed lines:
proton irr.
full lines:
neutron irr.

## Slide 16: Possible explanation for missing charge
Discrepancy between expected charge (Edge-TCT – depleted depth) and measured charge (Sr90): 50 % less charge collected than expected
The reason is due to top biasing
  Drift of both types of charge carriers ends on the chip surface
  Holes have to drift through a low E region, where trapping is high
  Trapped charge carriers only pass a part of the weighting field (Shockley Ramo theorem)
  The effect is strongly mitigated by a processed and metalized back plane
  Observed in LFoundry CMOS chips with and without processed back plane
n-well (+HV)
p-ring (gnd)
electrons
holes
low electric field

## Slide 17: Summary
Collected charge is roughly proportional to the depleted depth
Proton irradiation induces less effective space charge than neutrons
  Increased depletion zone at same fluences
  More charge
The absolute amount of collected charge is smaller due to trapping related with top bias