## Slide 1: Advanced Interconnects
Helmholtz Program: Matter and Technologies
PoF III Topic: Detector Technologies and Systems
DESY Research Unit: Detector Developments
Karsten Hansen
Center Evaluation DESY, 5 – 9 February 2018
In-house Bump Bonding

## Slide 2: Introduction
Essential Parts of a Detector System
Sensor
Readout
Interface
Data Acquisition
2. Future Aspects
PCB with 10-GE Link
HGF-AMC
Hybrid
  1. DESY Bump Bonding Facility
ASIC
Sensor
Bump
  Scope of this Talk
ASIC
Process Extension
higher Granularity
higher Integration Density
increased Bandwidth
(see previous Talks)

## Slide 3: In-house Bump Bonding
DESY Process with two Machines
1. Solder-Ball Placement (SB2-Jet)
2. ASIC Placement (FEMTO)
  Formic-Acid Cleaning
  Ball Reflow
  Module Reflow
Special Pick & Place Tool
DESY has both Chip-Level Processes (Bumping & Bonding) In-House
small Number of additional Tools → Equipment is very flexible also for Prototyping
Capillary
Solder Balls
Singulation Disk
Chip-to-Chip

## Slide 4: In-house Bump Bonding
Process Steps
1. Under-Bump Metaliz.
2. Bumping
3. Ball Reflow
4. Bonding
Lead-free
40-µm Balls
1.2-µm Accuracy (1-σ)
≤ 4.5 Bumps per Second
5. Module Reflow
Bare Module
18.9 mΩ per Bump
16 cN per Bump
external
Ball Placement
ASIC Placement
Pd / Au Finish
40 µm
100 µm
external X-Ray CT
Ni
We can run the full Assembly Chain from Ball Placement to the complete Module in a reliable Way.
Imprint
uniform Contact Array

## Slide 5: In-house Bump Bonding
CMS Pixel Detector Upgrade Phase I
Volume 418 Modules with 6,688 ASICs
Rate 6.7 Modules per Week
Connectivity Yield ≥ 99.96% best 256 Modules
Module Yield Loss
  missing Connections 1.2%
  high Sensor Leakage 3.3%
  ASIC Failures 1% after Repair
Bare Module with 66,592 Bumps
Connectivity Map of a Class-A Module
: missing Connection
½ Barrel Layer 4 (0.32 m²)
Sensor (6.7x1.9 cm²)
16 ASICs
256 x
32 cm
84%
96%
DESY
Yield Span
Five Production Sites:

## Slide 6: In-house Bump Bonding
Towards smaller Pitches and Copper Metallization for SiPMs
ASIC (16x16 Pixel)
Ball Placement
ASIC Placement
X-Ray
SiPM Sensor
ASIC
Cu-RDL
50 µm
Feasibility of 30-µm Balls at 50-µm Pitch: common Activity with Industry & Semiconductor Lab of MPG
The Process can also be applied for a higher Pixel Granularity.
50-µm Pitch is currently State-of-the-Art in our Community.
Quality is comparable to conventional Wafer-Level Processes.

## Slide 7: Future Aspects
Higher Pixel Granularity → more Functionality → higher Integration Density & Bandwidth
Density: Si Interposer
Bandwidth: Si-Photonics IC
Through Silicon Vias
Laser
Waveguide
ASIC
Fiber
Modulator
Detector
Redistribution Layers
ASIC
active CMOS Layer
Photonic Layer
Coupler
excellent Platform for multi-Chip Integration towards the 3rd Dimension
additional active Functions in Interposer & Photonics IC
DESY’s Bump Bonding Process is applicable
independent of specific IC Technologies
KIT’s & CERN’s Si Photonics Activities
IZM/DESY
Courtesy of KIT
TSV Example
PIC Example

## Slide 8: Summary & Outlook
We successfully applied the DESY Process for a Series Production with 100-µm Pitch
We demonstrated the Feasibility of 50-µm Pitch and Cu UBM
Our process can be applied for the Assembly of Interposers and Photonics ICs
optical
electrical
Photonic IC
ASICs
Sensor-ASIC Stack bump connected to Interposer
Interconnects
Interposer with TSV
Polymer Waveguide
optical Uplink
Flex Cable
Sensor
Readout
Interface w/ optical I/Os
Compact Integration