## Slide 1: Nióbio e CBMM
Abril/2018
RIKEN, Nishina Center
June 26, 2018
TTC Meeting

## Slide 2: The company

## Slide 3
CBMM

## Slide 4
Niobium Suppliers
9.000 FeNb tons/year
1.500 FeNb tons/year
13.700 FeNb tons/year
100.000 FeNb tons/year
CBMM is the top worldwide producer of Ferroniobium.

## Slide 5
CBMM - Products
Ferroniobium
Niobium Oxide
Special Alloys
High Purity Niobium Metal Ingot
High Purity
Optical grade
NiNb VG
FeNb VG

## Slide 6: Niobium Metal Refining Process

## Slide 7
Raw Material
Sojitz
Tóquio - Japão
~ 95% Niobium metal
~ 5% Aluminum compounds and ore residual elements
Typical ATR bar composition
(ATR bars - Global Reaction)
3 Nb2O5 + 10 Al = 6 Nb + 5 Al2O3
Niobium Oxide
High Purity
ATR Bars

## Slide 8
Refining Process – EB melting
High Purity
Niobium Metal
1st melt
Re-melts
Raw material
ATR ~ 95% Nb

## Slide 9
Niobium Metal Products
Production Capabilities
  Ingots dimensions:
    Diameter: From 150 mm up to 400 mm
    Length: Up to 2200 mm
  Ingots Specifications
    Reactor grade (Ta < 1000 ppm)
    Commercial grade (1000 < Ta < 2000 ppm)
    RRR grade

## Slide 10: Production point of view Traditional Specification for Niobium Sheet X Specification for Ingot Technology

## Slide 11: Traditional Specification for Niobium Sheet

## Slide 12
Traditional Specification for Nb sheet
RRR > 300
Ingot required to produce RRR sheets.
Critical points

## Slide 13
Impacts on production costs
Production Impacts
Multiple melting
Lower material yield due to the high volatilization
Lower melting rate
Low productivity
Higher production cost

## Slide 14: Specification for Ingot Technology

## Slide 15
Specification for Ingot Technology
Standard Specification

## Slide 16
Standard Specification
Production Impacts (Loosen Ta + Lower RRR)
Cost saving with raw material with higher Ta
Fewer melting numbers
Higher yield
Normal melting rate
More productivity
Lower production cost.
Approximately 50% less than higher RRR material
Impacts on production costs

## Slide 17
Other potential cost savings
Sojitz
Tóquio - Japão
Reduce the overall cost of manufacturing superconducting cavities by reducing the manufacturing steps (currently 16 steps).

## Slide 18
Visite o site: niobium.tech