## Slide 1: Large Grain Cavities at DESY
TTC Meeting,
Riken, 27 June 2018
Jacek Sekutowicz
for DESY testing team

## Slide 2
Outline
Motivation
LG Niobium used at DESY
Performance of LG cavities
XM-3 history
Recent tests
CW upgrade scenario for E-XFEL
Summary

## Slide 3
Motivation
An R&D program on SRF cavities at DESY is devoted to cw upgrade of E-XFEL
Before upgrade: 101 CMs in total, 17 in the IS and 84 in L3
After upgrade: New 17 CMs modified for cw will be installed in the IS
113 CMs in total, 17 in the IS and 96 in L3
12 present CMs from the IS will be re-installed at the end of L3
BC2
BC1
3H
Undulators
e- gun
L0 ; 1CM
cw:16 MV/m
L1; 4CMs
cw:11 MV/m
L2; 12CMs
cw: 15 MV/m
L3; 84 (96) CMs
Injector Section (IS): E=2-2.5 GeV

## Slide 4
Motivation, cont.
Main goals of the SRF R&D program
CW modification of the 17 CMs in the Injector Section (mainly He distribution and FPCs)
To define “cw” SRF technology for 136 cavities housed in that 17 CMs
Specification of the performance for the 136 cavity
    Eacc 28+ MV/m for operation in the nominal short pulse mode (Pulse 1.3ms, 10Hz)
High Qo at Eacc of 16 MV/m for cw operation
Low sensitivity to the magnetic flux (we want to keep shieldings )
Currently we investigate infusion and large grain

## Slide 5
LG Niobium used at DESY
In 2006 ACCEL (now RI) built 11 large grain TESLA cavities made of the Hereaus ingot
Courtesy W. Singer
Courtesy W. Singer
9-cell large grain TESLA cavity

## Slide 6
Performance of LG Cavities; Vertical test at 2K
Chart: Eacc [MV/m]
| 1190000 | 659000 | 365000 | 1190000 | 1930000 | 3170000 | 4690000 | 4600000 | 6130000 | 8380000 | 11900000 | 14400000 | 17600000 | 21600000 | 26200000 | 28200000 | 28900000 | 29400000 | 29900000 | 30400000 | 30700000 | 31100000 | 31400000
AC114 | 22300000000 | 21100000000 | 20100000000 | 22500000000 | 23100000000 | 23900000000 | 23800000000 | 20400000000 | 20400000000 | 21000000000 | 22800000000 | 22800000000 | 23500000000 | 22900000000 | 20900000000 | 18800000000 | 16100000000 | 14000000000 | 11600000000 | 9390000000 | 7760000000 | 6600000000 | 5670000000
AC156 | 23800000000 | 25000000000 | 25100000000 | 24500000000 | 23100000000 | 22000000000 | 20800000000 | 20000000000 | 19400000000 | 19200000000 | 19100000000 | 19000000000 | 18900000000 | 18900000000 | 18600000000 | 18600000000 | 18500000000 | 18100000000 | 17800000000 | 17400000000 | 17300000000
AC154 | 37100000000 | 36700000000 | 33900000000 | 30600000000 | 25700000000 | 23800000000 | 23200000000 | 23400000000 | 23300000000 | 22800000000 | 21500000000 | 20200000000 | 19400000000
AC157 | 20400000000 | 19700000000 | 18900000000 | 18900000000 | 19500000000 | 19500000000 | 19500000000 | 19700000000 | 20200000000 | 20900000000 | 21000000000 | 20200000000 | 17900000000 | 15000000000 | 12900000000 | 11200000000 | 8990000000 | 7500000000 | 5470000000 | 4210000000
AC158 | 29400000000 | 30500000000 | 28700000000 | 25300000000 | 22600000000 | 21200000000 | 20100000000 | 20300000000 | 20700000000 | 20600000000 | 20400000000 | 20300000000 | 19900000000 | 19500000000 | 18800000000 | 18300000000 | 17500000000 | 16500000000
AC151 | 30600000000 | 31300000000 | 31800000000 | 31200000000 | 30600000000 | 28900000000 | 27300000000 | 26300000000 | 25600000000 | 24000000000 | 22100000000 | 19100000000 | 15400000000 | 12000000000 | 9520000000 | 8730000000
AC152 | 26800000000 | 26500000000 | 22400000000 | 20400000000 | 19400000000 | 18700000000 | 17700000000 | 16400000000 | 15500000000 | 14400000000 | 13300000000 | 12300000000 | 11400000000 | 10500000000 | 10200000000 | 10100000000 | 9860000000
<Qo>=2.26E10@16MV/m
7 LG cavities which have been later assembled in the XM-3 cryomodule

## Slide 7
Chart: Eacc [MV/m]
| 1100000 | 1590000 | 2270000 | 2890000 | 3690000 | 4730000 | 6020000 | 7840000 | 10100000 | 11600000 | 13300000 | 15400000 | 17900000 | 19600000 | 21500000 | 23400000 | 25500000 | 28400000 | 30800000 | 33200000 | 35300000 | 37400000
AC154 | 54900000000 | 58600000000 | 60900000000 | 62000000000 | 63700000000 | 64700000000 | 63500000000 | 62800000000 | 57200000000 | 54700000000 | 51800000000 | 48800000000 | 46300000000 | 45700000000 | 45300000000 | 44200000000 | 42000000000 | 39500000000 | 37400000000 | 32300000000 | 28800000000 | 27000000000
AC155 | 27200000000 | 30500000000 | 34400000000 | 38500000000 | 41100000000 | 43500000000 | 45000000000 | 45000000000 | 43300000000 | 39200000000 | 36600000000 | 34600000000 | 32700000000 | 31200000000 | 29100000000 | 27100000000 | 25300000000 | 23700000000 | 22200000000 | 21300000000 | 19200000000 | 17400000000 | 15700000000 | 13900000000 | 14400000000
AC153 | 28700000000 | 32600000000 | 37300000000 | 42000000000 | 45800000000 | 49100000000 | 51300000000 | 52000000000 | 50500000000 | 46500000000 | 43300000000 | 40600000000 | 38500000000 | 37500000000 | 36200000000 | 34800000000 | 33200000000 | 31400000000 | 30200000000 | 28100000000 | 26100000000 | 24500000000 | 24900000000
AC158 | 36700000000 | 38800000000 | 40300000000 | 42500000000 | 44400000000 | 45400000000 | 42900000000 | 40500000000 | 38400000000 | 35500000000 | 34900000000 | 34900000000 | 34400000000 | 33100000000 | 29200000000 | 27100000000 | 24700000000
Performance of LG Cavities; Vertical test at 1.8K
<Qo>= 4.1E10@16MV/m
4 LG cavities, 2 marked black/white have been later assembled in the XM-3
Qo at 1.8K increases by ca. 80% as compared to Qo at 2K

## Slide 8
XM-3 History
7 cavities are made of LG niobium, one (Cav#3, AC146) is made of FG grain niobium.
XM-3 was for first time cw tested in 2013, at Eacc << than those demonstrated in the VT.
XM-3 is the mostly tested CM at DESY
XM-3 at CMTB

## Slide 9
XM-3 History; Nominal mode tests
Tests in 2013 and 2017; operational <Eacc> = 33.3 MV/m
Courtesy D. Kostin

## Slide 10
Recent (2018) XM-3 cw tests at 2K, 1.8K, 1.65K
Chart: Eacc [MV/m]
| 10.42 | 11.5 | 12.72 | 13.1 | 15.5 | 15.74 | 17.399999999999999
XM-3, 2.0K | 25000000000 | 24100000000 | 23100000000 | 22200000000 | 20700000000 | 20000000000 | 19000000000
XM-3, 1.8K | 41600000000 | 39500000000 | 36300000000 | 35600000000 | 34300000000 | 33000000000
T= 1.65K | 58500000000 | 50800000000
Gain in Qo(1.8K)/Qo(2K) | 1.7261 | 1.7793 | 1.7536 | 1.8053
Qo= 3.6E10@16MV/m
For whole CM Qo at 1.8K increases also ca. 80% as compared to Qo at 2K

## Slide 11
Recent (04/2018) cw test of each cavity at 1.8K
Chart: Eacc [MV/m]
| 7.02 | 11.59 | 15.14 | 20.14
C#1 | 45016790513.834 | 38801750069.437 | 36564792543.2128 | 33347382134.3874
C#2 | 52970184347.8261 | 50480519480.5195 | 44180239927.8829 | 40832051742.7237
C#3-FG | 39465345680.4065 | 33294849574.0009 | 28590912181.907 | 22485333473.8691
C#4 | 45875838735.1779 | 43488413801.9442 | 38445003920.3033 | 34067353571.3174
C#5 | 49255356665.4689 | 42828502433.9505 | 37978972898.3541 | 32428634998.2034
C#6 | 48973643501.2855 | 38236514330.8865 | 33121858549.9553 | 27844705138.3399
C#7 | 36920158516.1074 | 31607002561.2648 | 26395952330.5243 | 18494565389.2421
C#8 | 37860895677.6744 | 38977829624.6151 | 35136563839.6386 | 28318529373.2355
<Qo> | 44542276704.7226 | 39714422734.5773 | 35051787023.9723 | 29727319477.6648
<Qo> for 8 cavities is very close to Qo measured for whole XM-3 cryomodule

## Slide 12
Recent test; fast and slow cool-down
Chart: Eacc [MV/m]
| 5.9 | 7.7 | 9.8000000000000007 | 10.9 | 11.4 | 11.6 | 12.8 | 13 | 13 | 13.1 | 13.4 | 14.8 | 15.6 | 15.9 | 16.05 | 16.100000000000001
SCD-2K | 24000000000 | 23000000000 | 21000000000 | 20000000000 | 20000000000 | 0 | 19000000000 | 19000000000 | 18300000000 | 19000000000 | 18000000000 | 17000000000 | 16000000000 | 15400000000 | 0 | 15100000000 | 15400000000 | 15000000000
FCD-2K | 25000000000 | 24100000000 | 23100000000 | 22200000000 | 20700000000 | 20000000000 | 19000000000
SCD-1.8K | 23500000000 | 24500000000
FCD-1.8K | 41600000000 | 39500000000 | 36300000000 | 35600000000 | 34300000000 | 33000000000
33%
FCD increases Qo by 45% at 1.8K and 33% at 2K. B expulsion for FCD takes place.

## Slide 13
CW upgrade scenario for E-XFEL; parameters
33%
T [K] |  | 1.8 | 1.8 | 1.8 | 1.8 | 2.0 | 2.0 |  | 
 |  | L0 | L1 | L2 | Inj. Sect. L0+L1+L2 | Inj. Sect. L0+L1+L2 | L3 | Total cw | Total lp
Eacc | [MV/m] | 16.0 | 11.0 | 15.0 |  |  | 6.8 |  | L3 at 12.5
Energy/Linac | [GeV] | 0.13 | 0.4 | 1.5 | 2 | 2 | 5.4 | 7.4 | 12.0
HL/CM | [W] | 67 | 31 | 58 |  |  | 20 |  | 
HL/Linac | [W] | 67 | 123 | 699 | 889 | 1449 | 1880 |  | 
DF | [%] |  |  |  | 100 | 100 | 100 |  | 24
Capacity of present cryo-plant is ca. 2.4 kW. We will need additional one for the IS. The open question is, at what T shall the second plant operate?

## Slide 14
CW upgrade scenario for E-XFEL;RF vs microphonics
Chart: Optimal Qext for Ibeam= 25µA
| 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26 | 27 | 28 | 29 | 30
16.61 | 64.3639 | 45.7354 | 29.0113 | 20.5344 | 15.7556 | 12.7427 | 10.6831 | 9.1906 | 8.061 | 7.1772 | 6.4671 | 5.8843 | 5.3976 | 4.985 | 4.6308 | 4.3235 | 4.0544 | 3.8168 | 3.6054 | 3.4162 | 3.2459 | 3.0917 | 2.9514 | 2.8234 | 2.7059 | 2.5979 | 2.4981 | 2.4057 | 2.3199 | 2.24 | 2.1654 | 2.0957 | 2.0302 | 1.9688
11.42 | 44.6269 | 36.7905 | 26.2716 | 19.4909 | 15.2692 | 12.4812 | 10.5276 | 9.091 | 7.9936 | 7.1295 | 6.4321 | 5.858 | 5.3772 | 4.9689 | 4.6179 | 4.313 | 4.0458 | 3.8096 | 3.5993 | 3.411 | 3.2414 | 3.0878 | 2.9481 | 2.8204 | 2.7034 | 2.5956 | 2.4961 | 2.4039 | 2.3183 | 2.2386 | 2.1641 | 2.0945 | 2.0291 | 1.9678
15.57 | 60.4474 | 44.2648 | 28.6249 | 20.396 | 15.6928 | 12.7094 | 10.6634 | 9.1781 | 8.0526 | 7.1712 | 6.4627 | 5.8811 | 5.395 | 4.983 | 4.6292 | 4.3222 | 4.0534 | 3.8159 | 3.6047 | 3.4156 | 3.2453 | 3.0912 | 2.951 | 2.823 | 2.7056 | 2.5976 | 2.4979 | 2.4055 | 2.3197 | 2.2398 | 2.1653 | 2.0955 | 2.0301 | 1.9687
7.06 | 27.6135 | 25.4152 | 21.0435 | 17.0458 | 14.0049 | 11.7618 | 10.085 | 8.8014 | 7.7946 | 6.9872 | 6.3271 | 5.7783 | 5.3154 | 4.92 | 4.5786 | 4.2809 | 4.0192 | 3.7874 | 3.5806 | 3.3951 | 3.2277 | 3.076 | 2.9378 | 2.8114 | 2.6954 | 2.5886 | 2.4898 | 2.3983 | 2.3133 | 2.234 | 2.16 | 2.0908 | 2.0258 | 1.9647
12.98 | 50.1163 | 39.689 | 27.2682 | 19.8877 | 15.4577 | 12.5835 | 10.5888 | 9.1303 | 8.0203 | 7.1484 | 6.446 | 5.8684 | 5.3853 | 4.9753 | 4.6231 | 4.3172 | 4.0492 | 3.8125 | 3.6018 | 3.4131 | 3.2432 | 3.0894 | 2.9494 | 2.8216 | 2.7044 | 2.5965 | 2.4969 | 2.4046 | 2.3189 | 2.2391 | 2.1646 | 2.0949 | 2.0296 | 1.9682

## Slide 15
CW upgrade scenario for E-XFEL;RF vs microphonics
Chart: Prf/cavity
| 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26 | 27 | 28 | 29 | 30 | 31 | 32 | 33
16.61 | 0.42346 | 0.5097 | 0.68147 | 0.87538 | 1.0767 | 1.2812 | 1.4874 | 1.6945 | 1.9023 | 2.1105 | 2.319 | 2.5277 | 2.7365 | 2.9455 | 3.1546 | 3.3637 | 3.5729 | 3.7822 | 3.9915 | 4.2008 | 4.4102 | 4.6196 | 4.8291 | 5.0385 | 5.248 | 5.4574 | 5.6669 | 5.8764 | 6.086 | 6.2955 | 6.505 | 6.7146 | 6.9241 | 7.1337
11.42 | 0.28867 | 0.31941 | 0.38951 | 0.47481 | 0.56618 | 0.66041 | 0.75618 | 0.85286 | 0.95014 | 1.0478 | 1.1458 | 1.2439 | 1.3422 | 1.4406 | 1.5392 | 1.6378 | 1.7364 | 1.8351 | 1.9339 | 2.0327 | 2.1315 | 2.2304 | 2.3292 | 2.4281 | 2.527 | 2.6259 | 2.7249 | 2.8238 | 2.9228 | 3.0217 | 3.1207 | 3.2197 | 3.3187 | 3.4177
15.57 | 0.3963 | 0.46874 | 0.61658 | 0.7854 | 0.96139 | 1.1406 | 1.3214 | 1.5032 | 1.6856 | 1.8684 | 2.0515 | 2.2348 | 2.4182 | 2.6018 | 2.7855 | 2.9693 | 3.1531 | 3.337 | 3.5209 | 3.7049 | 3.8889 | 4.0729 | 4.2569 | 4.441 | 4.6251 | 4.8091 | 4.9932 | 5.1774 | 5.3615 | 5.5456 | 5.7298 | 5.9139 | 6.0981 | 6.2823
7.06 | 0.17828 | 0.18599 | 0.20611 | 0.23355 | 0.2649 | 0.29842 | 0.33322 | 0.36881 | 0.40494 | 0.44143 | 0.47819 | 0.51514 | 0.55224 | 0.58945 | 0.62676 | 0.66413 | 0.70157 | 0.73906 | 0.7766 | 0.81416 | 0.85176 | 0.88938 | 0.92702 | 0.96469 | 1.0024 | 1.0401 | 1.0778 | 1.1155 | 1.1532 | 1.191 | 1.2287 | 1.2665 | 1.3042 | 1.342
12.98 | 0.33194 | 0.37554 | 0.471 | 0.5842 | 0.70406 | 0.82697 | 0.95149 | 1.077 | 1.2031 | 1.3295 | 1.4563 | 1.5833 | 1.7105 | 1.8378 | 1.9651 | 2.0926 | 2.2201 | 2.3477 | 2.4753 | 2.603 | 2.7306 | 2.8584 | 2.9861 | 3.1138 | 3.2416 | 3.3694 | 3.4972 | 3.625 | 3.7528 | 3.8807 | 4.0085 | 4.1364 | 4.2642 | 4.3921

## Slide 16: Summary
LG Nb seems to be a reasonable choice for the new 136 cavities in the IS
LG Cavities fulfill Eacc spec ( 28+MV/m)
Qo is high at 2K:
  2.26E10@16MV/m (VT)
  2.0E10@16MV/m (CM) as measured with one FG cavity and one “not very clean” cavity#7
  and is 80% higher at 1.8K than at 2K
For cw/lp and Ibeam of 25µA (100pC and 250kHz) required Prf/cavity @ Qload=4E7 is:
  3.2 kW for L0
  1.6 kW for L1
  3.0 kW for L2
  0.7 kW for L3 (2kW peak in case of lp mode)
Open question: what T is optimal for the IS?
Currently XM-3 is tested by LLRF group for the VS stability at Qload between 2E7 and 6E7

## Slide 17: Acknowledgements
I want to express my gratitude to all Colleagues contributing to and supporting the experiments and R&D programs towards cw/lp operation modes
DESY: V. Ayvazyan, J. Branlard, R. Brinkmann, M. Ebert, J. Eschke, A. Gössel, D. Kostin, F. Mittag, W. Merz, W.-D. Möller, C. Müller, R. Onken, K. Przygoda, D. Reschke, R. Rybaniec, I. Sandvoss, H. Schlarb, A. Sulimov, E. Vogel, H. Weise……
TUL: W. Cichalewski, A. Piotrowski
Thank you for your attention