## Slide 1: Half-Wave Coaxial Test Cavities at ODU Results and Plans Work supported by NSF Grant PHY-1416051
TTC Meeting
RIKEN, 26-29 June 2018

## Slide 2: Introduction
Our goal is not necessarily to achieve the highest fields and lowest surface resistance
It is to get a better understanding of the physics of the mechanisms limiting the performance in the frequency range of interest for accelerators
The research consists of experimental and theoretical parts to address the unresolved issues of the surface resistance of superconductors at high rf field, and in particular how the surface composition and structure can be modified and tuned in order to reduce surface resistance.
One of the most effective ways to understand a physical process is to analyze its frequency dependence
It is very much work in progress

## Slide 3: Research Tool – Half Wave Coaxial Cavity
Cavity designed to provide range of frequency particular interest of accelerators: 325, 650, 975, 1300 MHz.
Field distribution almost identical in all TEM modes
  The same surface will be exposed to the highest fields at all frequencies
TEM modes should be sufficiently separated by other TM and TE modes.
Should be able to achieve high rf surface field.
Should be free of multipacting.

## Slide 4: Research Tool – Half Wave Coaxial Cavity
Lowest power dissipation for a given Hp on center conductor
  Smallest a possible, but big enough to be able to provide sufficient cooling
  b/L=0.25, shallow minimum, tweak to separate TE and TM modes
Mode | f (MHz) | G (Ohm)
TEM1 | 325.4 | 59
TEM2 | 650.8 | 119
TE111 | 869.6 | 
TEM3 | 976.1 | 179
TE112 | 1034.9 | 
TE113 | 1265.4 | 
TEM4 | 1301.3 | 239
TE211 | 1470.1 | 
2b=202 mm
2a=40 mm
L=459 mm

## Slide 5: Surface Fields of TEM Modes
Surface Electric Field
Surface Magnetic Field
325 MHz
650 MHz
325 MHz
650 MHz
975 MHz
1300 MHz
975 MHz
1300 MHz

## Slide 6: Multipacting Levels – Half-Wave Coaxial Cavity
Multipacting levels at the end plate in the cavity
Higher multipacting levels at higher frequency
Multipacting was processed gradually with increasing frequency
325 MHz
650 MHz
975 MHz
1300 MHz

## Slide 7: Fabrication Sequence

## Slide 8: Research Tool – Half Wave Coaxial Cavity
Fabricated cavity with many ports for diagnostics capability
Cavity ready for cold test
Clean room assembly

## Slide 9: Low Field Frequency Dependence
No low-T baking

## Slide 10: Low Field Frequency Dependence

## Slide 11: Field Dependence of Surface Resistance
No low-T baking

## Slide 12: Extracting Real Rs(H) from Q(Hp)
Geometrical factor
Average surface resistance
Define a(h) as the fraction of the total cavity area where
  Continuous, monotonically increasing
  a(0) = 0 a(1) = 1

## Slide 13: Extracting Real Rs(H) from Q(Hp)
Model by
  H0 arbitrary, to make coefficients dimensionless
  ai : suite of non-negative real numbers
Assume
  Continuous, monotonically increasing
  [1-a(h)] is the fraction of the total cavity area where

## Slide 14: Application to Half Wave Coaxial Cavity

## Slide 15: Application to Half Wave Coaxial Cavity
Chart: h
Chart: h

## Slide 16: Application to Half Wave Coaxial Cavity
Chart: a
| 1E-4 | 0.1 | 0.2 | 0.5 | 1 | 1.5 | 2 | 2.5 | 3 | 3.5 | 4 | 4.5 | 5
r = 0.4 | 1 | 1.0455 | 1.091 | 1.226 | 1.4425 | 1.644 | 1.8287 | 1.9971 | 2.151 | 2.2925 | 2.4237 | 2.5464 | 2.662
r = 0.3 | 1 | 1.0497 | 1.099 | 1.2424 | 1.4633 | 1.6592 | 1.832 | 1.9858 | 2.1247 | 2.2519 | 2.37 | 2.481 | 2.5862
r = 0.2 | 1.0001 | 1.0528 | 1.1042 | 1.2492 | 1.4595 | 1.6355 | 1.7863 | 1.9191 | 2.0393 | 2.1503 | 2.2542 | 2.3526 | 2.4465
r = 0.1 | 1.0001 | 1.0517 | 1.1005 | 1.2306 | 1.4042 | 1.5433 | 1.6623 | 1.7689 | 1.8672 | 1.9593 | 2.0465 | 2.1297 | 2.2095
r = 0.05 | 1 | 1.046 | 1.0882 | 1.196 | 1.3354 | 1.4485 | 1.548 | 1.6392 | 1.7245 | 1.8052 | 1.882 | 1.9557 | 2.0265
r = 0 | 1 | 1.0191 | 1.038 | 1.0925 | 1.1781 | 1.2581 | 1.3334 | 1.4047 | 1.4726 | 1.5376 | 1.6 | 1.6601 | 1.7181
Chart: r
| 9.9999999999999994E-12 | 0.01 | 0.02 | 0.03 | 0.04 | 0.05 | 0.06 | 7.0000000000000007E-2 | 0.08 | 0.09 | 0.1 | 0.15 | 0.2 | 0.3 | 0.4 | 0.5 | 0.6 | 0.7 | 0.8 | 0.9 | 1
a = 5 | 1.7181 | 1.8081 | 1.874 | 1.9304 | 1.9808 | 2.0265 | 2.0685 | 2.1074 | 2.1437 | 2.1777 | 2.2095 | 2.3438 | 2.4465 | 2.5862 | 2.662 | 2.6839 | 2.6484 | 2.5419 | 2.3492 | 2.067 | 1.7181
a = 4 | 1.6 | 1.683 | 1.7432 | 1.7948 | 1.8406 | 1.882 | 1.92 | 1.9551 | 1.9877 | 2.0181 | 2.0465 | 2.1653 | 2.2542 | 2.37 | 2.4237 | 2.4242 | 2.3708 | 2.2591 | 2.0873 | 1.8618 | 1.6
a = 3 | 1.4726 | 1.5476 | 1.6016 | 1.6475 | 1.688 | 1.7245 | 1.7578 | 1.7884 | 1.8166 | 1.8428 | 1.8672 | 1.9672 | 2.0393 | 2.1247 | 2.151 | 2.129 | 2.0636 | 1.9587 | 1.8196 | 1.6542 | 1.4726
a = 2 | 1.3333 | 1.3987 | 1.445 | 1.4839 | 1.5178 | 1.548 | 1.5753 | 1.6 | 1.6226 | 1.6433 | 1.6623 | 1.7371 | 1.7863 | 1.832 | 1.8287 | 1.7906 | 1.7269 | 1.6443 | 1.5481 | 1.4432 | 1.3333
a = 1 | 1.1781 | 1.2297 | 1.2641 | 1.2919 | 1.3153 | 1.3354 | 1.3529 | 1.3682 | 1.3817 | 1.3937 | 1.4042 | 1.4412 | 1.4595 | 1.4633 | 1.4425 | 1.4085 | 1.3672 | 1.322 | 1.2748 | 1.2265 | 1.1781
a = 0.5 | 1.0925 | 1.1304 | 1.1533 | 1.1707 | 1.1846 | 1.196 | 1.2055 | 1.2134 | 1.2201 | 1.2258 | 1.2306 | 1.245 | 1.2492 | 1.2424 | 1.226 | 1.2055 | 1.1833 | 1.1605 | 1.1376 | 1.1149 | 1.0925

## Slide 17: Field Dependence of Surface Resistance

## Slide 18: On-going Work and Plans
Influence of low temperature baking on A(w), D/k, Rres , Rs(H)
  No baking, 6 hours, 6+6 hours, 6+6+12 hours, 6+6+12+24 hours
Next:
  same thing with N infusion
  Trapping of magnetic field
  …..
Now building 2 new almost identical HW cavities
  OD slightly bigger for ease of assembly
  Entirely made of Nb to be able to go to high temperature
    Nb3Sn coating
    High temperature heat treatment