## Slide 1: Doping Results as a Function of Different Material for LCLS-II
Dan Gonnella
For the LCLS-II Project

## Slide 2: Outline
Introduction to LCLS-II
Cavity Preparation
Nitrogen-Doping in LCLS-II
Vertical Test Results by Material
Cryomodule Test Results by Material
Conclusions

## Slide 3: Outline
Introduction to LCLS-II
Cavity Preparation
Nitrogen-Doping in LCLS-II
Vertical Test Results by Material
Cryomodule Test Results by Material
Conclusions

## Slide 4: Introduction to LCLS-II
The SRF linac is closely based on the XFEL/ILC/TESLA Design
It consists of 35 cryomodules each with 8 cavities – total of 280 cavities
The 280 1.3 GHz 9-cell cavities have a very ambitious Q specification:
Additionally, cavities must reach 19 MV/m
2.7 x 1010 at 16 MV/m and 2 K
2.5 x 1010 at 16 MV/m and 2 K
Q specification lowered in VT due to addition of stainless steel blank on short side of cavity – adds ~0.8 nΩ of Rres

## Slide 5: Outline
Introduction to LCLS-II
Cavity Preparation
Nitrogen-Doping in LCLS-II
Vertical Test Results by Material
Cryomodule Test Results by Material
Conclusions

## Slide 6: Cavity Preparation
In order to achieve the ambitious Q specification, all 9-cell cavities for LCLS-II are prepared with nitrogen-doping
Original recipe:
  140 μm bulk EP
  800oC degas for 3 hours in vacuum
  2 minutes at 800oC in 20-30 mTorr of N2
  6 minutes at 800oC in vacuum
  5-7 μm light EP

## Slide 7: Cavity Preparation
In order to achieve the ambitious Q specification, all 9-cell cavities for LCLS-II are prepared with nitrogen-doping
Original recipe:
  140 μm bulk EP
  800oC degas for 3 hours in vacuum
  2 minutes at 800oC in 20-30 mTorr of N2
  6 minutes at 800oC in vacuum
  5-7 μm light EP

## Slide 8: Cavity Preparation
In order to achieve the ambitious Q specification, all 9-cell cavities for LCLS-II are prepared with nitrogen-doping
Original recipe:
  140 μm bulk EP
  800oC degas for 3 hours in vacuum
  2 minutes at 800oC in 20-30 mTorr of N2
  6 minutes at 800oC in vacuum
  5-7 μm light EP
Cavities are being produced by Research Instruments GmbH (RI) and Ettore Zanon S.p.a (EZ)
Niobium was procured from Tokyo Denkai and OTIC Ningxia

## Slide 9: Outline
Introduction to LCLS-II
Cavity Preparation
Nitrogen-Doping in LCLS-II
Vertical Test Results by Material
Cryomodule Test Results by Material
Conclusions

## Slide 10: Nitrogen-Doping Introduction

## Slide 11: Nitrogen-Doping Introduction
Q is improved by 2 mechanisms:
  Higher starting Q0
  Anti-Q slope
Both of these are a resulting of a changing RBCS
Q0’s of >3x1010 can consistently be produced

## Slide 12: Drawbacks of N-Doping
Q0 is significantly improved by the lowering of RBCS
There is a tradeoff however with Rres
Nitrogen-doped cavities are more sensitive to losses from trapped magnetic flux
For the same amount of trapped flux, a N-doped cavity will have a higher Rres than an un-doped cavity
  3.4x for the LCLS-II cavity recipe
This requires efficient flux expulsion or small ambient magnetic fields to maintain high Q0

## Slide 13: RBCS in Production Cavities
Strong Anti-Q Slope
Decreasing RBCS from ~7 to ~4 nΩ
Production cavities show similar anti-Q slope to R&D cavities

## Slide 14: RBCS in Production Cavities
RBCS at 16 MV/m and 2.0 K is consistently 4-6 nΩ
This is consistent with “2/6” N-Doping developed in the R&D phase of LCLS-II
Mix of Material from 3 Vendors
RBCS consistently between 4 and 6 nΩ at 16 MV/m

## Slide 15: Q vs E for First Article Cavities
Some Great Cavities
Some Good Cavities
All these cavities tested in very low (0-1 mG) magnetic fields

## Slide 16: Niobium Material Overview
266 cavities originally ordered
  3011 TD sheets

## Slide 17: Niobium Material Overview
266 cavities originally ordered
  3011 TD sheets
  2710 NX sheets
    337 of those sheets were “Lot C” (ASTM>7)

## Slide 18: Niobium Material Overview
266 cavities originally ordered
  3011 TD sheets
  2710 NX sheets
    337 of those sheets were “Lot C” (ASTM>7)
Additional cavities ordered, bringing total to 375
  692 additional TD sheets purchased to complete the order
Define: Lot A: ASTM<6
Lot B: 6<ASTM<7
Lot C: ASTM>7

## Slide 19: Flux Expulsion in Original Material
TD
NX
TD material shows poor flux expulsion after 3 hours at 800oC
NX material shows poor flux expulsion after 3 hours at 800oC
Data from A. Palczewski
Data from S. Posen

## Slide 20: Flux Expulsion in Original Material
TD
NX
TD material shows poor flux expulsion after 3 hours at 800oC
Improved to near perfect when temperature raised to 900oC
NX material shows poor flux expulsion after 3 hours at 800oC
900oC did not significantly improve flux expulsion
Data from S. Posen
Data from A. Palczewski

## Slide 21: Flux Expulsion in Original Material
TD
NX
TD material shows poor flux expulsion after 3 hours at 800oC
Improved to near perfect when temperature raised to 900oC
NX material shows poor flux expulsion after 3 hours at 800oC
900oC did not significantly improve flux expulsion
950 and 975oC necessary
Data from A. Palczewski
Data from S. Posen
Lesson Learned:
Flux expulsion must be verified on lot of material to ensure Q0 meets specification

## Slide 22: Cavity Preparation
In order to achieve the ambitious Q specification, all 9-cell cavities for LCLS-II are prepared with nitrogen-doping
Updated recipe:
  200 μm bulk EP
  900oC degas for 3 hours in vacuum for TD cavities
  950/975oC degas for 3 hours in vacuum for NX cavities
  2 minutes at 800oC in 20-30 mTorr of N2
  6 minutes at 800oC in vacuum
  5-7 μm light EP

## Slide 23: Q vs E for First Article Cavities

## Slide 24: Q vs E for First Article Cavities
Nitrogen-Doping has been successfully transferred to cavity vendors

## Slide 25: Outline
Introduction to LCLS-II
Cavity Preparation
Nitrogen-Doping in LCLS-II
Vertical Test Results by Material
Cryomodule Test Results by Material
Conclusions

## Slide 26: LCLS-II Vertical Test Requirements
Cavity Requirements for 9-Cell Qualification:
Q ≥ 2.5x1010 at 16 MV/m and 2.0 K
Emax ≥ 19 MV/m
No detectable field emission on final power rise

## Slide 27: Quench Fields by Material in VT
Nearly all cavities exceed the LCLS-II gradient specification
Average quench fields are ~23 MV/m, consistent with expectations from 2/6 Nitrogen-doping recipe
No significant difference in quench fields between material batches

## Slide 28: Q0 by Material in VT
Large spread in Q0 in vertical test due to differences in heat treatments and material
Material | <Q0> at 16 MV/m, 2K
TD/800* | 2.5x1010
TD/900 | 3.3x1010
NX/900* | 2.6x1010
NX/950/975 | 3.3x1010
*TD/800 tested in lower magnetic fields than NX/900

## Slide 29: Outline
Introduction to LCLS-II
Cavity Preparation
Nitrogen-Doping in LCLS-II
Vertical Test Results by Material
Cryomodule Test Results by Material
Conclusions

## Slide 30: Cavity Performance in CM by Material
Q0 for Cavities in CMs Tested at FNAL
Prototype cavities typically showed Q0 above spec

## Slide 31: Cavity Performance in CM by Material
Q0 for Cavities in CMs Tested at FNAL
Prototype cavities typically showed Q0 above spec
TD/800 cavities are consistently below spec
TD/800 = Cavities produced with Tokyo Denkai material, heat treated at 800oC

## Slide 32: Cavity Performance in CM by Material
Q0 for Cavities in CMs Tested at FNAL
Prototype cavities typically showed Q0 above spec
TD/800 cavities are consistently below spec
TD/900 cavities consistently far exceed the spec
TD/900 = Cavities produced with Tokyo Denkai material, heat treated at 900oC

## Slide 33: Cavity Performance in CM by Material
Q0 for Cavities in CMs Tested at FNAL
Prototype cavities typically showed Q0 above spec
TD/800 cavities are consistently below spec
TD/900 cavities consistently far exceed the spec
NX/900 cavities perform similarly to the TD/800 cavities and do not meet spec
NX/800 = Cavities produced with Ningxia material, heat treated at 900oC

## Slide 34: Cavity Performance in CM by Material
Q0 for Cavities in CMs Tested at FNAL
Prototype cavities typically showed Q0 above spec
TD/800 cavities are consistently below spec
TD/900 cavities consistently far exceed the spec
NX/900 cavities perform similarly to the TD/800 cavities and do not meet spec
NX/950 cavities perform similarly to TD/900 (limited statistics)
NX/950 = Cavities produced with Ningxia material, heat treated at 950oC

## Slide 35: Changes from Vertical to Cryomodule Test
Limited Statistics
Changes in performance from VT to CM by material are significant depending on the flux expelling properties
Assumes 16 MV/m operation

## Slide 36: Anti-Q Slope in CM
2 K
Good agreement between Q in VT and CM test at all fields
Anti-Q slope clearly present even in the cryomodules
Nitrogen-doping has been successfully demonstrated in cryomodules production
NX/950

## Slide 37: Outline
Introduction to LCLS-II
Cavity Preparation
Nitrogen-Doping in LCLS-II
Vertical Test Results by Material
Cryomodule Test Results by Material
Conclusions

## Slide 38: Conclusions
LCLS-II production has been challenged by performance differences due to differently expelling flux material
The nitrogen-doping has worked as planned – Q0 performance is significantly higher in cavities with good flux expulsion (TD/900, NX/950)
Nitrogen-doping has been successfully industrialized
    Equivalent performance in doped cavities can be achieved, but with different heat treatments to account for differences in flux expulsion in the bulk niobium
There has been NO demonstrated difference in quench fields in cavities produced with different material
Until a new material specification is defined governing flux expulsion, flux expulsion must be verified for all niobium to be used in new cavities