## Slide 1
Sam Posen, Fermilab SRF Team, LCLS-II Team
TTC Workshop Riken
26 June 2018
RIKEN Nishina Center, Saitama, Japan
Motivation/Background for Flux Expulsion: Performance in LCLS-II CMs at Fermilab
Notes: This is a talk about magnetic flux expulsion. In the last few years we have discovered how to manipulate this property of cavities in a practical way to minimize Q-degradation for machines where high Q0 is important.

## Slide 2: Why Flux Expulsion is Important
LCLS-II CAV0007 – fabricated and prepared by RI, TD material
LCLS-II CAV0019 – fabricated and prepared by RI, TD material
Notes: Now what do I mean by flux expulsion? I mean that for practical magnetic shielding, we expect a background field of 5-10 mG, and when we cool down a cavity through Tc, two sort of extremes are possible

## Slide 3: Why Flux Expulsion is Important
LCLS-II CAV0007 – fabricated and prepared by vendor B, TD material
LCLS-II CAV0019 – fabricated and prepared by vendor B, TD material
Notes: In one extreme, ambient flux is fully trapped in the material, leading to increased residual resistance, and in the other, it is fully expelled, leading to much closer to the intrinsic cavity Q0. What we’ve found is that we can take the same vendor and the same material and by adjusting the treatment parameters come up with very different levels of flux expulsion. So why is this important?

## Slide 4: LCLS-II - Preproduction
BSC/BNC
Full expulsion
Data measured by Jefferson Lab
As-received niobium material for LCLS-II production: very poor expulsion
Cooling in 5 mG applied field
(spec for background field in module)
1.3 GHz 1-cell cavities
Data measured by Fermilab

## Slide 5: LCLS-II - Preproduction
As-received niobium material for LCLS-II production: very poor expulsion
1.3 GHz 1-cell cavities
BSC/BNC
Full expulsion
Data measured by Jefferson Lab
Cooling in 5 mG applied field
(spec for background field in module)
LCLS-II CD2/3 Review Closeout, Dec 2015

## Slide 6: LCLS-II - Preproduction
BSC/BNC
Full expulsion
Data measured by Jefferson Lab
After 900°C treatment: much improved
Cooling in 5 mG applied field
(spec for background field in module)
As-received niobium material for LCLS-II production: very poor expulsion
1.3 GHz 1-cell cavities
Data measured by Fermilab
Data measured by Fermilab
Data measured by Fermilab

## Slide 7: LCLS-II - Preproduction
As-received niobium material for LCLS-II production: very poor expulsion
1.3 GHz 1-cell cavities
BSC/BNC
Full expulsion
Data measured by Jefferson Lab
After 900°C treatment: much improved
Cooling in 5 mG applied field
(spec for background field in module)
“Lot C” material – lower RRR, smaller grains
Data measured by Fermilab

## Slide 8: LCLS-II - Production
See below difference between flux trapping in baseline 800 C recipe compared to 900 C modification for TD material
These are production 9-cell cavities that are now in cryomodules for LCLS-II
Before recipe modification
After recipe modification
Data measured by Fermilab
Notes: Meanwhile the very first batch of LCLS-II production cavities had been fabricated and tested.

## Slide 9: LCLS-II Production Data
See vertical test data in next talk by D. Gonnella which shows strong Q0 dependence on material
I will show Cryomodule data from Fermilab
“Slow” cooldown
Mass flow ~a few g/s
“Fast” cooldown
Mass flow ~60-80 g/s
High mass flow during cooldown generates top-bottom ΔT at transition to expel flux

## Slide 10: Cavities in Fermilab LCLS-II Cryomodules
During cooldown through Tc
At 16 MV/m (or max usable gradient)
⨉ 1010
All cavities of a given material in CM averaged. Spread goes into y-errorbars.

## Slide 11: Cavities in Fermilab LCLS-II Cryomodules
⨉ 1010
During cooldown through Tc
At 16 MV/m (or max usable gradient)
⨉ 1010
All cavities of a given material in CM averaged. Spread goes into y-errorbars.

## Slide 12: Cavities in Fermilab LCLS-II Cryomodules
⨉ 1010

## Slide 13: Cavities in Fermilab LCLS-II Cryomodules
⨉ 1010

## Slide 14: Cavities in Fermilab LCLS-II Cryomodules
⨉ 1010

## Slide 15: Cavities in Fermilab LCLS-II Cryomodules
⨉ 1010

## Slide 16: Cavities in Fermilab LCLS-II Cryomodules
⨉ 1010

## Slide 17: Cavities in Fermilab LCLS-II Cryomodules
⨉ 1010

## Slide 18: Crucial Questions
What makes different niobium production runs have such different flux expulsion behavior?
  Variation between TD and NX
  Variation within a given vendor (e.g. NX-A/B and NX-C)
Can we avoid producing NX-C type material which would have required extremely high heat treatment temperatures to improve?
Can we modify specifications to give predictable flux expulsion behavior for a given heat treatment?
How to do so without compromising mechanical properties?
How to perform QA/QC of flux expulsion in feasible manner?

## Slide 19: Non-Doped Cavities
Sensitivity even for standard treatment cavities increases at high gradients, comparable to mid-field of doped cavities – still a significant factor for high gradient machines
- 120 C baked cavity slowly cooled in different external fields to extract sensitivity
- Strong field dependence observed:
5 MV/m ~ 0.4 n/mG
31.5 MV/m ~ 1.15 n/mG
35 MV/m ~ 1.4 n/mG
ILC
gradient
M. Checchin et al, FNAL, to be published