## Slide 1: Infusion R&D at DESY
TTC Meeting at RIKEN – 27.6.2018
M. Wenskat – on behalf of SRF Team

## Slide 2: Overview: Runs so far at DESY

## Slide 3: New Run – 1DE10 with Nitrogen @ 120°C
Temperature
Pressure
pmax = 5.5x10-6 mbar

## Slide 4: Partial Pressures during Run
RGA – 800°C beginning, ptot=5.5x10-6 mbar
H
O
N2
CO
CO2
H20
O2
Ne

## Slide 5: Partial Pressures during Run
N2
CO
O
RGA – 800°C after 3h, ptot=8.7x10-7 mbar
O2
H20
H
CO2

## Slide 6: Partial Pressures during Run
RGA – 120°C before infusion, ptot=2.7x10-7 mbar
O2
H20
H

## Slide 7: Partial Pressures during Run
RGA – 120°C after infusion, ptot=5.8x10-7 mbar
O2
H20
H
N2
In conclusion: as clean as we get (which is pretty clean)

## Slide 8: RF Test – 1DE10
@2K
no FE

## Slide 9: Samples 1DE10
Star-like precipitates and new black structures observable.
Both show a grain orientation dependency
No difference in BCP/EP or between Nb suppliers
Samples (2x3x FG):
-EP / BCP
-Tokyo Denkai / Ningxia / Heraeus
Treatment:
Chemistry (110 μm)
800°C@3h
Chemistry (40 μm)
120°C@48h
SEM before / after baking with cavity
Analysis ongoing
Preliminary results (only SEM/EDX):

## Slide 10: Origin of Deterioration I
@ 2K
Sample: 1DE16 – 1st Infusion Run
1DE16 – RF Tests at 2K

## Slide 11: 1DE16 – f vs. T aka Δλ vs. T
λ0 = 74 nm
Mean free path: 14 nm → RRR: 51
=

## Slide 12: 1DE16 – f vs. T aka Δλ vs. T
Interpretation
Sketch of dependencies on mean free path
f vs. T in the range 3.5 - 10 K
Q vs. T in the range 1.5 - 4.2 K
→ 100 nm penetration depth
→ 40 nm penetration depth
[Kugeler - A Combined Temperature and Magnetic Field Mapping System for SRF Cavities – MT Meeting 2018]
1DE16

## Slide 13: Origin of Deterioration II
Use data from
  2nd Sound & T-Map & Optical inspection before 1st infusion run
  2nd Sound after 1st infusion run
  T-Map & H-Map after 2nd infusion run
And cut samples from cavity (hot- & cold- spots)
@ 2K
T-Map & H-Map @ HZB
1DE16 – RF Tests at 2K

## Slide 14: 1DE16 – TMap @ HZB
First glance at measurements
Global increase of heating observed
No features observed in TMap data for previous quench spots

## Slide 15: Summary
Intensive effort to improve furnace cleanliness & pressure
  ‘Saturation’ achieved – further improvements need hardware change
Latest infusion run
  Performance different to previous runs
  ‘Old’ and new precipitates
  Cavity/Samples analysis ongoing
Infusion run has been repeated with second cavity – rf test pending
  Do we really control the process and the resulting cavity performance?
Detailed analysis of cavity performances evolution and their causes
  Combine f vs. T & Q vs. T for better characterization of surface evolution
  TMap shows global heating – HMap still analyzed (HZB)
  Cavity cut outs for detailed surface analysis and correlation to rf performance

## Slide 16: Thanks for Listening
Thanks to the complete DESY and Nanolab SRF team, I gave this talk on their behalf
Special thanks to Christopher Bate, Julia Köszegi, Oliver Kugeler and Jörn Schaffran for providing material
Only collaboration with many partners allows for complex R&D work

## Slide 17: Back Up

## Slide 18: Penetration depth

## Slide 19: 1DE16 – Frequency vs. Temperature
Determine mean free path