## Slide 1: Update on infusion studies at Cornell
P. N. Koufalis
Cornell University

## Slide 2
PART I
Low temperature N-infusion at Cornell so far:
  48 hr @ 160 oC in N2 gas
  Various post-infusion vacuum anneal times
PART II
Low temperature C/O-infusion at Cornell so far:
  48 hr @ 160 oC in Ar+CO2 gas
  Various amounts of post-treatment etching
PART III
High frequency results with N-doping
  Field dependence of surface resistance at 1.3 and 2.6 GHz
  Clean niobium and N-doped
Outline

## Slide 3
PART I:
N-Infusion

## Slide 4
Low temperature baking (120 – 160 oC) in a low pressure N2 atmosphere results in ‘Q-rise’:
N-infusion
A. Grassellino and S. Aderhold, New Low T Nitrogen Treatments Cavity Results with Record Gradients and Q, TTC Saclay, 2016.
P. N. Koufalis, M. Liepe, J. T. Maniscalco. Low Temperature Doping of Niobium Cavities: What is really going on?, TUXBA01, SRF2017.

## Slide 5
RF layer (~)
Oxide layer (~5 nm)
Very high concentrations of impurities near the surface
  surface roughness passivation by dirty surface layer that is superconducting by proximity effect?
  quasiparticle overheating reduced in RF layer?
  pinning sites for magnetic flux lines?
C and O concentrations TWO ORDERS OF MAGNITUDE HIGHER than N in RF layer
SIMS Analysis
EP + 800 °C (5 hr; UHV) + 160 °C (48 hr; N2) + 160 °C (168 hr; UHV)
(0.09 – 0.36 at. % N) for N-doped cavities

## Slide 6
PART II:
C/O-Infusion

## Slide 7
C/O Infusion Results
EP + 800 °C (5 hr; UHV) + 160 °C (48 hr; Ar+CO2)
Very high concentrations of impurities near the surface
  surface roughness passivation by dirty surface layer that is superconducting by proximity effect?
  quasiparticle overheating reduced in RF layer?
  pinning sites for magnetic flux lines?
C and O concentrations TWO ORDERS OF MAGNITUDE HIGHER than N in RF layer

## Slide 8
C/O Infusion Results
HF Rinse: ‘Q-rise’
HF Rinse + OP: ‘Q-drop’
The ‘Q-rise’ disappeared after oxypolishing. Why?
To better understand what is happening, we must look at the field dependence of the surface resistance
EP + 800 °C (5 hr; UHV) + 160 °C (48 hr; Ar+CO2)

## Slide 9
C/O Infusion Results
Strong reduction of with in both cases; strong increase of with in both cases
dominates behavior of cavity with HF + OP; In HF case, is lower in magnitude and decreases from its low field value up until
Presence of impurities lowers mean free path  increases electron-phonon coupling  lowers quasiparticle overheating  strong reduction in

## Slide 10
C/O Infusion Results
160 oC ArCO2 + HF
160 oC N2 (1-cell)
160 oC N2 (9-cell)

## Slide 11
PART III:
High Frequency Results

## Slide 12
High Frequency Results
M. Martinello et al, “Advancement in the understanding of the field and frequency dependent microwave surface resistance of niobium,” in Proceedings of SRF2017, Lanzhou, China, 2017.
Baseline 2.6 GHz shows ‘Q-rise’ and after a 2/6 N-dope the Q increases and the ‘Q-rise’ gets even stronger
Breakdown surface resistance into BCS and residual components:

## Slide 13
Baseline 2.6 GHz data showed a 30% reduction of and after 2/6 N-doping dropped by a little more than 50%
At 2.6 GHz you see ‘Q-rise’ even without doping; however, doping further enhances the ‘Q-rise’
High Frequency Results

## Slide 14
THANK YOU FOR LISTENING