## Slide 1
Martina Martinello
TTC Meeting 2018
Latest insight from high-frequency cavity experiments

## Slide 2: Analyzed Cavities
N-doping
EP/BCP
120C baking
1.3 GHz, 2 K
 | 650 MHz | 1.3 GHz | 2.6 GHz | 3.9 GHz
EP |  |  |  | 
BCP |  |  |  | 
120 C baking |  |  |  | 
2/6 N-doping |  |  |  | 

## Slide 3: Field Dependence at Different Frequencies
Different thermal treatments were studied at different frequencies:
BCP and EP
120 oC baking
Nitrogen doping (2/6 recipe)

## Slide 4: Anti Q-slope in BCP’d 3.9 GHz Cavities
anti Q-slope
T=2.0 K
M. Martinello et al. SRF 2017 (TUYAA02), IPAC 2018 (WEPML013)

## Slide 5: Anti Q-slope in BCP’d 3.9 GHz Cavities
anti Q-slope
Anti-Q-slope visible in clean Nb cavities, at 1.3 GHz
T=2.0 K

## Slide 6: Anti Q-slope in EP’ed 2.6 GHz Cavities
anti Q-slope
Anti-Q-slope visible in clean Nb cavities, at 1.3 GHz
T=2.0 K
M. Martinello et al., IPAC 2018 (WEPML013)

## Slide 7: Anti Q-slope in EP’ed 2.6 GHz Cavities
As for N-doping, anti-Q-slope of these cavities is due to decreasing of the temperature-dependent surface resistance

## Slide 8: First 9 GHz EP Cavity
A. Romanenko et al., IPAC 2018

## Slide 9: Field Dependence at Different Frequencies
Different thermal treatments were studied at different frequencies:
BCP and EP
120 oC baking
Nitrogen doping (2/6 recipe)

## Slide 10: 1. Normalized for 120 C Baking
M. Martinello et al. SRF 2017 (TUYAA02), IPAC 2018 (WEPML013)

## Slide 11: Q0 of 2.6 GHz at high field tends to the one at 1.3 GHz
120C baked cavities
Q-factor of 2.6 GHz cavity converge to the one at 1.3 GHz at high gradients
T=2.0 K
M. Martinello et al. SRF 2017 (TUYAA02), IPAC 2018 (WEPML013)

## Slide 12: Field Dependence at Different Frequencies
Different thermal treatments were studied at different frequencies:
BCP and EP
120 oC baking
Nitrogen doping (2/6 recipe)

## Slide 13: 3. Normalized for N-doping
N-doping effect (decreasing of RT(Eacc)) more pronounced in cavities with f>1.3 GHz and absent in 650 MHz cavities
M. Martinello et al. SRF 2017 (TUYAA02), IPAC 2018 (WEPML013)

## Slide 14: Unprecedented Medium Field Q0 at 3.9 GHz
Q-factor of N-doped 3.9 GHz comparable to 120 C baked 1.3 GHz cavity at
T=2 K
M. Martinello et al. SRF 2017 (TUYAA02),
IPAC 2018 (WEPML013)

## Slide 15: Further Improvement in Q0 at 3.9 GHz w 900C baking
T=2.0 K

## Slide 16: Further Improvement in Q0 at 3.9 GHz w 900C baking
T=2.0 K
Cavity needs to be re-measured because of wrong antennas mounted for this test

## Slide 17: Recent results from Cornell agrees with this trend
J. Maniscalco et Al., IPAC 2018
P. Koufalis et Al., IPAC 2018
M. Martinello et al. SRF 2017 (TUYAA02), IPAC 2018 (WEPML013)

## Slide 18: Summary on the frequency dependence of RBCS(Eacc)
The physical mechanism underneath the RT reversal has a stronger effect at high frequencies
The RT reversal, that has been considered the signature of the N-doped treatment, is actually visible also in clean Nb but at high frequency
On the other hand, N-doped cavities at low frequencies do not show the RT reversal observed at 1.3 GHz
EP/BCP
N-doping
120C baking
M. Martinello et al. SRF 2017 (TUYAA02), IPAC 2018 (WEPML013)

## Slide 19: Non-equilibrium superconductivity
Non equilibrium SC: QPs occupy high energy states above the energy gap
Competition between speed of the RF field and the relaxation and recombination times of QPs → condition for non-equilibrium effects:
The higher the frequency, the higher the probability to met condition for non-equilibrium
N-doping may modify and allowing to see non equilibrium effects at lower frequencies
Romanenko, LINAC 2014; M. Martinello et al. SRF 2017 (TUYAA02), IPAC 2018 (WEPML013)

## Slide 20: Sensitivity for different frequencies
120C baking
BCP/EP
Trapped flux sensitivity increases with frequency
The increment strongly depends on the surface treatment, i.e. on the mean free path
Higher frequencies seem to have a larger field dependence
N-doping
M. Checchin, M. Martinello et al., Appl. Phys. Lett. 112, 072601 (2018)
M. Checchin et al., Supercond. Sci. Technol. 30, 034003 (2017)

## Slide 21: The advantage of N-doping at 3.9 GHz
N-doping wins over standard treatments as long as the field trapped is <17 mG
M. Martinello et al. SRF 2017 (TUYAA02), TTC Meeting Milan 2018

## Slide 22: Conclusions
RT(Eacc) shows a strong frequency dependence: high frequencies are favorable to lower RT at high field
The decreasing of RT(Eacc) can appear also in high-frequencies non-doped cavities and, vice versa, RT(Eacc) increases in low frequencies N-doped cavities
High-Q in high-frequency cavity is possible, especially at medium field → new possibility for CW machine
Non-equilibrium SC may qualitatively explain the decreasing of the surface resistance as a function of the field and its enhancement at higher frequencies
Trapped flux sensitivity increases with frequency but depending on the treatment magnetic shielding may be more or less stringent

## Slide 23
Thank you for your attention!