## Slide 1
  Nitrogen Doping Study at Peking University
Jiankui Hao
On behalf of SRF Laboratory
Institute of Heavy Ion Physics
Peking University
TTC2018, RIKEN, June 26-29, 2018

## Slide 2
TTC2018, RIKEN, June 26-29, 2018
Outline
Motivation and background
N-doping researches of 1-cell cavities
  Sample analyses
  D-doping process
  Vertical test
Summary

## Slide 3
Motivation and background
N-doping Researches
  Driven by the needs of CW XFEL plans
    e. g. Shanghai XFEL, 8 GeV, 600  1.3 GHz 9-cell cavities, 16 MV/m, 2-31010
  Carried out with single cell cavities
  Large grain cavities adopted based on the previous researches
6 large grain 9-cell cavities were fabricated by PKU/OSTEC
BCP 180m + 800C 3h + BCP 30m
no EP
Eacc of all 6 cavities larger than 25 MV/m
Q0~1.6-2.4E10 @ 16 MV/m @ 2.0 K
LG 9-cell cavities for XFEL
high Q at vertical test

## Slide 4
N-doping procedure
N-doping researches with single cell cavities
BCP
HPR
800C annealing 3 hrs
Nitrogen doping
EP
Ethanol rinsing
Ultra sonic cleaning
HPR
Vertical Test
Simple EP
HPR
VTS
Furnace

## Slide 5
Light doping with large grain cavity LG2
N-doping researches with single cell cavities
BCP 250 m + HPR
800C 3 h
N-doping at 2.7-4.0 Pa for 2 min
Annealing 6 min
EP 6 m, ethanol rinsing and HPR
Vertical test
  Eacc: 23.4 MV/m
  2.31010 @ 20 MV/m, 2K
  3.11010 @ 20 MV/m, 1.8K
Large grain cavity LG3
BCP 250m + 800C 3 h + EP 6m
baseline
More work will be carried out

## Slide 6
N-doping researches with single cell cavities
BCP 250 m + HPR
800C annealing 3 h
N-doping at 2.7-4.0 Pa (20-30 mTorr), 20 min
Annealing at 800C, 30 min
Cooldown to 55C in vacuum
EP 15 m
Ethanol rinsing and HPR
Heavy doping with cavity LG1
Temperature and Pressure
Pressure in doping

## Slide 7
Nitrogen content of N-doped samples
（TOF-SIMS）
EP 15 m is enough to remove the bad NbN phase
top1m
different depth
N-doping researches with single cell cavities
Samples
Nb samples are N-doped together with cavity
(Heavy doping, N20A30)
N contents measure by TOF-SIMS
  4 N-doped samples: EP 0, 7, 15, 25 m
  1 non-doped sample

## Slide 8
1st vertical test of N-doped cavity LG1
EP 15 m
Ethanol rinsing and HPR
Vertical test
  3.41010 @ 11 MV/m, 2K
  5.61010 @ 11 MV/m, 1.8K
  Q-drop after 11 MV/m
  Minor field emission
  Q vs E at 2.15 K measured
  anti-Q-slope observed
N-doping researches with single cell cavities

## Slide 9
2nd test of LG1
Added HPR + Reassembly
4.01010 @ 12.3 MV/m, 2K
6.91010 @ 12.4 MV/m, 1.8K
Q vs E at 1.6K measured, Q0~8.81010
obvious anti-Q-slope
low Eacc:
  Simple EP device
  EP parameters need to be optimized
N-doping researches with single cell cavities
SRIMP Code

## Slide 10
3rd test of LG1
+ EP 8 m (total 23 m after doping)
Ethanol rinsing and HPR
Q-drop after 12 MV/m ( 3.11010 @ 12.3 MV/m, 2K)
Eacc -> 13.8 MV/m
N-doping researches with single cell cavities

## Slide 11
N-doping researches have been carried out with single cell large grain cavities.
With only BCP before N-doping, Q0 of 4.01010 @ 12.3 MV/m @ 2K is obtained for heavy doping N20/A30.
Effect of light doping is not obvious. Improvement of Q is obvious for heavy doping, but Eacc is influenced.
More researches on N-doping and EP will be carried out.
Summary
Thank you for your attention！