## Slide 1
Sam Posen, FNAL Nb3Sn SRF Team
TTC Workshop Riken
27 June 2018
RIKEN Nishina Center, Saitama, Japan
Nb3Sn Results from FNAL

## Slide 2: Nb3Sn SRF Experimental Program at Fermilab
Goals: 1) further improvement to Q0 and Eacc 2) scale up to production-style cavities
Large Nb3Sn SRF coating apparatus commissioned
First samples coated Jan 30, 2017
New door and heat shields
New Nb chamber, 20”diam, 82” long
Existing vacuum furnace
1.3 GHz 1-cell (current state of Nb3Sn R&D)
650 MHz 5-cell (future)

## Slide 3: Coating Mechanism: Vapor Diffusion
3
Sn vapor arrives at surface
Sn diffusion
Ts = Sn source temperature
=~1200 C
By independently controlling Sn vapor abundance, it can balanced with Sn diffusion rate to achieve desired stoichiometry
Sn
Nb
Nb3Sn
UHV furnace
Nb cavity substrate
Tf = furnace temperature
=~1100 C
Sn Vapor
Heater
Technique development: Saur and Wurm, Die Naturwissenchaften 1962, Hillenbrand et al. IEEE Transactions on Magnetics 1977, Peiniger et al, SRF’88.

## Slide 4
Cavity Coatings

## Slide 5: Recipe Development
Appearance appears to correlate with performance
Several parameters found to be important:
0.4 g tin evaporated
Apparent thin or uncoated areas
1.5 g tin evaporated
Apparent Residual tin
  Crucible diameter
  Heater power
  Coating time
  Annealing time

## Slide 6: Recipe Development
For residual tin:
  Tc ~ 3.7 K
  Hc ~ 0.03 T
0.4 g tin evaporated
Apparent thin or uncoated areas
1.5 g tin evaporated
Apparent Residual tin

## Slide 7
0.7 g tin evaporated

## Slide 8: Recipe Development
To date, best appearance and performance at Fermilab achieved with:
  Smallest diameter crucible tested
  Heater at maximum power (crucible ~1200 C)
  Large grain cavity anodized prior to coating (as advocated by Siemens in the 1970s and recently revived by Cornell)

## Slide 9
D3 non-anodized
D6 anodized to 30 V
D2 non-anodized
Microscopy by J. Lee
Anodization helps! But “patchy” regions can persist
D1 anodized to 30 V

## Slide 10: Cooldown

## Slide 11: Q vs E
Substantial improvement in our second year of coating
Still some Q-slope, not yet flat Q0 like Cornell
Very high Q0 at 2.0 K, similar to Wuppertal

## Slide 12: T-map at Highest Field Before Quench

## Slide 13: T-map After Quench

## Slide 14
Both hot spots and cold spots show beyond Ohmic heating above ~15 MV/m

## Slide 18
Development of Understanding

## Slide 19
13% lattice mismatch between Nb3Sn film and Nb bulk for thin regions
Epitaxial relationship observed between Nb3Sn film and Nb bulk – appears to be key clue to understand formation of thin, lossy regions – arXiv preprint to be posted soon
Jae-Yel Lee, Northwestern University & Fermilab – presented at TTC 2018

## Slide 20
Outlook

## Slide 21: Outlook
Recipe development at Fermilab has led to nice performance on single cell cavity
  Quench field 18 MV/m
  Q0 at 4.4 K >1e10 at 10 MV/m, Q0 at 2.0 K >5e10 at 10 MV/m
  Some Q-slope above 10 MV/m
Next steps:
  Reproducibility on single cells
  Push to remove Q-slope and increase maximum gradient
  Move into other frequencies and into multicells
650 MHz 1-cell Nb flange welding