## Slide 1: WG3 Summary ’High Q and high gradient performance’
Alex Romanenko (FNAL)
Kensei Umemori (KEK)
Marc Wenskat (DESY)

## Slide 2: Some Numbers…
4 Sessions
  2 Cavity related / 1 Sample related / 1 Theory related
18 Contributions
Chart: 
 | 11 | 5 | 2
North America
Asia
Europe

## Slide 3: …and some kind of „Magic“

## Slide 4: Status Update KEK on Infusion
Intensive Effort
Failed & successfull runs @ JParc Furnace
New furnace at KEK

## Slide 5: Update on N-infusion at JLab
Successful infusion runs at multiple temperatures
Need to inject at higher T to succeed
Upgrade of furnace diagnostics &

## Slide 6: Infusion R&D at DESY
No successfull infusion yet – extensive R&D on necessary furnace conditions
Collaboration with several labs

## Slide 7: Update on high Q/high G R&D @ FNAL
Air leak in injection valve fixed
Showed that infusion works on BCP cavities as well
„Magic low T bake“
  Luck favors the prepared

## Slide 8: Update on infusion studies at Cornell
Successful Infusion run with N
Showed that Anti-Q-Slope possible with ArCO2 infusion
Extend the R&D towards different frequencies

## Slide 9: Latest insight from high-frequency cavity experiments
s
 | 650 MHz | 1.3 GHz | 2.6 GHz | 3.9 GHz
EP |  |  |  | 
BCP |  |  |  | 
120 C baking |  |  |  | 
2/6 N-doping |  |  |  | 
The higher the frequency, the higher the probability to met condition for non-equilibrium
N-doping may modify and allowing to see non equilibrium effects at lower frequencies

## Slide 10: Nitrogen Doping Study at Peking University
Furnace
Heavy / light N-doping R&D on large grain cavities.
Successful run on LG1
Might be problems with EP

## Slide 11: N-doping study at KEK
Light doping for 3-cell cavity
Before doping
preliminary
preliminary
Doping using J-PARC furnace
Temperature dependency of doping effect under investigation

## Slide 12: Nb3Sn Results from FNAL
New door and heat shields
New Nb chamber, 20”diam, 82” long
Existing vacuum furnace
Epitaxial relationship observed between Nb3Sn film and Nb bulk – appears to be key clue to understand formation of thin, lossy regions – arXiv preprint to be posted soon

## Slide 13: Results of the direct cutout studies of a N-infused cavity
Nb2O5
NbN-
~15-20 nm N-rich layer
50 K
Hydrides

## Slide 14: Sample analysis at KEK
800℃ Annealing
1st N-infusion
(Failure)
2nd N-infusion
(Success)
Depth (nm)
Depth (nm)
Depth (nm)
Sample for QA of furnace runs (D- & TOF-SIMS and XPS)
Carbon and Oxygen signal maybe key to distinguish success/failure
NbN signal under investigation
Hc1 measurements with 2mm sphere sample by SQUID MPMS (N-dope < Anneal < N-infusion)

## Slide 15: Surface study of nitrogen-infused Nb samples
Normal-exit XPS
Nb
NbO
Nb-C
Nb
NbxO
Nb2O5
NbO2
Nb2XyO5-y
0°
70°
Nb
Interstitial -rich Nb
NbxO
NbxCy / Nb2XyO5-y/NbO2
NbO
Nb2O5
Systematic XPS studies
TEM investigatons confirmes
carbon-rich layer below the
surface oxide

## Slide 16: Sample Analysis: Understanding the RF performance of SRF cavities
NbN1-xOx is found on Nb baked at 140-160 °C in N atmosphere
Bulk Hc2 is increased in case of N-infusion at 140 °C and 160 °C
Higher N concentration for 140 and 160C/48hrs treatments.

## Slide 17: Nb Sample analysis at IHEP
TOF-SIMS / SEM / PPMS & MPMS
Doped samples (OTIC furnace)
SS/SIS samples

## Slide 18: Theoretical insight on the roles of disorder heterogeneity in enhancing the maximum gradients

## Slide 19: Insights from muSR
s
Theoretical Bsh
Theoretical Bc1
Recently MgB2 and Nb3Sn on niobium samples of different thickness have been tested.
Findings: A layer of a higher Tc material on niobium can enhance the field of first entry by about 40% from a field consistent with Hc1 to a field consistent with Hsh.
This enhancement does not depend on material or thickness suggesting that superheating is indeed induced in niobium by the overlayer

## Slide 20: Cornell Theory
vortex line
impurities (point defects)
Model flux pinning dynamics in Nb with random impurity distribution
Apply Gurevich QP-Heating and relation of heating parameter with mfp
Investigate f-dependency in the model
CO-Infusion
(1.3 GHz)

## Slide 21: Dunning-Kruger Effect
We are here(?)
Makes sense to merge efforts for „High Q“ and for „High G“ to „High Q at High G“?
Current results showed a strong entanglement of both topics