## Slide 1: TTC WG-2 focusing on Nb Material – Properties and Specifications
Hanau, 18.06.2018, Bernd Spaniol

## Slide 2: Hello to the TTC Meeting at Riken
As I could not join the meeting, please let me give you a warm Hello by this way.
I asked Akira Yamamoto to present our comments.
Thank you and I wish you fruitful discussions.
Best regards
Bernd Spaniol

## Slide 3: Tesla shape cavities - material and components
Products:

## Slide 4: RF SC Landscape
The Nb RF SC Landscape:
- a quite small number of players
- best prediction for Standardization
and well agreed Specifications
Nb RRR material
Producer
RF SC manufaturer
Industry
High Energy Physik
Institutes
~ 50
~ 10
6

## Slide 5: Heraeus comments to the questionnaire of the TTC Chairs
RRR smaller than 300?
- a high RRR is the assurance for material failures and process failures
- the RRR is a reference for the thermal conductivity at low temperatures
- a high thermal conductivity is leading the heat, caused by smaller imperfections, fast into the He
- all the efforts by improved cleaning, EP, BCP, N treading has been resulting in less need of extreme
high RRR values
This is describing the trend, but what is the right RRR level?

## Slide 6: Heraeus comments to the questionnaire of the TTC Chairs
Grain size:
High purity to get high RRR values vs fine grains after recrystallization
  - RRR 300 + is predicting a minimum of Interstitials and metallic impurities
  - The Interstitials and metallic impurities are acting as growing-cells for new grains during the recrystallization
  - the absence of that impurities will end in a grain growth during the recrystallization
  - We have to do a bad compromise of not fully annealing and degradation of the RRR to find the “working window” to meet
  the specifications ( RRR vs grain size vs mechanical properties)
  - Here some figures from the same Nb material with different recrystallization rate.
  - we have to decide between best RRR values vs finest grain size

## Slide 7: Heraeus comments to the questionnaire of the TTC Chairs
FG vs LG:

## Slide 8: Heraeus comments to the questionnaire of the TTC Chairs
Mechanical properties / Impurities / RRR
- the table is showing the interactions between impurities, mechanical properties and RRR value
as a result or as a prediction

## Slide 9: Heraeus comments to the questionnaire of the TTC Chairs
Impurities Ta Content:
- practically as well from the cost side, the Ta content is limited by the chosen RRR value
- the table is showing some samples how we have to reduce the Interstitials by increased Ta content to get the
same RRR result.
- calculation done for RRR 350 and for RRR 250
- a significant higher Ta content is feasible for RRR values of 250 and less, but costs will increase by additional
remelts to reduce the gases
- a significant higher Ta content for RRR > 300 will increase the cost as the No. of remelts has be increased to get
the low Interstitials level
- the higher the RRR value the more critical is the Ta content, as the gases has to reduced dramatically

## Slide 10: Heraeus comments to the questionnaire of the TTC Chairs
Cost savings:
- Ta content:
- a higher Ta content will not end in a significant cost saving, to get the same RRR value, the Interstitials has to be
reduced by additional remelts.
- a higher Ta content can ensure the stable availability of large quantities of Nb pre-material for large projects,
such as ILC
- Interstitials:
- higher content of Interstitials are ending in a cost saving, as the No. of remelts can be reduced, but the RRR
value will also be reduced
- LG:
- LG discs can be produced with a cost saving potential of about 20% compared to rolled sheets

## Slide 11: Heraeus comments to the questionnaire of the TTC Chairs
Other questions:
Temperature uniformity during the annealing process
- resistant furnaces has a typically temperature uniformity of better than 10 K in the heating zone
- inductive furnaces has a typically temperature uniformity of better than 25 K in the heating zone
The temperature uniformity in the annealed Nb parts is depending
- on the furnace load
- on the dimension of the parts
- on the heating speed from RT to the annealing temperature
- to minimize the temperature ununiformity it is usual to have a holding point before reaching the
annealing temperature to get a more homogeneous temperature distribution in the parts.

## Slide 12: Heraeus comments to the questionnaire of the TTC Chairs
Other questions:
Temperature uniformity during the annealing process
- typically annealing curve with a holding time of 30 min at 700°C to get homogeneous temperature
distribution in the Nb parts

## Slide 13: Heraeus comments to the questionnaire of the TTC Chairs
Other questions:
Damage layer:
- the thickness of a damage layer on fully annealed material could be determined by X-ray investigations
- using the “Laue” X-ray investigation, you will get a clear “Laue” picture only for
undamaged crystals
- the thickness of an damage layer could be determined by
gradually etching of the sample, as long till you find a clear “Laue” picture
- we found that effect by investigations of grain orientation on Nb RRR
but we never determined the thickness of the damage layer of sheet,
discs or tubes

## Slide 14
Heraeus comments to the questionnaire of the TTC Chairs
Thank you and
best regards
Bernd Spaniol

## Slide 15: Harmonization - Material and component reference
The influence of unusable standards:
- how wrong HARMONIZATION is opening the way to diversification
- O < 40 µg/g - C < 30 µg/g - N < 30 µg/g - H < 5 µg/g  RRR 25

## Slide 16: Harmonization - Material and component reference
The influence of usable standards:
- less discussions, less interpretation, a signpost

## Slide 17: Harmonization - Material and component reference
The influence of usable standards:
- less discussions, less interpretation, a signpost
The IEC Standard 61788-23
Will describe an international Standard on measurement of the RRR value of Nb superconductors
- measurement at 9,2 K
- measurement U vs time
- measurement with external magnetic field
- extrapolation to 4,2 K

## Slide 18: Harmonization - Material and component reference
 |  | DESY |  | Heraeus |  | KEK | FNAL |  |  | Summary 9,2 K |  |  | Summary 4,2 K |  | 
Lot 3253 |  | RRR (9.2K) | RRR (4.2K) | RRR (9.2K) | RRR (4.2K) | RRR (9,2K) | RRR (9.2K) | RRR (9.2K) | RRR (4.2K) | min (9,2K) | max (9,2K) | range (9,2K) | min (4,2K) | max (4,2K) | range (4,2K)
sample 1 |  | 367 | 399 | 370 | 402 |  |  | 365 |  | 365 | 370 | 5 | 399 | 402 | 3
sample 2 |  | 347 | 375 | 348 | 376 |  | 345 | 343 | 371 | 343 | 348 | 5 | 371 | 376 | 5
Lot 3244 |  | RRR (9.2K) | RRR (4.2K) | RRR (9.2K) | RRR (4.2K) | RRR (9.2K) | RRR (9.2K) | RRR (9.2K) | RRR (4.2K) |  |  |  |  |  | 
sample 1 |  | 391 | 427 | 390 | 426 |  |  |  |  | 390 | 391 | 1 | 426 | 427 | 1
sample 2 |  | 379 | 413 | 378 | 411 |  |  |  |  | 378 | 379 | 1 | 411 | 413 | 2
Lot 3247 |  | RRR (9.2K) | RRR (4.2K) | RRR (9.2K) | RRR (4.2K) | RRR (9.2K) | RRR (9.2K) | RRR (9.2K) | RRR (4.2K) |  |  |  |  |  | 
sample 1 |  | 417 | 458 | 418 | 460 | 417 |  |  |  | 417 | 418 | 1 | 458 | 460 | 2
sample 2 |  | 408 | 448 | 395 | 431 |  |  |  |  | 395 | 408 | 13 | 431 | 448 | 17
Lot 3259 (No 149) |  | RRR (9.2K) | RRR (4.2K) | RRR (9.2K) | RRR (4.2K) | RRR (9.2K) | RRR (9.2K) | RRR (9.2K) | RRR (4.2K) |  |  |  |  |  | 
sample 1 |  | 382 | 416 | 377 | 411 |  |  |  |  | 377 | 382 | 5 | 411 | 416 | 5
sample 2 |  | 383 | 417 | 370 | 403 |  |  |  |  | 370 | 383 | 13 | 403 | 417 | 14
Lot 3259 (No 150) |  | RRR (9.2K) | RRR (4.2K) | RRR (9.2K) | RRR (4.2K) | RRR (9.2K) | RRR (9.2K) | RRR (9.2K) | RRR (4.2K) |  |  |  |  |  | 
sample 1 |  | 344 | 372 | 328 | 354 |  |  |  |  | 328 | 344 | 16 | 354 | 372 | 18
sample 2 |  | 332 | 358 | 332 | 358 | 336 |  |  |  | 332 | 336 | 4 | 358 | 358 | 0
FNAL sample R2 |  | 376 | 409 | 355 | 385 |  |  | 375 |  | 355 | 376 | 21 | 385 | 409 | 24
FNAL sample R3 |  | 310 | 332 | 302 | 323 |  |  | 293 |  | 293 | 310 | 17 | 323 | 332 | 9
FNAL sample R4 |  | 334 | 360 | 346 | 374 |  |  | 320 |  | 320 | 346 | 26 | 360 | 374 | 14
FNAL sample R6 |  | 319 | 343 | 318 | 341 |  |  | 313 |  | 313 | 319 | 6 | 341 | 343 | 2
 |  | I) messured R vs Temperature @ 9,2 K | II) calculated from I) using TTC-Report 2010-02 | III) messured R vs time @ TC | IV) calculated from III) using TTC-Report 2010-02 | V) messured R vs Temperature @ 9,2 K | VI) messured R vs time @ TC | VII) messured R vs Temperature @ 9,2 K | VIII) messsured R vs Temperature @4,2 K using outer magnetic field |  |  |  |  |  | 

## Slide 19: Harmonization - Material and component reference
The influence of the tendering process:
- national law is applicable
- only a reduced influence on the specifications during the tendering process
- example: ESS, high beta ASTeC
- at the end the tendering was stopped and postponed

## Slide 20: Harmonization - Material and component reference
The AMICI conference, more than giving proposals:
- Questions:
how are the results of the AMICI conference being implemented in the future ?
shall there be a HARMONIZATION based on international Standards ?
IEC, CEN, CENELEC, ….. ?
- Motivation:
let´s work together to end up
with much more than a proposal

## Slide 21: Harmonization - Material and component reference
Thank You !