## Slide 1: WG2 Experience with LG Niobium SRF Cavities
K. Saito and H. Umezawa* MSU/FRIB SRF Development Manager
* Tokyo Denkai, Co. Ltd, Japan

## Slide 2: Multi-Wire Slicing Method Apply silicon wafer slicing technology for Nb Ingot
“Multi-wire slicing of Nb ingot”
K. Saito, Single Crystal-Large Grain Niobium Technology Workshop in Brazil 2006
Nb
Pressing
Splay liquid abrasives

## Slide 3: Wire Sliced Niobium Sheets from Ingot (TD)
11-13/May/2011/ K.Saito
RRR reduction by this slicing
is small, within the material
variation.
480 → 430
Degradation of RRR by this slicing is
about 10% . but it is within the location
variation of the Nb ingot.
102 sheets from 265f x 307mm long Ingot

## Slide 4
1387 ± 1.2 g
Scatter 0.09%
2.906 ± 0.038 mm
Scatter 0.13%
Very Uniform
Very Smooth
KEK 102 sheets
KEK 19 sheets
Weight of individual sheet
Thickness of individual sheet
Surface roughness of individual sheet
Feature of sliced sheet material:
Very uniform
~ 0.1% deviation in thickness
Very smooth
Rz ~ 5mm
Needless of mechanical finishing
Very fast sheet production
102 sheets within 48 hr
Feature of Sliced Nb Sheets from Ingot

## Slide 5: Sheet Cleaning after Slicing BCP and Annealing
BCP
Ultrasonic rinsing
Annealing @ 750OC
Ti box

## Slide 6: Half-Cell Deep Drawing
11-13/May/2011 K.Saito
Crack
but no issue
for fabrication

## Slide 7: Fabrication @ KEK Machine Shop
Inside equator
Welding parts were trimmed fitting structure
EBW
Trimming EBW

## Slide 8: CBP at KEK
Rough stone : 5 times
Green stone : Once
Brown stone : Once
White stone : Once
Totally ~ 200 mm removed @ equator
equator
equator
Rotated ~100rpm on a oppositely rotating table
Water
stone
Equator EBW after CBP
Equator light BCP after CBP

## Slide 9: Large Grain ICHIRO Single Cell Cavity (End-Cell) Performance
Process:
  CBP ~ 80mm, light BCP ~ 10mm, Annealing 750OC 3 hr, BCP 160mm, HPR (55 kg/cm2for 15 min), Baking 120OC for 48 hr
Reached 42.6 MV/m by BCP at the first test.
High field Q-slop (HFQS) limits the performance.
Additional BCP produces more serious HFQS.

## Slide 10: 9-Cell Cavity Performance by BCP
96mm in average BCP after CBP
Removal material distribution with vertical and horizontal BCP
Cavity performance is limited by HFQS !
DESY has a similar result with BCP.
Expected to mprove the gradient > 40 MV/m, DESY result (next slide).

## Slide 11: DESY Large Grain 9-Cell Cavity Results
Q(Eacc) of the cavities AC112-AC114: first test after about 100 mm bulk etching with BCP, annealing 800OC 2 hrs followed by light BCP of 20 mm. AC113 was quenched.
Q(Eacc) of the cavities AC112-AC114: after additional EP.
EP
BCP

## Slide 12: Merit for Large Grain for Nitrogen Doping or Infusion
Less vendor material dependence for N-doping or N-infusion cavity performance
  Nb material dependence was observed with N-doping with LCLS-II cavity performance.
  Nb material production has two category: High purity ingot production and sheet material production.
  The final material property is very sensitive to the sheet production, which is in vendor know-how.
  Slicing sheet production can ship the sheet production, as the result the vendor material dependence will be less than fine grain cavity.
Less sensitive the flux trapping during cooldown
  Large grain has less flux trapping, as the result can be expected high Qo.
  High Q quality will be controlled more easily than fine grain cavity.

## Slide 13: Summary
Cavity fabrication is no problem if use fitting structure for EBW welding parts.
The performance of the large grain cavity is limited by high field Q slop below 30 MV/m with BCP’ed 9-cell cavity, even taking 120OC baking.
However, DESY experience shows the high gradient performance > 40MV/m with EP’ed 9-cell.
Slicing technology have advantages in sheet production speed and cost, in addition with the N-doping or N-infusion cavity performance.