## Slide 1: Ingot Niobium for Efficient and Potentially Low Cost SRF Cavities
TTC Meeting 2018
26-29 June 2018
RIKEN Nishina Center
Pashupati Dhakal

## Slide 2
SRF Cavities
Performance is measured as Q0 (Eacc) Curves.
Q-factor ():
High → Lower operating cost
High → Lower construction cost
Pushing Cavity Performance Limits  High Q0, High Eacc
Gradient limitations
Critical field
Field emission
Multipacting
Q0 limitations
Rs
Process, Metallurgy and
Superconductivity

## Slide 3: SRF Cavities
SRF Cryomodule
EXFEL ~ 100 (~800 cavities) LCLS-II ~ 40 (~300 cavities) ILC ~ 1000 (~8000 cavities)
Keys for Cost reductions
Lower manufacturing/processing cost
Lower material cost
High Q and high gradient
ILC TDR

## Slide 4: ILC Machine Staging Report 2017
Work on Ingot Niobium started in 2004 at Jefferson Lab and was quickly adopted in several lab around the world.
Ingot niobium cavities have been successfully produced by industry.
Eight 9-cell cavities were installed in one X-FEL cryomodule.

## Slide 5: Ingot Niobium Cavities
JLAB Single cells
DESY 9-cell
KEK Single cells
Kneisel et al., NIMA 774, 133 (2015)
Kneisel, SRF 2007
Performance of SRF cavities built from ingot materials is comparable to that achieved using standard fine grain materials.
33 MV/m
37 MV/m
35 MV/m

## Slide 6
Processing Steps (FG vs Ingot)
Less steps  Lower manufacturing cost
 Low material cost

## Slide 7: Cost Comparison for Niobium Discs
  Fine grain low tantalum discs $1,400 from vendor A
  High tantalum ingot discs with slicing from
  vendor B: $310
Multi wire slicing
Surface finishing
Photos: courtesy Ursula Weitzel-Hoefler, Heraeus
Cut into slices in one of two ways
  Electronic Discharge Machining (EDM) with single wire
    Expensive
    Affects niobium surface quality
  Multi-wire slurry slicing
    Cost effective
    Produces the best results
    Production steps are reduced

## Slide 8: Tantalum Effect on SRF Cavity Performance
P. Kneisel, G. Myneni, G. Ciovati, D. Proch, W. Singer, T. Carneiro et al in Proceedings of PAC 2005
8
Performance of cavities is unaffected by tantalum content up to ~1300 wt. ppm

## Slide 9: Ingot Cavities with different shapes
Eacc (MV/m)
41
35
49
33
32
R. Geng et al., IPAC 15

## Slide 10: Ti/N2 Doping
First observation of Q-rise in medium purty (RRR ~106) ingot Nb, high Ta cavity
T = 2K, 1.5 GHz
T = 2K, 1.3 GHz
Bp/Eacc = 4.2
N-Doping with successive EP removal
Reduced dissipation due to the current-induced broadening of the quasiparticle density of states in dirty limit.
Gurevich, PRL (2014)

## Slide 11: Cavity Performance Vs RRR
For TESLA Cavity, Bp/Eacc = 4.2 mT/(MV/m)
FG
LG
Ciovati et al., Supercond. Sci. Technol. 29 (2016) 064002
An average quench field of ∼100 mT has been obtained in medium-purity (RRR =100–140) ingot Nb cavities at 2.0 K.
Q0-value of 2×1010 at 2 K has been obtained in medium-purity, 1.3–1.5 GHz ingot Nb cavities

## Slide 12
5C75-001
5C75-002
5C75-003
Three prototype cavities built, processed and tested “in house” (Sep. 2016 – Jan. 2017)
Two cavities (5C75-001 and 5C75-002) made from large-grain Nb discs multi-wire sliced from CBMM ingot (RRR~120, Ta = 670-1350 wt.ppm)
One cavity (5C75-003) made from large-grain Nb discs from Tokyo-Denkai (RRR = 496, Ta = 29 wt. ppm)
The limitation is fabrication/processing issues
Q0 in cryomodule is better than C50 (FG) cavities
Prototype 5-cell Ingot Cavities
G. Ciovati, TTC Milan 2018

## Slide 13: Medium-purity large-grain single-cell from KEK
Q= 2x1010 @
36 MV/m
Ta concentration = 1034 ppm

## Slide 14: RRR vs Thermal Conductivity (FG vs Ingot)
Kneisel et al., NIMA 774, 133 (2015)
Enhanced phonon peak
For better thermal stability

## Slide 15: Flux Expulsion/Trapping (LG vs FG)
Posen et al., APL 119, 213903 (2016)
Haung and Geng Phys. Rev. Accel. Beams 19, 082001
Magnetic flux trapped in superconducting niobium increases RF losses, decreasing the Q0
Nitrogen doping exacerbates this problem
Ingot material is less susceptible to this effect regardless of the RRR of Ingot materials
P. Dhakal, “Flux trapping in Large Grain Nb cavities”, TTC Topical Workshop, FNAL, 2017. To be published
Trapped flux sensitivity vs RRR (Ingot)
DT<0.1K
Flux expulsion

## Slide 16: Summary
Ingot Nb Cavities:
Material cost is ~1/4 for “TESLA spec”.
Ingot niobium can be the material of choice for high-field cavities.
Cavities made from medium purities consistently achieved > 20 MV/m with Q0 > 2x1010.
Q0 is statistically 30-40% higher than fine grain material processed with similar recipe.
Still need to focus on optimizing processing technique.
Acknowledgements
G. Ciovati, P. Kneisel, G. R. Myneni, R. Geng
and all Jefferson Lab Scientific/technical staff

## Slide 17
Nb
N2
Ti
Recipe for high Q and high gradient
Thank you !!