## Slide 1: Superconducting CH Structure Development in Mainz, Frankfurt, Darmstadt
F. Dziuba1
K. Aulenbacher1,4, W. Barth1,2, M. Basten3, M. Busch3, V. Gettmann1, M. Heilmann2, J. List1 , T. Kürzeder1, M. Miski-Oglu1, H.Podlech3, A. Rubin2, A. Schnase2, M. Schwarz3, S.Yaramyshev2
1HIM, Helmholtz Institute Mainz, Mainz, Germany
2GSI Helmholtzzentrum, Darmstadt, Germany
3IAP, Goethe Univ. Frankfurt, Frankfurt, Germany
4KPH, Johannes Gutenberg Univ., Mainz, Germany

## Slide 2: The Family of H-mode DTL Cavities
r.t. IH-DTL
r.t. CH-DTL
s.c. CH-DTL
H111
H211
H211
p-Linac prototype for GSI
340 MHz
CNAO Italy
217 MHz
1st superconducting CH prototype
360 MHz

## Slide 3: The CH Cavity
E field
H field
E field
E field along beam axis
H211 mode of ”pillbox“ cavity
Multigap drift tube cavity for the acceleration of protons and ions in the low energy range
Drift tubes are alternating connected to “+” and “-” potential
Cross-bar-H-mode cavity  CH cavity

## Slide 4: Superconducting cw-LINAC
Recent Layout of the superconducting cw-LINAC
Layout properties
Multigap CH cavities
Cavities with short lengths (<1m) and small transverse dimensions (<0.5 m)
Modular construction with 4 cryo modules
Each containing 3 CH cavities, 1 buncher, 2 solenoids
Ea= 5.5 MV/m enables compact linac design
First step Demonstrator project

## Slide 5: RF Design of the Demonstrator Cavity CH0 (based on beam dynamic design by S. Mineav 2009)
Inclined stem
Helium vessel
Static tuner
Dynamic tuner
Preparation
ports
3rd superconducting CH cavity developed at IAP
Manufacturered at Research Instruments
Most complex superconducting cavity ever been built
Bulk Niobium (RRR 300) from Tokyo Denkai

## Slide 6: Cavity Tuning
Main properties of the tuning system:
Enables slow & fast frequency adjustment
Capacitive bellow tuner
Max. mechanical displacement ±1 mm (≈ ±60 kHz)
Required force < 800 N
Lever with pivot point ratio ≈ 2:1
Gear reduction ratio 50:1
Piezo actuator ‚connected in series‘ with slow tuning unit
Required displacement of piezo ±6 µm (≈ ±360 Hz)
Rotation axis
Stepping motor
Piezo
actuator
Bellow tuner
Lever
Spindle
50 mm

## Slide 7: High Power Coupler
Coaxial antenna setup (inner conductor made from copper)
Capacitive coupling of RF power
Devided into cold & warm part by 2 ceramic windows (Al2O3), TiN coated
5 kW cw operation, cold window connected to LN2 supply
216.816 MHz operation frequency with 33 MHz bandwidth
Outer conductor
3 1/8‘‘
Bellow
Outer conductor
Diagnosis port
502.6 mm
Warm part
Inner
conductor
Cold part
300 K
Warm window
70 K
Cold window
4 K
Coupler design based on the work of S. Kazakov, Fermilab

## Slide 8: Surface Preparation at Research Instruments
Before assembly of He vessel (before 1st cold test):
1. BCP - 50 µm
2. BCP - 25 µm (after welding of static tuners)
3. BCP - 3 µm
HPR for 2 h, 12 h drying, assembly of antennas
HPR for 12 h (from both sides repectively), 12 h drying
After 1st cold test:
HPR for 12 h (from both sides repectively), 12 h drying
Final welding of He vessel
HPR only along beam axis!
No Baking!

## Slide 9: RF Conditioning of the Cavity
Uf
Ut
Ur
RF conditioning using VNA (sweep of frequency and variation of forward power)
1. Low level RF test in vertical orientation w/o He vessel at 4 K (01/2016) - Experimental setup at IAP
TLD
Temperature probes
Piezo elements
strong barrier remained for 12 h
conditioning of whole cavity took 2 days

## Slide 10: Cavity Performace at 4 K
1. RF test in vertical orientation w/o He vessel at IAP (01/2016)
Cavity was limited by field emission due to
insufficient surface preparation
HPR was not possible inside each quadrant
Beginn field emission
Cross check of RF power meters with
cavity x-ray spectrum

## Slide 11: Frequency Sensitivity (Cavity without He vessel)
Analysis of dynamic frequency variations
Operated as generator driven resonator, directed by rf control system, no tuning
Recording of VCO signal over 10 h
Very stable operation of the cavity
Max. frequency shift of ±7 Hz
Mechanical modes and corresponding VCO signal due to an excitation with a harmonic ac voltage at 4.2 K

## Slide 12: Microphonics (Cavity without He vessel)
Mechanical modes and corresponding VCO signal due to an excitation with a harmonic ac voltage at 4.2 K
Analysis of mechanical resonances
Piezo actuator to excite the cavitiy, piezo sensor to recorded mechanical amplitudes
No microphonics up to 100 Hz in VCO signal
Compensation of frequency shifts caused by higher resonances by rf control system
Not all mechanical resonances causing frequency changes
143 Hz
180 Hz
318 Hz

## Slide 13: Lorence Force Detuning (Cavity without He vessel)
Pulsed operation - 800 ms RF pulses at various field levels
Measurement of corresponding VCO signal (green curve)
K factor of -2.1 Hz/(MV/m)2 ∆f = -64 Hz at 5.5 MV/m
Forward power
Reflected power
Transmitted power
VCO signal
Ea = 5.5 MV/m

## Slide 14: Cavity Performace at 4 K
2. RF test in horizontal orientation with He vessel at GSI (10/2016)
Improved performance due to second HPR
No field emission activity
High gradient
Thermal quenching above 9.6 MV/m
@ Eamax

## Slide 15: Power Consumption
1. RF test
Rapidly increase of total losses
at Ea = 5 MV/m (Ep = 32 MV/m)
Indication for field emitter activation
Extremely reduced total losses
Minor increase of total losses
at Ea = 7.8 MV/m (Ep = 49 MV/m)
2. RF test (after second HPR)
Total losses inside the cavity

## Slide 16: Detection of Field Emitters
Dose
Dose
1. RF test
(vertical test, without He vessel)
2. RF test
(horizontal test, second HPR, with He vessel)
Integrated radiation dose after 9 h of operation at high field levels measured with thermoluminescent detectors (TLD)

## Slide 17: Demonstrator Beam Commissioning Environment
ECR
HLI-IH
HLI-RFQ
Demonstrator
Control room
LHe reservoir (3000 l)
UNILAC
The High Charge State Injector (HLI) at GSI served as an injector for the demonstrator
Experimental setup of the demonstrator at GSI
15 m
Layout of the horizontal cryo module
Superconducting
9.3 T solenoids
Support frame
Superconducting
217 MHz CH cavity
2.2 m

## Slide 18: Assembly of Acceleration String at GSI
Upgrade of clean room
Outer part: ISO8  ISO6
Inner part: ISO4
Integration into Cryostat

## Slide 19: Test of Tuning System during Beam Commissioning
Problems measuring Q0:
No calibration of He gas flow meter to measure cryogenic losses
Determining Q0 not possible
Input coupling:
Strongly over coupled to increase bandwidth
QL = 7.1 ∙ 105, ∆f = 300 Hz
1.5 kW CW max. forward power
Max. Ea = 6.4 MV/m at 1.5 kW forward power
RF control system:
Amplitude, phase and frequency control
Operation of one slow tuner (tuner 2 & 3 standby, piezos not used)
Max. displacement during operation: 500 steps – 25 µm, ∆f = 700 Hz
Stable frequency operation: 1 step/min due to change of He level
CW amplifier, 217 MHz, 5 kW
Tuning system

## Slide 20: Time of Flight Measurements Ar9+
Measurement of transient signal induced by traveling bunch
cavity RF off
cavity RF on (CW), Ea = 3.6 MV/m
Beam input parameters:
50 Hz, 5 ms (25% beam duty)
1.36 MeV/u input energy
1.5 pµA (particle current)
Beam output parameters:
Design energy of 1.86 MeV/u
95% of beam transmission
15% of trans. emittance growth
0.25 ns bunch length (∆φ = 20°)
Test is successful!
Acceleration! Energy gain of 0.5 MeV/u
Systematic scan of RF phase and amplitude

## Slide 21: Beam Energy vs. RF Phase and Amplitude Ar9+
Changing phase and amplitude of RF power enables energy variation
Beam transmission is high for most of RF phases
2.2 MeV/u reached at 830 W forward power
Energy variation 1.4 - 2.2 MeV/u  Feature of EQUUS beam dynamics

## Slide 22: Cavity Assembly, Preparation and Testing at HIM
    Infrastructure in Mainz:
    Clean room environment
    Cavity bakeout 120°C
    High Pressure Rinsing
    Setup for cavity RF testing at 4 K and 2 K
    Further improvement of cavity performance
ISO-class 4
ISO-class 6
HPR
Rinsing off axis

## Slide 23: Acknowledgements
Thank you very much for your attention!
Collaboration partners
GSI / HIM
KPH - Johannes Gutenberg University Mainz
IAP - Goethe University Frankfurt
Work supported by the BMBF, project number 05P15RFBA, MYRTE which is funded by the European Commission under Project-ID 662186 and Helmholtz International Center for FAIR.
June 2017:
First beam test

## Slide 24: GSI and the FAIR Facility
Existing GSI facility and future FAIR complex
SIS 18
p-LINAC
UNILAC
SIS 100
Production of new atmoic nuclei
Production of antiprotons
Antiproton ring
Experimental and storage ring
Existing facility
Planned facility
Experiments
100 m
Notes: Inbetriebnahme UNILAC 1975

## Slide 25: Requirements for FAIR and the SHE-Program
FAIR requirements:
high beam currents
low repetition rate (max. 3 Hz)
low duty factor (0.1 %, pulse length for SIS18 only 100 µs)
“Super Heavy Element” requirements:
relatively low beam currents
high repetition rate (50 Hz)
high duty factor (100 %, pulse length up to 20 ms)

## Slide 26: What is the advantage of a sc CH Cavity?

## Slide 27: What is the advantage of a sc CH Cavity?

## Slide 28: Commissioning of Cryomodule and Solenoids
Superconducting solenoids were ramped at 9.3 T (0.2 A/s)
Standby losses of cryostat 3 W
Transversal drift of components during cooldown ±0.15 mm (tolerance: ±0.2 mm)

## Slide 29: Fowler-Nordheim Plot
Fowler-Nordheim plot
for 2 different surface qualities

## Slide 30: RF Conditioning and Testing of Power Couplers at Room Temperature
Coupler #1
I1
I2
T1
T2
Coupler #2
Results of Coupler #2:
5 kW reached with 5 Hz, 15 ms RF pulses
Few multipacting events
CW operation limited to 2.5 kW (T1 = 81°C, T2 = 72°C)
Thermal losses at windows: P1 = 34 W, P2 = 32 W
Problems with TiN coating, too thick?
Improved power coupler in production
Master thesis of J. List, IAP, Frankfurt University

## Slide 31: Bandpass of Coupler Setup

## Slide 32
Matching Line – Demonstrator
HLI
1,4 MeV/u
R2
x | y
cw Demonstrator
R1
T
P
P
HLI provides Ar11+, Ar9+, Ar6+, He2+ @ 1,4 MeV/u
Steering magnets
Additional Re-Buncher
Quadrupole doublet
Profile Grid
Phase probes for TOF measurement
Beam current transformers for transmission measurement
Bunch shape monitor (Feschenko monitor)
Slit-Grid emittance measurement device
Transversal matching is measured in 2015
6d characterization of the beam
 Matching in 6d
T
G
BSM
Mob
EMI
P
QT
QD
QD

## Slide 33: Emittance Measurements
Ion species: 40Ar11+, 40Ar9+, 40Ar6+ (A/q=6.7),
50 Hz, 5ms, 25% beam duty, cw (rf duty), 1.5pµA (particle current),
95% (beam transmission), 0.460 MeV/u (W), transv. emittance growth 12%

## Slide 35: Next Phase: Advanced Demonstrator
New cryo module layout: CM1 containing demonstrator CH0 cavity, 2 short CH cavities CH1&2, 1 buncher and 2 solenoids
Simplified cavity design (easier manufacturing & surface processing, cost reduction)
CH1 & CH2 are already in production (delivery at 4th quarter of 2018)
Tendering for cryostat at 3rd quarter of 2018

## Slide 36: Short CH Cavity Design
 |  | 0.069
Frequency | MHz | 216.816
Cell number | # | 8
Length (βλ-definition) | mm | 381.6
Cavity diameter (outer) | mm | 400
Cell length | mm | 47.7
Aperture diameter | mm | 30
Dynamic bellow tuner | # | 2
Wall thickness | mm | 3-4
Accelerating gradient df/dp | MV/m Hz/mbar | 5.5 -13
Ep/Ea |  | 5.2
Bp/Ea | mT/(MV/m) | <10
G | Ω | 50
Ra/Q0 |  | 1070
Design parameters of short CH cavities CH1 & CH2
PhD thesis of M. Basten, IAP, Frankfurt University
CH1 w/o He vessel is currently being RF tested at 4 K @ IAP

## Slide 37: Timeline of Advanced Demonstrator Project
10/2018
11/2018
10/2020
02/2015
09/2016
11/2019
02/2020
Funding of the Advanced Demonstrator within POF3
Ordering of two short CH cavities
Tendering of cryostat, solenoids, buncher cavity
Delivery of short cavities
Delivery of cryostat, solenoids, buncher cavity
Assembly of cryomodule @ HIM
Beamtest @ GSI
User Operation
>12/2020